	Supplemental Table 1. Descriptive statistics and multiple comparison results of color changes (ΔE00) according to restorative materials and bleaching agents

	
Materials
	
	Bleaching Agents
	
Total 
	

	
	ΔE00
Evaluation Period
	Control
	Opalescence Boost (HP)
	Opalescence Quick (CP)
	
	
	Test Statistics
	px

	
Clearfil Majesty ES-2 Universal (CME)
	ΔE001
	3,53 ± 0,71ABCDEFGHİJ
	2,6 ± 0,46ABCDEFG
	4,01 ± 0,62ABCDEFGHİJ
	3,34 ± 0,36ABC
	Material
	165,000
	<0,001

	
	ΔE002
	2,68 ± 0,44ABCDEFG
	2,59 ± 0,36ABCDEFG
	2,83 ± 0,67ABCDEFGİ
	2,72 ± 0,26AB
	Bleaching
	29,200
	<0,001

	
	ΔE003
	5,4 ± 0,61ABCDEFGHİJK
	2,61 ± 0,38ABCDEFG
	2,94 ± 0,72ABCDEFGİ
	3,58 ± 0,44ABC
	Time Period
	204,200
	0,001

	
	Total 
	3,86 ± 0,43ABCD
	2,6 ± 0,21ABC
	3,23 ± 0,38ABCD
	3,18 ± 0,21a
	Material x Bleaching
	37,000
	0,002

	
Essentia Universal 
(EU)
	ΔE001
	4,35 ± 0,9ABCDEFGHİJK
	3,98 ± 0,54ABCDEFGHİJ
	5,21 ± 0,33AFHİJK
	4,44 ± 0,31CD
	Material x Time Period
	119,800
	0,001

	
	ΔE002
	2,97 ± 1,14ABCDEFGHİJK
	2,72 ± 0,45ABCDEFG
	3,22 ± 0,79ABCDEFGHİJ
	2,83 ± 0,39ABC
	Bleaching x Time Period
	27,700
	0,001

	
	ΔE003
	3,17 ± 0,3ABCDFHİJ
	3,57 ± 0,31ABFHİJ
	2,73 ± 0,34ABCDEFGH
	3,16 ± 0,19ABC
	Material x Bleaching x Time  Period
	59,400
	0,004

	
	Total 
	3,41 ± 0,47ABCD
	3,39 ± 0,25ABCD
	3,69 ± 0,37ABCD
	3,45 ± 0,19ab
	

	
Vittra Unique 
(VU)
	ΔE001
	6,31 ± 0,81ABCDEFGHİJK
	9,41 ± 0,81HJK
	8,51 ± 1,6ABCDEFGHİJK
	8,02 ± 0,69EF
	

	
	ΔE002
	4,76 ± 2,01ABCDEFGHİJK
	4,82 ± 0,67ABCDEFGHİJK
	5,98 ± 1,17ABCDEFGHİJK
	5,18 ± 0,77ABCDF
	

	
	ΔE003
	9,97 ± 1,98ABCDEFGHİJK
	11,25 ± 0,88K
	12,87 ± 1,58ABCDEFGHİJK
	11,52 ± 0,86E
	

	
	Total 
	6,96 ± 1,07ADEF
	8,5 ± 0,77E
	9,05 ± 1,05EF
	8,24 ± 0,56c
	

	
Charisma Topaz One (CT)
	ΔE001
	8,81 ± 2,3ABCDEFGHİJK
	6,46 ± 0,84ABCDEFGHİJK
	5,87 ± 1,07ABCDEFGHİJK
	6,55 ± 0,52DF
	

	
	ΔE002
	1,95 ± 0,83ABCDEFGİ
	3,25 ± 0,55ABCDEFGHİJ
	1,27 ± 0,36BCE
	2,05 ± 0,36BG
	

	
	ΔE003
	6,28 ± 0,94ABCDEFGHİJK
	3,74 ± 0,69ABCDEFGHİJ
	5,12 ± 1,01ABCDEFGHİJK
	5 ± 0,54ACDF
	

	
	Total 
	5,19 ± 0,72ABCDEF
	4,34 ± 0,5ABDF
	4,01 ± 0,69ABCDF
	4,54 ± 0,37b
	

	
OneShade (OS)
	ΔE001
	8,07 ± 0,79ADGHİJK
	2,09 ± 0,55ABCDEFG
	5,3 ± 1,24ABCDEFGHİJK
	5,11 ± 0,78ABCDF
	

	
	ΔE002
	2,29 ± 0,7ABCDEFGİ
	4,45 ± 0,67ABCDEFGHİJ
	3,15 ± 0,87ABCDEFGHİJ
	3,2 ± 0,43ABC
	

	
	ΔE003
	7,36 ± 0,54İJK
	2,78 ± 0,36ABCDEFG
	5,03 ± 0,78ABCDEFGHİJK
	5,04 ± 0,54ACDF
	

	
	Total 
	5,95 ± 0,73DEF
	2,97 ± 0,29ABCD
	4,41 ± 0,53ABCDF
	4,41 ± 0,36b
	

	
Omnichroma (OC)
	ΔE001
	6,42 ± 1,51ABCDEFGHİJK
	2,78 ± 0,66ABCDEFGİ
	2,95 ± 0,39ABCDEFGH
	3,68 ± 0,45ABC
	

	
	ΔE002
	1,67 ± 0,51BCEF
	0,56 ± 0,16EG
	0,45 ± 0,15EG
	0,77 ± 0,15G
	

	
	ΔE003
	6,76 ± 1,43ABCDEFGHİJK
	2,64 ± 0,43ABCDEFG
	4,2 ± 0,86ABCDEFGHİJK
	4,28 ± 0,57ABCD
	

	
	Total 
	4,73 ± 0,85ABCDEF
	1,9 ± 0,32C
	2,35 ± 0,39ABC
	2,85 ± 0,32a
	

	
Zenchroma (ZC)
	ΔE001
	5,91 ± 1,06ABCDEFGHİJK
	2,75 ± 0,66ABCDEFGİ
	4,51 ± 0,78ABCDEFGHİJK
	4,24 ± 0,48ABCD
	

	
	ΔE002
	0,08 ± 0CDEG
	0,11 ± 0,01CDEG
	0,18 ± 0,1EG
	0,1 ± 0,01H
	

	
	ΔE003
	6,14 ± 1,06ABCDEFGHİJK
	3,03 ± 0,68ABCDEFGİ
	4,76 ± 0,75ABCDEFGHİJK
	4,5 ± 0,47ACD
	

	
	Total 
	3,89 ± 0,84ABCDF
	1,85 ± 0,43BC
	3,06 ± 0,63ABCD
	2,85 ± 0,36a
	

	
Total
	ΔE001
	5,92 ± 0,38CE
	4,15 ± 0,45ABC
	4,99 ± 0,37BCE
	5,03 ± 0,24 α 
	

	
	ΔE002
	2,1 ± 0,39D
	2,55 ± 0,3AD
	2,21 ± 0,33D
	2,24 ± 0,18β
	

	
	ΔE003
	6,25 ± 0,49E
	3,95 ± 0,47AB
	5,1 ± 0,59BCE
	5,06 ± 0,31α
	

	
	Total 
	4,75 ± 0,28y
	3,48 ± 0,24x
	4,05 ± 0,29xy
	
	

	px based on Robust ANOVA; Multiple comparisons were analysed by Bonferroni post-hoc Test. 
ΔE1: Color change between discoloration and baseline; ΔE2: Color change between bleaching application and discoloration; ΔE3: Color change between  bleaching application and baseline; 
Mean ± Standard Error; a-c: Different lowercase letters within a column indicate statistically significant differences among materials; x-y: Different lowercase letters within a row indicate statistically significant differences among bleaching agents.; α- β: Different letters within a column indicate statistically significant differences among time periods; 
A-K: Different uppercase letters within interactions indicate statistically significant differences.



	Supplemental Table 2. Descriptive statistics and multiple comparison results of whiteness changes (ΔWID) according to restorative materials and bleaching agents

	
Materials
	
	Bleaching Agents
	
Total 
	

	
	ΔWID Evaluation Period
	Control
	Opalescence Boost (HP)
	Opalescence Quick (CP)
	
	
	Test Statistics
	px

	
Clearfil Majesty ES-2 Universal (CME)
	ΔWID1
	-3,61 ± 1,51
	-5,93 ± 1,08
	-10,24 ± 1,67
	-6,52 ± 0,88ABC
	Material
	190,140
	<0,001

	
	ΔWID2
	5,08 ± 0,85
	6,83 ± 0,61
	7,67 ± 1,54
	6,55 ± 0,61G
	Bleaching
	13,970
	0,002

	
	ΔWID3
	1,47 ± 0,98
	0,9 ± 0,69
	-2,56 ± 1,3
	0,03 ± 0,66DEF
	Time Period
	308,570
	0,001

	
	Total 
	1,07 ± 1,04A
	0,65 ± 1,37A
	-1,62 ± 1,92AB
	0,06 ± 0,82a
	Material x Bleaching
	26,610
	0,025

	
Essentia Universal 
(EU)
	ΔWID1
	-12,91 ± 1,81
	-11,82 ± 2,13
	-11,9 ± 2,09
	-12,31 ± 0,95H
	Material x Time Period
	125,020
	0,001

	
	ΔWID2
	6,67 ± 3,85
	8,34 ± 1,43
	3,82 ± 2,74
	6,05 ± 0,91Gİ
	Bleaching x Time Period
	4,830
	0,335

	
	ΔWID3
	-6,24 ± 2,26
	-3,48 ± 1,35
	-8,09 ± 0,76
	-6,26 ± 0,81AB
	Material x Bleaching x Time Period
	29,360
	0,398

	
	Total 
	-4,88 ± 1,75AB
	-2,21 ± 2,16AB
	-5,64 ± 1,98AB
	-4,29 ± 1,11bc
	

	
Vittra Unique 
(VU)
	ΔWID1
	-24,66 ± 0,85
	-26,41 ± 7,55
	-25,51 ± 4,88
	-25,41 ± 2,25J
	

	
	ΔWID2
	-2,39 ± 6,06
	2,45 ± 7,04
	-11,23 ± 1,89
	-4,8 ± 2,8ABCDEFGHİ
	

	
	ΔWID3
	-27,05 ± 5,99
	-23,96 ± 7,66
	-36,74 ± 3,8
	-30,83 ± 2,87J
	

	
	Total 
	-18,49 ± 3,72BC
	-16,38 ± 4,42ABC
	-24,72 ± 3,29C
	-20,16 ± 2,23d
	

	
Charisma Topaz One (CT)
	ΔWID1
	-15,94 ± 4,65
	-13,08 ± 2,11
	-12,04 ± 2,84
	-12,82 ± 1,26H
	

	
	ΔWID2
	0,46 ± 1,48
	5,36 ± 1,01
	2,14 ± 0,91
	2,78 ± 0,51Dİ
	

	
	ΔWID3
	-15,48 ± 6,11
	-7,72 ± 1,67
	-9,9 ± 2,58
	-9,58 ± 1,25ACH
	

	
	Total 
	-9,06 ± 2,87ABC
	-5,15 ± 2,04AB
	-6,36 ± 1,94AB
	-6,58 ± 1,11b
	

	
OneShade (OS)
	ΔWID1
	-11,49 ± 2,09
	-9,87 ± 1,16
	-10,56 ± 1,38
	-10,56 ± 0,74CH
	

	
	ΔWID2
	2,65 ± 2,13
	7,06 ± 1,63
	5,2 ± 1,47
	4,89 ± 0,94Gİ
	

	
	ΔWID3
	-8,83 ± 2,28
	-2,82 ± 0,49
	-5,36 ± 0,82
	-5,44 ± 0,95AB
	

	
	Total 
	-6,01 ± 1,84AB
	-2,03 ± 1,66AB
	-3,72 ± 1,76AB
	-3,9 ± 1,03bc
	

	
Omnichroma (OC)
	ΔWID1
	-9,2 ± 4,98
	-0,3 ± 2,84
	0,11 ± 1,24
	-1,96 ± 1,27BDEF
	

	
	ΔWID2
	0,14 ± 5,85
	-0,08 ± 1,01
	-2,72 ± 1,08
	-1,58 ± 1,24BDEF
	

	
	ΔWID3
	-9,06 ± 2,95
	-0,38 ± 2,31
	-2,61 ± 1,64
	-3,79 ± 1,43ABEF
	

	
	Total 
	-6,19 ± 1,81AB
	-0,02 ± 1,07A
	-1,54 ± 0,69A
	-2,4 ± 0,76ac
	

	
Zenchroma (ZC)
	ΔWID1
	-6,16 ± 1,26
	-4,01 ± 2,27
	-3,91 ± 2,4
	-4,59 ± 1,11ABE
	

	
	ΔWID2
	0,28 ± 0,03
	0,14 ± 0,02
	0,19 ± 0,03
	0,2 ± 0,02F
	

	
	ΔWID3
	-5,88 ± 1,24
	-3,88 ± 2,28
	-3,72 ± 2,38
	-4,39 ± 1,1ABE
	

	
	Total 
	-3,81 ± 0,92AB
	-2,15 ± 1,12AB
	-2,15 ± 1,16AB
	-2,68 ± 0,6ac
	

	
Total
	ΔWID1
	-11,42 ± 1,28
	-9,41 ± 1,38
	-10,09 ± 1,38
	-10,3 ± 0,77 α
	

	
	ΔWID2
	1,62 ± 1,15
	4,22 ± 0,85
	0,92 ± 1,07
	2,27 ± 0,59 γ
	

	
	ΔWID3
	-9,26 ± 1,76
	-5,24 ± 1,51
	-8,96 ± 1,91
	-7,63 ± 1,01 β
	

	
	Total 
	-6,25 ± 0,86y
	-3,26 ± 0,87x
	-5,66 ± 0,87xy
	
	

	[bookmark: _GoBack]px based on Robust ANOVA; Multiple comparisons were analysed by Bonferroni post-hoc Test. ΔWID1: Color change between discoloration and baseline; ΔWID2: Color change between bleaching application and discoloration; ΔWID3: Color change between bleaching application and baseline;  Mean ± Standard Error; a-d: Different lowercase letters within a column indicate statistically significant differences among materials; x-y: Different lowercase letters within a row indicate statistically significant differences among bleaching agents.; α- γ: Different letters within a column indicate statistically significant differences among time periods; A-İ: Different uppercase letters within interactions indicate statistically significant differences.



	Supplemental Table 3. Descriptive statistics and multiple comparison results of translucency parameter changes (ΔTP) according to restorative materials and bleaching agents

	
Materials
	
	Bleaching Agents
	
Total 
	

	
	ΔTP Evaluation Period
	Control
	Opalescence Boost (HP)
	Opalescence Quick (CP)
	
	
	Test Statistics
	px

	
Clearfil Majesty ES-2 Universal (CME)
	ΔTP1
	3,31 ± 1,27
	2,08 ± 0,48
	2,84 ± 1,3
	2,51 ± 0,59ABCDE
	Material
	32,300
	<0,001

	
	ΔTP2
	4,65 ± 0,66
	3,24 ± 0,86
	2,56 ± 1,01
	3,45 ± 0,5ABC
	Bleaching
	13,000
	0,003

	
	ΔTP3
	7,97 ± 1,62
	3,88 ± 0,68
	3,06 ± 0,95
	4,61 ± 0,6AB
	Time Period
	73,100
	0,001

	
	Total 
	5,01 ± 0,63A
	3,03 ± 0,41AB
	2,6 ± 0,53AB
	3,5 ± 0,33ab
	Material x Bleaching
	47,400
	0,001

	
Essentia Universal 
(EU)
	ΔTP1
	6,76 ± 1,97
	2,76 ± 1,4
	6,16 ± 0,27
	5,07 ± 0,88ABC
	Material x Time Period
	67,900
	0,001

	
	ΔTP2
	2,37 ± 0,72
	4,51 ± 0,7
	3,35 ± 0,49
	3,39 ± 0,37AB
	Bleaching x Time Period
	21,400
	0,001

	
	ΔTP3
	5,42 ± 1,06
	3,65 ± 0,51
	2,81 ± 0,31
	3,82 ± 0,42AB
	Material x Bleaching x Time Period
	33,600
	0,244

	
	Total 
	4,65 ± 0,86AB
	3,53 ± 0,5AB
	4,11 ± 0,4A
	4,01 ± 0,32a
	

	
Vittra Unique 
(VU)
	ΔTP1
	2,42 ± 0,62
	5,66 ± 1,68
	3,92 ± 1,42
	3,64 ± 0,68ABCD
	

	
	ΔTP2
	1,65 ± 0,71
	5,25 ± 1,49
	4,6 ± 1,18
	3,7 ± 0,73ABCD
	

	
	ΔTP3
	1,85 ± 0,25
	4,2 ± 1,41
	1,58 ± 0,42
	2,22 ± 0,31ACD
	

	
	Total 
	1,89 ± 0,3B
	4,8 ± 0,78AB
	3,2 ± 0,65AB
	3,21 ± 0,38ab
	

	
Charisma Topaz One (CT)
	ΔTP1
	4,04 ± 0,5
	3,03 ± 0,97
	3,25 ± 1,29
	3,28 ± 0,47ABC
	

	
	ΔTP2
	1,53 ± 0,69
	1,04 ± 0,27
	0,92 ± 0,47
	1,05 ± 0,25DE
	

	
	ΔTP3
	2,81 ± 0,69
	3,36 ± 0,74
	3,54 ± 1,07
	3,1 ± 0,38ABC
	

	
	Total 
	2,77 ± 0,41AB
	2,31 ± 0,43AB
	2,32 ± 0,59AB
	2,41 ± 0,25b
	

	
OneShade (OS)
	ΔTP1
	5,46 ± 1,24
	4,45 ± 0,74
	5,24 ± 1,29
	5,07 ± 0,61B
	

	
	ΔTP2
	1,31 ± 0,4
	1,52 ± 0,55
	3,23 ± 0,9
	1,87 ± 0,37ACD
	

	
	ΔTP3
	5,54 ± 1,06
	3,63 ± 1,01
	3,11 ± 0,52
	4,05 ± 0,52AB
	

	
	Total 
	4,05 ± 0,72AB
	3,2 ± 0,52AB
	3,75 ± 0,56AB
	3,64 ± 0,35ab
	

	
Omnichroma (OC)
	ΔTP1
	5,3 ± 0,64
	2,51 ± 0,48
	3,22 ± 0,73
	3,64 ± 0,43AB
	

	
	ΔTP2
	2,56 ± 0,47
	0,97 ± 0,19
	0,9 ± 0,27
	1,4 ± 0,26CD
	

	
	ΔTP3
	4,26 ± 0,94
	2,51 ± 0,3
	3,13 ± 0,67
	3,17 ± 0,35AB
	

	
	Total 
	3,99 ± 0,44AB
	1,93 ± 0,23B
	2,36 ± 0,4AB
	2,73 ± 0,24b
	

	
Zenchroma (ZC)
	ΔTP1
	5,8 ± 1,05
	2,55 ± 0,62
	3,63 ± 1,35
	3,87 ± 0,66ABCD
	

	
	ΔTP2
	0,18 ± 0,03
	0,17 ± 0,03
	0,15 ± 0,03
	0,17 ± 0,02E
	

	
	ΔTP3
	5,98 ± 1,05
	2,72 ± 0,62
	3,77 ± 1,36
	4,03 ± 0,66ABCD
	

	
	Total 
	3,89 ± 0,81AB
	1,76 ± 0,4B
	2,24 ± 0,73AB
	2,54 ± 0,4ab
	

	
Total
	ΔTP1
	4,54 ± 0,4C
	3,07 ± 0,33ABCD
	3,94 ± 0,44AC
	3,83 ± 0,24α
	

	
	ΔTP2
	1,92 ± 0,27D
	2,19 ± 0,36ABD
	2,08 ± 0,34BD
	2,03 ± 0,18β
	

	
	ΔTP3
	4,67 ± 0,4C
	3,33 ± 0,25ABC
	2,83 ± 0,27ABD
	3,57 ± 0,2α
	

	
	Total 
	3,66 ± 0,24y
	2,84 ± 0,19x
	2,91 ± 0,22x
	
	

	px based on Robust ANOVA; Multiple comparisons were analysed by Bonferroni post-hoc Test. ΔTP1: Color change between discoloration and baseline; ΔTP2: Color change between bleaching application and discoloration; ΔTP3: Color change between bleaching application and baseline; Mean ± Standard Error; a-b: Different lowercase letters within a column indicate statistically significant differences among materials; x-y: Different lowercase letters within a row indicate statistically significant differences among bleaching agents.; α- β: Different letters within a column indicate statistically significant differences among time periods; A-E: Different uppercase letters within interactions indicate statistically significant differences.



	Supplemental Table 4. Descriptive statistics and multiple comparison results of gloss (GU) values according to restorative materials and bleaching agents

	
Materials
	
	Bleaching Agents
	
Total 
	

	
	Time Period
	Control
	Opalescence Boost (HP)
	Opalescence Quick (CP)
	
	
	Test Statistics
	px

	
Clearfil Majesty ES-2 Universal (CME)
	T0
	41,8 ± 2,82AB
	40,1 ± 2,95AB
	40,1 ± 2,15AB
	40,8 ± 1,45ABC
	Material
	60,130
	<0,001

	
	T1
	45,8 ± 3,14AB
	48 ± 4,43AB
	35,9 ± 1,89AB
	43 ± 2,23ABCD
	Bleaching
	7,800
	0,023

	
	T2
	41,2 ± 2,51AB
	37,7 ± 1,35AB
	41,5 ± 2,03AB
	40,1 ± 1,15ABC
	Time Period
	6,960
	0,034

	
	Total 
	42,8 ± 1,49
	41,7 ± 2,01
	39 ± 1,17
	41 ± 0,94abc
	Material x Bleaching
	11,740
	0,530

	
Essentia Universal 
(EU)
	T0
	40,6 ± 2,19AB
	41 ± 1,41AB
	39,8 ± 2,68AB
	40,4 ± 1,14ABC
	Material x Time Period
	94,980
	0,001

	
	T1
	40,6 ± 2,31AB
	41,2 ± 1,52AB
	35 ± 2,11AB
	38,9 ± 1,25ABC
	Bleaching x Time Period
	5,430
	0,259

	
	T2
	42,9 ± 2,32AB
	43 ± 1,64AB
	44 ± 0,87AB
	43,6 ± 0,86ABD
	Material x Bleaching x Time Period
	65,950
	0,001

	
	Total 
	41,5 ± 1,21
	41,7 ± 0,84
	39,8 ± 1,41
	41 ± 0,69ab
	

	
Vittra Unique 
(VU)
	T0
	42 ± 1,94AB
	40 ± 2,02AB
	36,8 ± 1,72AB
	39,6 ± 1,14ABC
	

	
	T1
	41,8 ± 3,04AB
	41,3 ± 1,33AB
	40 ± 1,92AB
	41,1 ± 1,19ABC
	

	
	T2
	47,6 ± 2,18AB
	43,8 ± 2,76AB
	42 ± 1,61AB
	44,5 ± 1,29ABD
	

	
	Total 
	43,9 ± 1,35
	41,5 ± 1,18
	39,7 ± 1,08
	41,7 ± 0,73ac
	

	
Charisma Topaz One (CT)
	T0
	38,8 ± 2,2AB
	37 ± 2,16AB
	39,5 ± 2,12AB
	38,5 ± 1,19ABC
	

	
	T1
	42 ± 2,31AB
	41,6 ± 1,58AB
	45,4 ± 1,71AB
	43,1 ± 1,08ABCD
	

	
	T2
	40,7 ± 2,22AB
	49,5 ± 2,78AB
	38 ± 2,83AB
	42,9 ± 1,76ABCD
	

	
	Total 
	40,6 ± 1,21
	42,7 ± 1,71
	41,2 ± 1,35
	41,4 ± 0,81abc
	

	
OneShade (OS)
	T0
	38,9 ± 2,41AB
	36,1 ± 2,91AB
	34,3 ± 3,11AB
	36,5 ± 1,56AC
	

	
	T1
	45,1 ± 1,6AB
	42,8 ± 2,49AB
	45,2 ± 2,21AB
	44,5 ± 1,1BD
	

	
	T2
	38,4 ± 1,18AB
	45,1 ± 0,86AB
	42,1 ± 1,78AB
	42 ± 0,83ABC
	

	
	Total 
	40,9 ± 1,2
	41,4 ± 1,42
	40,7 ± 1,62
	41 ± 0,83abc
	

	
Omnichroma (OC)
	T0
	49,3 ± 2,15AB
	46,9 ± 1,74AB
	50 ± 1,61A
	48,7 ± 1,02D
	

	
	T1
	41,2 ± 2,89AB
	46 ± 2,2AB
	42,6 ± 1,36AB
	43,4 ± 1,29ABCD
	

	
	T2
	39,5 ± 1,23AB
	43,3 ± 0,96AB
	39,6 ± 1,88AB
	41 ± 0,82ABC
	

	
	Total 
	43,2 ± 1,57
	45,5 ± 0,96
	44 ± 1,16
	44,2 ± 0,7c
	

	
Zenchroma (ZC)
	T0
	35,5 ± 2,26AB
	40,9 ± 1,43AB
	37,6 ± 1,99AB
	37,9 ± 1,14AC
	

	
	T1
	41,8 ± 0,94AB
	34,2 ± 2,96AB
	41,3 ± 1,62AB
	39 ± 1,35ABC
	

	
	T2
	37,6 ± 1,32AB
	39,8 ± 1,16AB
	36,5 ± 1,45B
	38 ± 0,72C
	

	
	Total 
	38,3 ± 1,07
	38,1 ± 1,27
	38,4 ± 1
	38,3 ± 0,63b
	

	
Total
	T0
	40,8 ± 0,94
	40,3 ± 0,9
	39,7 ± 1
	40,3 ± 0,54
	

	
	T1
	42,6 ± 0,82
	42 ± 1,07
	40,8 ± 0,87
	41,8 ± 0,53
	

	
	T2
	41 ± 0,79
	43,1 ± 0,82
	40,7 ± 0,7
	41,5 ± 0,44
	

	
	Total 
	41,5 ± 0,49
	41,8 ± 0,53
	40,4 ± 0,49
	
	

	px based on Robust ANOVA; Multiple comparisons were analysed by Bonferroni post-hoc Test. T0: Baseline; T1: Following discoloration; T2: Following application of bleaching. Mean ± Standard Error; a-c: Different lowercase letters within a column indicate statistically significant differences among materials; A-D: Different uppercase letters within interactions indicate statistically significant differences among material-bleaching agent-time periods.




	Supplemental Table 5. Descriptive statistics and multiple comparison results of surface roughness (Ra/µm) values according to restorative materials and bleaching agents

	
Materials
	
	Bleaching Agents
	
Total 
	

	
	Time Period
	Control
	Opalescence Boost (HP)
	Opalescence Quick (CP)
	
	
	Test Statistics
	px

	
Clearfil Majesty ES-2 Universal (CME)
	T0
	0,25 ± 0,1
	0,46 ± 0,21
	0,27 ± 0,16
	0,29 ± 0,08
	Material
	41,070
	<0,001

	
	T1
	0,31 ± 0,04
	0,3 ± 0,08
	0,22 ± 0,05
	0,27 ± 0,03
	Bleaching
	2,600
	0,280

	
	T2
	0,22 ± 0,07
	0,41 ± 0,09
	0,25 ± 0,09
	0,29 ± 0,05
	Time Period
	1,630
	0,447

	
	Total 
	0,25 ± 0,04
	0,36 ± 0,07
	0,22 ± 0,05
	0,27 ± 0,03c
	Material x Bleaching
	21,120
	0,092

	
Essentia Universal 
(EU)
	T0
	0,25 ± 0,1
	0,48 ± 0,16
	0,12 ± 0,04
	0,26 ± 0,06
	Material x Time Period
	6,440
	0,910

	
	T1
	0,2 ± 0,08
	0,42 ± 0,11
	0,2 ± 0,09
	0,26 ± 0,05
	Bleaching x Time Period
	6,070
	0,211

	
	T2
	0,23 ± 0,12
	0,09 ± 0,01
	0,24 ± 0,11
	0,16 ± 0,05
	Material x Bleaching x Time Period
	20,260
	0,801

	
	Total 
	0,2 ± 0,05
	0,31 ± 0,07
	0,17 ± 0,04
	0,23 ± 0,03bc
	

	
Vittra Unique 
(VU)
	T0
	0,12 ± 0,1
	0,18 ± 0,14
	0,14 ± 0,09
	0,11 ± 0,05
	

	
	T1
	0,13 ± 0,08
	0,22 ± 0,2
	0,28 ± 0,13
	0,17 ± 0,06
	

	
	T2
	0,18 ± 0,12
	0,19 ± 0,1
	0,27 ± 0,15
	0,18 ± 0,06
	

	
	Total 
	0,12 ± 0,05
	0,15 ± 0,07
	0,2 ± 0,06
	0,15 ± 0,03abc
	

	
Charisma Topaz One (CT)
	T0
	0,18 ± 0,07
	0,24 ± 0,1
	0,16 ± 0,07
	0,18 ± 0,04
	

	
	T1
	0,31 ± 0,11
	0,21 ± 0,06
	0,21 ± 0,09
	0,22 ± 0,04
	

	
	T2
	0,28 ± 0,11
	0,15 ± 0,06
	0,22 ± 0,1
	0,21 ± 0,05
	

	
	Total 
	0,24 ± 0,05
	0,19 ± 0,04
	0,19 ± 0,05
	0,2 ± 0,03bc
	

	
OneShade (OS)
	T0
	0,08 ± 0,05
	0,03 ± 0
	0,08 ± 0,04
	0,05 ± 0,02
	

	
	T1
	0,22 ± 0,08
	0,09 ± 0,03
	0,13 ± 0,04
	0,13 ± 0,03
	

	
	T2
	0,16 ± 0,06
	0,08 ± 0,03
	0,14 ± 0,06
	0,12 ± 0,03
	

	
	Total 
	0,14 ± 0,03
	0,06 ± 0,02
	0,11 ± 0,03
	0,1 ± 0,02a
	

	
Omnichroma (OC)
	T0
	0,1 ± 0,07
	0,18 ± 0,12
	0,11 ± 0,05
	0,1 ± 0,03
	

	
	T1
	0,2 ± 0,08
	0,18 ± 0,06
	0,1 ± 0,02
	0,15 ± 0,03
	

	
	T2
	0,21 ± 0,09
	0,17 ± 0,04
	0,12 ± 0,04
	0,15 ± 0,03
	

	
	Total 
	0,15 ± 0,04
	0,15 ± 0,03
	0,1 ± 0,02
	0,13 ± 0,02ab
	

	
Zenchroma (ZC)
	T0
	0,12 ± 0,07
	0,26 ± 0,13
	0,09 ± 0,02
	0,13 ± 0,05
	

	
	T1
	0,19 ± 0,06
	0,24 ± 0,09
	0,24 ± 0,07
	0,22 ± 0,04
	

	
	T2
	0,1 ± 0,02
	0,17 ± 0,11
	0,29 ± 0,13
	0,16 ± 0,05
	

	
	Total 
	0,12 ± 0,03
	0,21 ± 0,06
	0,18 ± 0,04
	0,17 ± 0,03abc
	

	
Total
	T0
	0,14 ± 0,03
	0,23 ± 0,05
	0,11 ± 0,02
	0,15 ± 0,02
	

	
	T1
	0,21 ± 0,03
	0,21 ± 0,03
	0,18 ± 0,03
	0,2 ± 0,02
	

	
	T2
	0,18 ± 0,03
	0,16 ± 0,03
	0,19 ± 0,03
	0,18 ± 0,02
	

	
	Total 
	0,17 ± 0,02
	0,2 ± 0,02
	0,16 ± 0,02
	
	

	px based on Robust ANOVA; Multiple comparisons were analysed by Bonferroni post-hoc Test. T0: Baseline; T1: Following discoloration; T2: Following application of bleaching. Mean ± Standard Error; a-c: Different lowercase letters within a column indicate statistically significant differences among materials.





	Supplemental Table 6. Descriptive statistics and multiple comparison results of microhardness (VHN/HV) values according to restorative materials and bleaching agents

	
Materials
	
	Bleaching Agents
	
Total 
	

	
	Time Period
	Control
	Opalescence Boost (HP)
	Opalescence Quick (CP)
	
	
	Test Statistics
	px

	
Clearfil Majesty ES-2 Universal (CME)
	T0
	38,4 ± 0,62
	35,1 ± 0,7
	37,8 ± 1,04
	37,1 ± 0,54A
	Material
	1657,880
	<0,001

	
	T1
	38,6 ± 0,38
	37,1 ± 0,81
	37,6 ± 0,57
	37,7 ± 0,37A
	Bleaching
	7,310
	0,029

	
	T2
	45,9 ± 1,1
	46,7 ± 3,02
	48 ± 0,82
	46,5 ± 0,69BC
	Time Period
	70,410
	0,001

	
	Total 
	40,7 ± 0,89AB
	38,8 ± 1,17A
	40,9 ± 1,22ABC
	40,2 ± 0,65a
	Material x Bleaching
	28,910
	0,014

	
Essentia Universal 
(EU)
	T0
	41,1 ± 1,28
	43 ± 1,04
	41,7 ± 1,25
	41,9 ± 0,67D
	Material x Time Period
	95,080
	0,001

	
	T1
	36,8 ± 0,62
	37,4 ± 1,7
	37,1 ± 1,62
	37 ± 0,75A
	Bleaching x Time Period
	5,240
	0,281

	
	T2
	42,6 ± 1,81
	45,7 ± 1,73
	42,5 ± 2,08
	43,5 ± 1,03BD
	Material x Bleaching x Time Period
	11,550
	0,992

	
	Total 
	40,1 ± 0,92AB
	42 ± 1,13ABCD
	40,3 ± 0,94AB
	40,8 ± 0,55a
	

	
Vittra Unique 
(VU)
	T0
	52,1 ± 4,08
	40,9 ± 3,42
	46,5 ± 4,35
	46,5 ± 2,45ABCDEF
	

	
	T1
	55,8 ± 4,98
	51,1 ± 4,62
	52,6 ± 3,79
	52,7 ± 2,48BCEFG
	

	
	T2
	54,7 ± 4,59
	52,6 ± 5,8
	57,9 ± 3,6
	54,3 ± 2,46CEFG
	

	
	Total 
	54,1 ± 2,4EFG
	47,3 ± 2,56ABCDEF
	52,4 ± 2,28EF
	51,3 ± 1,43bc
	

	
Charisma Topaz One (CT)
	T0
	61,6 ± 3
	60,7 ± 0,96
	63,2 ± 1,85
	62,2 ± 0,98GHİ
	

	
	T1
	73,1 ± 3,17
	69,9 ± 2,27
	70,9 ± 2,25
	71,1 ± 1,41J
	

	
	T2
	67,2 ± 3,32
	64,6 ± 2,62
	70,3 ± 1,47
	67,4 ± 1,38HJ
	

	
	Total 
	67,4 ± 1,89H
	64,9 ± 1,36H
	68,3 ± 1,2H
	66,8 ± 0,88d
	

	
OneShade (OS)
	T0
	62 ± 1,23
	61,1 ± 1,51
	60,5 ± 1,5
	61,2 ± 0,76Gİ
	

	
	T1
	67 ± 3,37
	66,9 ± 5,52
	67,9 ± 2,89
	68,2 ± 1,69HİJ
	

	
	T2
	66,6 ± 1,87
	64,6 ± 4,7
	70,8 ± 2,31
	68,1 ± 1,3HJ
	

	
	Total 
	64,8 ± 1,37H
	64,8 ± 2,26GH
	66,3 ± 1,6H
	65,6 ± 0,88d
	

	
Omnichroma (OC)
	T0
	46,9 ± 2,23
	48,5 ± 1,93
	46,5 ± 1,73
	47,2 ± 1,08BCE
	

	
	T1
	42,7 ± 3,24
	47,6 ± 3,64
	43,6 ± 1,56
	44,5 ± 1,61BCD
	

	
	T2
	49,9 ± 2,54
	53,9 ± 2,33
	55,9 ± 2,92
	53,4 ± 1,4EF
	

	
	Total 
	46,7 ± 1,57BCDE
	50 ± 1,57EF
	48,4 ± 1,65CDEF
	48,3 ± 0,9b
	

	
Zenchroma (ZC)
	T0
	53,2 ± 2,07
	46,2 ± 2,19
	52,2 ± 2,57
	50,7 ± 1,44CEF
	

	
	T1
	56,7 ± 3,23
	46,9 ± 2,21
	55 ± 2,98
	52,7 ± 1,74CEF
	

	
	T2
	57,8 ± 3,05
	53,6 ± 2,78
	56,9 ± 4,08
	56,1 ± 1,74FG
	

	
	Total 
	55,8 ± 1,56FG
	48,6 ± 1,46DEF
	54,8 ± 1,83EFG
	53,1 ± 0,99c
	

	
Total
	T0
	50,7 ± 1,59
	47,8 ± 1,58
	49,7 ± 1,57
	49,4 ± 0,91α
	

	
	T1
	52,5 ± 2,31
	50,6 ± 2,21
	51,8 ± 2,17
	51,6 ± 1,27α
	

	
	T2
	54,7 ± 1,69
	54,1 ± 1,59
	57,5 ± 1,78
	55,4 ± 0,98β
	

	
	Total 
	52,5 ± 1,07
	50,8 ± 1,06
	52,9 ± 1,1
	
	

	px based on Robust ANOVA; Multiple comparisons were analysed by Bonferroni post-hoc Test. T0: Baseline; T1: Following discoloration; T2: Following application of bleaching. Mean ± Standard Error; a-d: Different lowercase letters within a column indicate statistically significant differences among materials; α-β:  Different letters within a column indicate statistically significant differences among time periods; A-J: Different uppercase letters within interactions indicate statistically significant differences.



