Effects of different numbers of micro-osteoperforations on acceleration of orthodontic tooth movement and alveolar bone remodeling in rats

Yingyu Chen, Mao Liu , Fan Yang , Yi Lu, Di Jiang , Bin Wu , and Bin Yan

Address correspondence to: Bin Yan, Department of Orthodontics, The Affiliated Stomatological Hospital of Nanjing Medical University, 1 Shanghai St, Gulou District, Nanjing 210029, China; Tel: 86-025-85031982; Fax:86-025-86516414; e-mail: byan@njmu.edu.cn

Supplementary Table

Note: Table S1–Table S10 presents data on OTM, trabecular parameters, Raman spectroscopy, and nanoindentation, with values expressed as mean ± standard deviation‌.

Table S1. Tukey’s post hoc test results (p values) for OTM distance in different MOPs groups

| ‌Intergroup comparisons | Time points |  |  |
| --- | --- | --- | --- |
|  | 3 days | 7 days | 14 days |
| OTM vs 2MOP | 0.5480 | 0.0889 | 0.0044 |
| OTM vs 3MOP | 0.0005 | 0.0029 | 0.0010 |
| OTM vs 4MOP | 0.0011 | 0.0033 | 0.0010 |
| 2MOP vs 3MOP | 0.0022 | 0.0233 | 0.0240 |
| 2MOP vs 4MOP | 0.0039 | 0.0223 | 0.0549 |
| 3MOP vs 4MOP | 0.9856 | 0.9955 | 0.8020 |

Table S2. The OTM rate (μm/day) at each time period in different MOPs groups

| ‌Group | Time periods |  |  |
| --- | --- | --- | --- |
|  | 0-3 days | 4-7 days | 8-14 days |
| OTM | 7.8±2.8 | 5.7±1.5 | 8.4±1.7 |
| 2MOP | 9.7±1.6 | 8.3±1.8 | 18.3±2.7 |
| 3MOP | 20.3±3.9 | 13.8±3.1 | 27.3±4.9 |
| 4MOP | 21.1±4.5 | 14.2±3.3 | 23.6±4.8 |

Table S3. The ‌alveolar bone BV/TV (%) at each time point in different MOPs groups

| ‌Group | Time points |  |  |
| --- | --- | --- | --- |
|  | 3 days | 7 days | 14 days |
| OTM | 76.5±9.5 | 71.7±6.5 | 70.0±8.9 |
| 2MOP | 63.3±10.1 | 66.1±4.0 | 66.5±6.5 |
| 3MOP | 67.4±6.9 | 60.2±5.3 | 79.9±2.9 |
| 4MOP | 69.2±6.4 | 71.0±6.8 | 78.6±5.2 |

Table S4. The ‌alveolar bone Po(tot) (%) at each time point in different MOPs groups

| ‌Group | Time points |  |  |
| --- | --- | --- | --- |
|  | 3 days | 7 days | 14 days |
| OTM | 23.5±9.5 | 29.8±7.3 | 30.0±8.9 |
| 2MOP | 36.7±10.1 | 33.9±4.0 | 33.5±6.5 |
| 3MOP | 32.6±6.9 | 38.2±5.4 | 20.5±3.6 |
| 4MOP | 30.8±6.4 | 29.0±6.8 | 22.2±3.9 |

Table S5. The ‌alveolar bone Tb.Sp (μm) at each time point in different MOPs groups

| ‌Group | Time points |  |  |
| --- | --- | --- | --- |
|  | 3 days | 7 days | 14 days |
| OTM | 6.1±1.5 | 7.1±2.5 | 5.8±1.2 |
| 2MOP | 7.1±1.2 | 6.8±1.2 | 7.1±2.5 |
| 3MOP | 5.8±1.2 | 7.8±1.5 | 4.3±1.0 |
| 4MOP | 6.4±1.4 | 6.2±2.1 | 4.3±1.4 |

Table S6. The ‌alveolar bone Tb.Th (μm) at each time point in different MOPs groups

| ‌Group | Time points |  |  |
| --- | --- | --- | --- |
|  | 3 days | 7 days | 14 days |
| OTM | 9.5±2.0 | 8.8±1.4 | 8.5±1.0 |
| 2MOP | 8.0±1.4 | 8.3±0.9 | 8.2±1.3 |
| 3MOP | 7.2±0.6 | 8.2±1.0 | 7.8±0.5 |
| 4MOP | 8.7±0.8 | 8.0±1.2 | 7.7±2.1 |

Table S7. The mineral-to-matrix ratio at each time point in different MOPs groups

| ‌Group | Time points |  |  |
| --- | --- | --- | --- |
|  | 3 days | 7 days | 14 days |
| OTM | 6.29 ± 0.42 | 3.79 ± 0.33 | 4.35 ± 0.16 |
| 2MOP | 5.75 ± 0.51 | 3.31 ± 0.11 | 4.78 ± 0.32 |
| 3MOP | 5.11 ± 0.65 | 2.99 ± 0.24 | 5.62 ± 0.23 |
| 4MOP | 5.70 ± 0.36 | 3.57 ± 0.35 | 5.02 ± 0.38 |

Table S8. The carbonate substitution index at each time point in different MOPs groups

| ‌Group | Time points |  |  |
| --- | --- | --- | --- |
|  | 3 days | 7 days | 14 days |
| OTM | 0.05±0.01 | 0.10±0.01 | 0.10±0.02 |
| 2MOP | 0.05±0.01 | 0.09±0.02 | 0.08±0.00 |
| 3MOP | 0.07±0.01 | 0.08±0.01 | 0.10±0.01 |
| 4MOP | 0.06±0.01 | 0.08±0.01 | 0.08±0.01 |

Table S9. The elastic modulus (Gpa) at each time point in different MOPs groups

| ‌Group | Time points |  |  |
| --- | --- | --- | --- |
|  | 3 days | 7 days | 14 days |
| OTM | 21.59 ± 1.04 | 18.26 ± 1.32 | 21.87 ± 0.46 |
| 2MOP | 20.16 ± 0.56 | 16.84 ± 0.88 | 21.50 ± 0.39 |
| 3MOP | 22.14 ± 0.88 | 18.30 ± 0.55 | 22.50 ± 1.10 |
| 4MOP | 20.59 ± 0.53 | 18.50 ± 1.37 | 22.93 ± 0.48 |

Table S10. The hardness (Gpa) at each time point in different MOPs groups

| ‌Group | Time points |  |  |
| --- | --- | --- | --- |
|  | 3 days | 7 days | 14 days |
| OTM | 0.88±0.05 | 0.81±0.04 | 0.81±0.07 |
| 2MOP | 0.89±0.05 | 0.75±0.05 | 0.88±0.03 |
| 3MOP | 0.85±0.06 | 0.73±0.02 | 0.95±0.07 |
| 4MOP | 0.86±0.04 | 0.73±0.08 | 0.99±0.10 |

| Table S11.Correlation between mineral-to-matrix ratio and biomechanical properties stratified by experimental group. |  |  |  |  |
| --- | --- | --- | --- | --- |
| Group | Comparison | N | r | p-value |
| OTM | Mineral/Matrix vs. Elastic Modulus | 18 | 0.514 | 0.029 |
| OTM | Mineral/Matrix vs. Hardness | 18 | 0.610 | 0.007 |
| 2MOP | Mineral/Matrix vs. Elastic Modulus | 18 | 0.704 | 0.001 |
| 2MOP | Mineral/Matrix vs. Hardness | 18 | 0.742 | < 0.001 |
| 3MOP | Mineral/Matrix vs. Elastic Modulus | 18 | 0.843 | < 0.001 |
| 3MOP | Mineral/Matrix vs. Hardness | 18 | 0.871 | < 0.001 |
| 4MOP | Mineral/Matrix vs. Elastic Modulus | 18 | 0.560 | 0.016 |
| 4MOP | Mineral/Matrix vs. Hardness | 18 | 0.465 | 0.052 |

Note: normality of the data was assessed using the Shapiro-Wilk test. Pearson correlation analysis was applied for data meeting the normality assumption; otherwise, Spearman rank correlation analysis was used; All correlations were statistically significant at p < 0.05; Mineral/Matrix: mineral-to-matrix ratio; r: correlation coefficient.

Supplementary Figure

Supplementary Figure 1. Correlation between mineral-to-matrix ratio and biomechanical properties. (A-D) Scatter plots illustrating the correlation between the mineral-to-matrix ratio and elastic modulus. (E-H) Scatter plots illustrating the correlation between the mineral-to-matrix ratio and hardness. (A-H) Data are stratified by experimental group (OTM, 2MOP, 3MOP, 4MOP). Each dot represents an individual sample, with n = 18 per group (combining samples from all three time points).