Table S1. Materials used in the study (manufacturer-reported composition and lot numbers

| Category / Use | Material (trade name) | Manufacturer (Country) | Manufacturer-reported composition | Lot No. |
| --- | --- | --- | --- | --- |
| CAD/CAM subtractive material (milling) | NanoKsa G-Plus Disc | INOX MENA Co. (USA) | High-performance polymers with nano-zirconia and carbon | 4293 |
| Additive material (3D printing) | NanoKsa G-Plus resin | INOX MENA Co. (USA) | Resin filled with high-performance polymers (HPP), nano-zirconia and carbon | 4293 |
| Finishing & polishing system | Sof-Lex Finishing & Polishing System | 3M/ESPE, St Paul, MN (USA) | Urethane-coated abrasive discs containing aluminum oxide grits (coarse to superfine; color-coded) | 7982 |
| Luting agent (cementation) | RelyX U200 (dual-cure, self-adhesive resin cement) | 3M ESPE Dental Products (USA) | Methacrylate monomers containing phosphoric acid groups, methacrylate monomers, silanated fillers, initiator components, stabilizers, rheologic additives, alkaline fillers, pigments | 714236 |
| Staining medium | Nescafé Classic | Nestlé (Switzerland) | Instant coffee (roasted coffee beans, spray-dried) | 6221007 |