Additional Information

Additional file 1: Table S1 - Cr K-edge fitting results for the local structure of chromate adsorbed to ferrihydrite based on the monodentate and bidentate two-complex model. The fitting was evaluated with a reduced χ2 = 7.32 and a goodness of fit (R-factor) of 0.009.

| Path | Na | R (Å) | σ2 (Å2)b |
| --- | --- | --- | --- |
| Cr→O | 4.0 | 1.65 | 0.0014 |
| Cr→O→O | 12.0 | 3.00 | 0.0014 |
| Cr→Fe | 0.7 | 3.35 | 0.0107 |
| Cr→Fe | 0.4 | 3.58 | 0.0107 |

a N values for Cr-O single and multiple scattering paths were fixed to theoretical values.

b Global value floated for each Fe path.

Additional file 1: Table S2 - Frequency correlations with various exchange correlation functionals using the 6-311+G(d,p) basis set. Note values are not listed for the outer-sphere models because calculated frequencies only match with one observed frequency near 955 cm-1.

Slope	Intercept	R2	Residual Sum of Squares

Bidentate binuclear

B3LYP	1.25±0.14	-237±125	0.95	1473

M06-2X	1.30±0.12	-243±106	0.95	1359

PBE0	1.47±0.08	-400±71	0.98	604

Bidentate binuclear (B)

B3LYP	0.87±0.09	118±79	0.94	912

M06-2X	0.99±0.04	18±37	0.99	136

PBE0	0.81±0.18	163±157	0.86	1007

Monodentate

B3LYP	0.97±0.07	15±65	0.97	624

M06-2X	1.27±0.21	-227±188	0.85	4398

PBE0	0.94±0.08	48±66	0.97	397