Additional information

Ultrasensitive haptoglobin biomarker detection based on amplified chemiluminescence of magnetite nanoparticles

Narsingh R. Nirala1, Yifat Harel2, Jean-Paul Lellouche2, Giorgi Shtenberg1*

1 Institute of Agricultural Engineering, ARO, the Volcani Center, Bet Dagan 50250, Israel

2 Department of Chemistry, Nanomaterials Research Center, Institute of Nanotechnology & Advanced Materials (BINA), Bar-Ilan University, Ramat-Gan 5290002, Israel

*Corresponding author: giorgi@agri.gov.il

Table S1.  Peak area comparison of amide bonds vs. Fe-O for the different MNPs modifications obtained by ATR-FTIR

| Sample | Peak Area |  | Ratio (υ(amide I and II)υ(Fe-O)) |
| --- | --- | --- | --- |
|  | υ(amide I and II)a | υ(Fe-O)b |  |
| MNPs | 2.16 | 6.17 | 0.35 |
| G-MNPs | 3.92 | 2.33 | 1.68 |
| Hb-MNPs | 3.55 | 0.65 | 5.46 |

a 1474-1709 cm-1.

b 479-603 cm-1.

Table S2. MNPs size distribution obtained by DLS

| Sample |  | Averaged diameter (nm) |
| --- | --- | --- |
| MNPs |  | 211±6 |
| G-MNPs |  | 469±31 |
| Hb-MNPs |  | 535±173 |

Data are reported as mean ± SD (n = 3).

Table S3. Hb binding efficiency to MNPs surface

| Hb (µg mL-1) |  | Added Hb (µg) | Washed Hb a (µg) | Immobilized Hb b (µg) |
| --- | --- | --- | --- | --- |
| 1 |  | 0.2 | N/A * | N/A |
| 10 |  | 2 | 1.4±0.4 | 0.6±0.4 |
| 100 |  | 20 | 13.6±1.4 | 6.4±1.4 |

a Quantified by the Bradford dye-binding method.

b Immobilized Hb content per 0.49 mg magnetite.

* Below linear quantification range.

Figure S1. CL values of the magnetic bioassay for three concentrations of Hb catalyst (1, 10, and 100 µg mL-1) within dissimilar milk samples qualities: healthy (H), cattle sick (CS, representing clinical mastitis) and in buffer (Hb-MNPs used as a positive control). Data are reported as mean ± SD (n ≥ 3). * Statistically different (t-test, p<0.05).

Figure S2. (a) CL signal stability of the Hb-MNPs bioassay within healthy milk sample (H) used for blocking (insignificant Hp content) and spiked Hp (0.005 µg mL-1) in buffer and milk, respectively; (b) The corresponding averaged CL data. Data are reported as mean ± SD (n ≥ 3).

Figure S3. Calibration curve of the CL bioassay for standard Hp concentrations based on Hb-MNPs in buffer.

Table S4. Hp concentrations in spiked buffer and milk samples using Hb-MNPs CL emission system in comparison to bovine ELISA

| Spiked Hp (µg mL-1) | Hp Hb-MNPS (µg mL-1) | Hp ELISA (µg mL-1) |  |  | CL Recovery (%) | ELISA Recovery (%) | Deviation (%) b |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0050 in buffer | 0.0060±0.0002 a | 0.0046±0.0002 |  |  | 120 | 92 | 130 |
| 0.0050 in milk | 0.0069±0.0008 | 0.0052±0.0002 |  |  | 138 | 104 | 133 |

a Calculated based on calibration curve in buffer conditions (milk-free assay, Figure S3).

b Recovery of Hp output obtained by CL emission system with respect to bovine ELISA.