Additional file

# Exosome-based biomimetic nanoparticles targeted to inflamed joints for enhanced treatment of rheumatoid arthritis

Yan Feili #1, Zhong Zhirong #1, Wang Yao #1, Feng Yue 2,3, Mei Zhiqiang 4, Li Hui 1, Chen Xiang 1, Cai Liang *2,3, Li Chunhong *1,5

1Department of Pharmaceutical Sciences, School of Pharmacy, Southwest Medical University, Luzhou 646000, Sichuan, China.

2Department of Nuclear medicine, The Affiliated Hospital of Southwest Medical University, Luzhou, Sichuan, 646000, China.

3Nuclear Medicine and Molecular Imaging Key Laboratory of Sichuan Province, Luzhou, Sichuan, 646000, China.

4The Research Center for Preclinical Medicine, Southwest Medical University, Luzhou, Sichuan 646000, China.

5Engineering Research Center in Biomaterials, Sichuan University, Chengdu, Sichuan, 610064, P. R. China.

Corresponding author: Cai Liang

E-mail: cllc131420@sina.com

Tel: +86 18982702720

Fax numbers: +86 08306302050

Mail address: Department of Nuclear medicine, The Affiliated Hospital of Southwest Medical University, 3-319 Zhongshan Road, Luzhou, Sichuan 646000, People’s Republic of China.

Corresponding author: Li Chunhong

E-mail: lispringhong@126.com

Tel: +86 13679696586

Fax numbers: +86 08306302050

Mail address: Department of Pharmaceutical Sciences, School of Pharmacy, Southwest Medical University, 3-319 Zhongshan Road, Luzhou, Sichuan 646000, People’s Republic of China.

Yan Feili, Zhong Zhirong and Wang Yao contributed equally to this work.

# SUPPLEMENTARY SCHEMES AND FIGURES

Fig. S1

Fig. S2

# SUPPLEMENTARY METHOD

## Materials

Folic acid (FA) was supplied by the Solarbio science & Technology Co., Ltd (Beijing, China). N-hydroxysuccinimide (NHS) and dicyclohexylcarbodiimide (DCC) were purchased from Chengdu Runze Local Chemical Co., Ltd (Chengdu, China). Chol-PEG-NH2 (MWCO 2000 Da) was obtained from Melo Technology (Shenzheng China). Others chemical reagents and solvents were of analytic grade.

## Synthesis of FA-NHS Ester

N-hydroxysucci-mide (NHS) and dicyclohexylcarbodiimide (DCC) were used to activate the carboxylate group of FA [1]. Briefly, 1 g of FA was dissolved in 50 mL dimethyl sulfoxide (DMSO). Then, 1.2 ratio molar excess of NHS and DCC were added to the solution, which was stirred for 24 h at room temperature under shielding from light. Next, the by-product was removed by filtration and supernatant was freeze-dried. Finally, 1H-NMR of FA-NHS ester was analyzed by Nuclear Magnetic Resonance Spectra (400 MHz, DMSO-d6).

Figure S3

## Preparation of FA-PEG-Chol Conjugate

Furthermore, FA-NHS ester was reacted with PEG-Chol-NH2 to form FA-PEG-Chol as following method. FA-NHS, 161.5 mg (0.3 mm), mixed with 503 mg (0.2 mm）of Chol-PEG-NH2 was dissolved in 10 mL DMSO and reacted under nitrogen atmosphere at room temperature for 5 h [1,2]. Then 20 mL of acetone was added to dilute the resultant solution, which was further centrifuged at 4000 rpm for 10 min. Next, the supernatant was dialyzed against water for three times (MWCO 2000Da) and then it was freeze-dried [3]. Finally, the structure of FA-PEG-Chol was determined using 1H-NMR spectroscopy (400 MHz, DMSO-d6).

Figure S4

# REFERENCE FOR SUPPORT MATERIAS

- Güliz Ak, Sanlıer SH. Synthesis of folate receptor-targeted and doxorubicin-coupled chemotherapeutic nanoconjugate and research into its medical applications. Prep Biochem Biotechnol. 2013; 42: 551-563.

- Puchkov PA, Shmendel EV, Luneva AS, Morozova NG, Zenkova MA, Maslov MA. Design, synthesis and transfection efficiency of a novel redox-sensitive polycationic amphiphile. Bioorg Med Chem Lett. 2016; 26: 5911-5915.

- Malhi SS, Budhiraja A, Arora S, Chaudhari KR, Nepali K, Kumar R. Intracellular delivery of redox cycler-doxorubicin to the mitochondria of cancer cell by folate receptor targeted mitocancerotropic liposomes. Int J Pharm. 2012; 432: 63-74.