LRP1-mediated pH-sensitive polymersomes facilitate combination therapy of glioblastoma in vitro and in vivo

Chen He1, Zhiyuan Zhang2, Yinan Ding1, Kangli Xue1, Xihui Wang1, Rui Yang3, Yanli An1, Dongfang Liu1, Chunmei Hu4* and Qiusha Tang1*

1Medical School of Southeast University, 87 Dingjiaqiao Road, Nanjing, China.

2Department of Neurosurgery, Nanjing Jinling hospital, Nanjing University , Nanjing, China.

3Research Institute for Reproductive Health and Genetic Diseases, The Affiliated Wuxi Maternity and Child Health Care Hospital of Nanjing Medical University, Wuxi , China.

4Department of Tuberculosis, the Second Affiliated Hospital of Southeast University (the second hospital of Nanjing), Nanjing, China

*Correspondence:

Chunmei Hu and Qiusha Tang

Department of Tuberculosis, the Second Affiliated Hospital of Southeast University (the second hospital of Nanjing), Nanjing, China

Medical School of Southeast University, 87 Dingjiaqiao Road, Nanjing, China.

hcm200702@163.com, panyixi-tqs@163.com

Fig. S1. Characterization of AuNPs, AuNPs-NH2. TEM images of AuNPs (a-1) and AuNPs-NH2 (a-2). Size distribution and size in water of AuNPs (b-1) and AuNPs-NH2 (b-2). c Zeta-potentials of AuNPs and AuNPs-NH2. d Spectrophotometer results of AuNPs and AuNPs-NH2. e In vitro toxicity evaluation of U87-MG cells after co-incubation with AuNPs-NH2 for 24 h by Cell Counting Kit-8 (CCK-8) method. f Dynamic light scattering (DLS) size measurements of AuNPs-NH2 in PBS for varied time durations (0 ~ 29 days).

Fig. S2. Characterization of Au-DOX. IC50 of DOX (a) and AuNPs combined with radiotherapy of 6Gy (b). c TEM image of Au-DOX. d Spectrophotometer results of AuNPs , AuNPs-NH2 and Au-DOX. e FT-IR spectrum of Au-DOX. f Size distribution and size in water of Au-DOX

Fig. S3. Characterization of PCL-PEOz- maleimide. a XPS spectra of PCL-PEOz- maleimide. b 1HNMR spectrum of the polymer.

Fig. S4. Photographs of blank polymersomes (a-1) and cargo-loaded polymersomes (a-2). TEM images of blank polymersomes (b-1) and cargo-loading polymersomes (b-2).c In vitro toxicity evaluation of U87-MG cells after co-incubation with PO and ANG-PO for 24 h by Cell Counting Kit-8 (CCK-8) method.

Fig. S5. The particle number of polymersomes was measured using NTA. The original sample was diluted 250 times before testing. The particle number of original sample was yielded a value of 6×1011 particles/mL after calculation.

Stats: Mean +/- Standard Error:

Mean: 216.8 +/- 3.2 nm

Concentration (Upgrade): 2.40e+09 +/- 1.12e+08 particles/ml

Fig. S6. Identification of primary astrocytes (a-1) and cerebral microvascular endothelial cells (a-2) by flow cytometry. b Expression levels of LRP1 on cell lines of U87-MG, BMECs, and normal  astrocyte determined by Western blot. c Quantitative analysis of LRP1 protein levels. Data are presented as the mean plus or minus the standard deviation (SD), and n=3 for each group,**P<0.01,***P<0.001.

Fig. S7. Confocal analysis of the U87 cells treated with Au-DOX@PO for 6 hours.