Additional file 1.

Triazine-cored Polymeric Vectors for Antisense Oligonucleotide Delivery in vitro and in vivo

Mingxing Wang*, Bo Wu, Jason D Tucker, Sapana N Shah, Peijuan Lu, Qilong Lu

McColl-Lockwood Laboratory for Muscular Dystrophy Research, Carolinas Medical Center, 1000 Blythe Blvd. Charlotte, NC 28231, USA

Phone: 1-704-355-5588;  Fax: 1-704-355-1679; Email: mingxing.wang@atriumhealth.org

Synthesis and characterization of Triazine-cored amphiphilic polymers (TAPs)

The synthesis and characterization of TAPs have been reported in our previous study.30 The structure and code of Jeffamine M series and LPEI were given in Figure S1, and the code abbreviations and corresponding compositions of the TAP polymers are presented in Table S1.

Figure S1. Structure illustration of substituents A (Jeffamine M ) and B (LPEI).

Table S1. Polymer code abbreviations and corresponding compositions

| Code | Composition | Code | Composition | Code | Composition | Code | Composition |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1A41B1 | M2070-Cy(Cl)-PEI 0.8k | 1A31B1 | M2005-Cy(Cl)-PEI 0.8k | 1A21B1 | M1000-Cy(Cl)-PEI 0.8k | 1A11B1 | M600-Cy(Cl)-PEI 0.8k |
| 1A41B2 | M2070-Cy(Cl)-PEI 1.2k | 1A31B2 | M2005-Cy(Cl)-PEI 1.2k | 1A21B2 | M1000-Cy(Cl)-PEI 1.2k | 1A11B2 | M600-Cy(Cl)-PEI 1.2k |
| 1A41B3 | M2070-Cy(Cl)-PEI 2.0k | 1A31B3 | M2005-Cy(Cl)-PEI 2.0k | 1A21B3 | M1000-Cy(Cl)-PEI 2.0k | 1A11B3 | M600-Cy(Cl)-PEI 2.0k |
| 1A42B1 | M2070-Cy-2PEI 0.8k | 1A32B1 | M2005-Cy-2PEI 0.8k | 1A22B1 | M1000-Cy-2PEI 0.8k | 1A12B1 | M600-Cy-2PEI 0.8k |
| 1A42B2 | M2070-Cy-2PEI 1.2k | 1A32B2 | M2005-Cy-2PEI 1.2k | 1A22B2 | M1000-Cy-2PEI 1.2k | 1A12B2 | M600-Cy-2PEI 1.2k |
| 1A42B3 | M2070-Cy-2PEI 2.0k | 1A32B3 | M2005-Cy-2PEI 2.0k | 1A22B3 | M1000-Cy-2PEI 2.0k | 1A12B3 | M600-Cy-2PEI 2.0k |
| 2A41B1 | 2M2070-Cy-PEI 0.8k | 2A31B1 | 2M2005-Cy-PEI 0.8k | 2A21B1 | 2M1000-Cy-PEI 0.8k | 2A11B1 | 2M600-Cy-PEI 0.8k |
| 2A41B2 | 2M2070-Cy-PEI 1.2k | 2A31B2 | 2M2005-Cy-PEI 1.2k | 2A21B2 | 2M1000-Cy-PEI 1.2k | 2A11B2 | 2M600-Cy-PEI 1.2k |
| 2A41B3 | 2M2070-Cy-PEI 2.0k | 2A31B3 | 2M2005-Cy-PEI 2.0k | 2A21B3 | 2M1000-Cy-PEI 2.0k | 2A11B3 | 2M600-Cy-PEI 2.0k |

Figure S2. Comparison of transduction and cytotoxicity between TAP (10 µg) and LF-2k (4 µg) mediated 2′-OMePSE50 (2 µg) stained by Propidium iodide (PI, red) and Hoechst 33342 (blue) after six-day delivery (original magnification, x200; scale bar: 500 µm).