## Additional file 1

# In vivo performance of electrospun tubular hyaluronic acid/collagen nanofibrous scaffolds for vascular reconstruction in the rabbit model

Yuqing Niua, Massimiliano Galluzzib, Ming Fua, Jinhua Hua, Huimin Xiaa,*

a Department of Pediatric Surgery, Guangdong Provincial Key Laboratory of Research in Structural Birth Defect Disease, Guangzhou Women and Children's Medical Center, Guangzhou Medical University, Guangzhou 510623, Guangdong, P.R. China.

b Materials Interfaces Center, Shenzhen Institutes of Advanced Technology, Chinese Academy of Sciences, Shenzhen 518055, Guangdong, P.R. China.

*Correspondence: xia-huimin@foxmail.com

Fig. S1. Vascular grafts fabricated with cellularized tubular HA/collagen nanofibrous scaffold facilitates vascular reconstruction. H&E staining the cross-section of a retrieved tubular HA/collagen nanofibrous grafts 6 weeks after transplant at 2.5×(upper panel) and 40× (lower panel) compared with rabbit carotid artery (b, d, g). Scale bars, 100 μm.

Table S1. The size of the obtained electrospun tubular HA/collagen nanofibrous scaffolds.

| Sample | Length (cm) | Internal diameter (mm) | Wall thickness (mm) | Fiber diameter (nm) |
| --- | --- | --- | --- | --- |
| HA/collagen | (0.5-9) cm | (2.6-3.0) mm | (0.6-1.0) mm | (905±113) nm |