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Figure S1. Ag nanoparticle diameter statistical distribution of Ag-Fe3O4 hybrid BMPs synthesis at room temperature and 80°C. The average diameter of Ag nanoparticles was 9.85±2.22 nm and 17.51±3.14 nm under room temperature and 80℃, which increased almost two fold.
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Figure S2. Functional groups and crystal lattice analysis of BMP-Ag synthesized under AgNO3 concentration 1.0 mg/mL, reaction time 1 min, reaction temperature 80°C, and room temperature by FTIR and XRD. The functional groups of BMP-Ag no obvious change under different synthesized parameters. There is a faint diffraction peak at 38.1o of BMP-Ag responding to the (111) crystal plane of face-centered cubic Ag compared with BMP, and the full width at half maximum decreased as the Ag NP size increased at a reaction temperature of 80 °C.

Figure S2. Crystal lattice and functional groups analyze of BMP-Ag synthesized under AgNO3 concentration 1.0 mg/mL, incubation time 1 min, incubation temperature 80

[bookmark: _GoBack][image: ]
Figure S2. (A) Magnetotactic bacteria MSR-1 cultured at different concentrations of AgNO3 solution. The bacterial growth was inhibited when the AgNO3 concentrations >1.0 mg/mL. (B) Transmission electron microscopy image of MSR-1 cultured under 1.0 mg/mL AgNO3 solution. There is no synthesis of Ag-Fe3O4 hybrid BMP.
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Figure S42. Transmission electron microscopy image of chemically synthesized Fe3O4(A), commercial biotinylated magnetic beads(B), and streptavidin magnetic beads(C) and BMPs(D) after incubating with AgNO3 solution. Only BMP can mineralize Ag+ into Ag nanoparticles.
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Figure S53. Construction of MGMSRv2_1436 gene deletion mutant. (A) Schematic diagram of the construction of suicide vector pUXcusA. (B) Amplified upstream and downstream fragments of MGMSRv2_1436 gene and gentamicin resistance cassette gene. (C) Polymerase chain reaction (PCR) amplified the internal gene of  MGMSRv2_1436 (1436), gentamicin resistance gene (Gm), upstream and downstream fragments of MGMSRv2_1436 gene to confirm the screened MGMSRv2_1436 mutant strain. #: MGMSRv2_1436 mutant strain, + WT MSR-1 positive control, - ddH2O negative control. There was no MGMSRv2_1436 gene, but has gentamicin resistance gene, upstream, and downstream fragments in the screened colonies, mean MGMSRv2_1436 deletion mutant was obtained successfully. (D) PCR amplified the genes (mamB, mamD, mamE, mamO, mamX, mamZ, mms6, feoB) associated with the magnetosome synthesis. It was confirmed that no genes were lost in the construction process.
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Figure S64. Transmission electron microscopy image of MSR-Δ1436 BMP after incubating with AgNO3 solution. MSR-Δ1436 BMP still can mineralize Ag+ into Ag nanoparticles; it was indicated that Ag+ transported into BMP membrane did not base on efflux pump MGMSRv2_1436 protein in vitro state.
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Figure S75. Transmission electron microscopy image of Fe3O4 crystal and vesicle(B) of BMP after incubating with AgNO3 solution. There was no Ag nanoparticle was synthesis on those two components. It was indicated that remineralization of BMP needs synergy of each element of BMP.
































Table S1 Proteins of only exist on BMP membrane



Supplementary experimental section
Construction of MGMSRv2_1436 deletion mutant : MGMSRv2_1436 deletion mutant (MSR-Δ1436) was constructed by biparental conjugation. The fragments 1000 bp upstream and downstream of MGMSRv2_1436 were amplified from the MSR-1 genome using primers sets. Gentamicin resistance cassette was amplified from the pUCGm vector. Then the amplified upstream fragment was digested by restriction endonucleases XhoI and BamHI. The downstream fragment was digested by XbaI and BamHI, and the Gentamicin resistance cassette was digested by BamHI. Upstream, downstream and gentamicin resistance cassettes were ligated into suicide vector pUX19 to form pUXcusA (Figure S3AB). pUXcusA was transformed into E. coli S17-1 to construct donor strain. Then pUXcusA was introduced into WT MSR-1 by biparental conjugation. MSR-Δ1436 was screened and selected by Gmr and Nxr and confirmed by Polymerase chain reaction (PCR). There was no MGMSRv2_1436 gene, but has gentamicin resistance gene, upstream and downstream fragments in the screened colonies, mean achieved MGMSRv2_1436 deletion mutant successfully(Figure S3C). The genes associated with magnetosomes synthesis were detected in MSR-Δ1436 and confirmed that no genes were lost in the construction process(Figure S3D).
Extraction vesicle and Fe3O4 crystal of magnetosome: To detect a different component of BMP effect on Ag+ mineralization, vesicle and Fe3O4 crustal of BMP were extracted, respectively. Magnetotactic bacteria could survive empty synthesis magnetosomes when cultured in iron-poor condition(1). We constructed in vivo biotinylated magnetosome in MSR-1 as described previously(2). The constructed recombinant strain (MSR-∆F-BF) that synthesized biotinylated magnetosome were cultured without iron medium for 24 h—then collected by centrifugation at 8000 rpm for 10 min. The cell was suspended in 10 mmol/L of PBS buffer and lysed by ultrasonication (NingBo Scientz Biotechnology Co., Ltd., China) at 100 W for 30 min. We extracted biotinylated vesicle from cell lysis solution based on particular biotin bind with streptavidin. Streptavidin magnetic beads were purchased from Thermo Fisher and incubated with a cell lysis solution. Then biotinylated BMP vesicle was extracted according to the instructions.
   Fe3O4 crustal was prepared by suspended 1 mg BMP in 10 mL 10% sodium dodecyl sulfate (SDS) and 3 mol/L NaOH mixture, then boiled for 15 min, magnetic separation, and 10 mL ddH2O washed 3-5 times.
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