PLA-lignin nanofibers as antioxidant biomaterials for cartilage regeneration and osteoarthritis treatment

Ruiming Liang a# , Xingchen Yang a# , Pek Yin Michelle Yew b,c#, Sigit Sugiarto b, Qiang Zhu b, Jinmin Zhao a,d, Xian Jun Loh b, Li Zheng a,d*, Dan Kai b,e*

a Guangxi Engineering Center in Biomedical Materials for Tissue and Organ Regeneration & Collaborative Innovation Center of Regenerative Medicine and Medical Biological Resources Development and Application, Life Sciences Institute, Guangxi Medical University, Nanning, 530021, China

b Institute of Materials Research and Engineering (IMRE), A*STAR, 2 Fusionopolis Way, #08-03 Innovis, 138634, Singapore

c Department of Biomedical Engineering, Faculty of Engineering, National University of Singapore, 117583, Singapore

d Department of Orthopaedics Trauma and Hand Surgery, Guangxi Key Laboratory of Regenerative Medicine, The First Affiliated Hospital of Guangxi Medical University, Guangxi Medical University, Nanning, 530021, China

e Institute of Sustainability for Chemicals, Energy and Environment (ISCE2), A*STAR, 2 Fusionopolis Way, Innovis, #08-03, Singapore 138634

E-mail: zhengli224@163.com; kaid@imre.a-star.edu.sg

Totally 10 pages with 2 tables and 7 figures

Table S1 Table characterization of lignin-g-PLA copolymers

| Sample | Feed Ratio |  |  | Mn i | Mw i | PDI | Yield ii |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Lignin : Lactide |  |  | [ kDa ] | [ kDa ] |  | [%] |
| PL5 | 5 | : | 95 | 75.6 | 100.2 | 1.33 | 92 |
| PL10 | 10 | : | 90 | 61.5 | 87.2 | 1.42 | 80 |
| PL20 | 20 | : | 80 | 49.0 | 57.2 | 1.17 | 72 |
| PL30 | 30 | : | 70 | 38.7 | 47.7 | 1.23 | 76 |
| PL40 | 40 | : | 60 | 28.5 | 35.9 | 1.26 | 69 |
| PL50 | 50 | : | 50 | 15.4 | 21.2 | 1.38 | 65 |
| i Determined by GPC. ii Isolated yield. |  |  |  |  |  |  |  |

Table S2 TGA characterisation table of PLLA and PLLA/PLA-lignin nanofibers

| Sample | T95 (°C) a | Tmax (°C) b | Residue at 400°C | Residue at 500°C |
| --- | --- | --- | --- | --- |
| PLLA | 311 | 366 | 2.5% | 1.9% |
| PLLA/PL10 | 310 | 360 | 7.1% | 4.5% |
| PLLA/PL20 | 302 | 365 | 8.5% | 6.6% |
| PLLA/PL30 | 292 | 356 | 8.4% | 6.1% |
| PLLA/PL40 | 290 | 354 | 12.9% | 9.8% |
| PLLA/PL50 | 281 | 351 | 15.2% | 11.5% |
| a Temperature at 5 wt% loss. b Maximum degradation temperature. |  |  |  |  |

Figure S1 1H NMR (CDCl3) of the synthesized alkylated lignin

Figure S2 1H NMR (CDCl3) of the alkylated lignin-g-PLA

Figure S3 FTIR spectra of lignin and PLA-lignin copolymers.

Figure S4 Images showing the water contact angles of PLLA and PLLA/PLA-lignin nanofibers

Figure S5 Typical stress-strain curves of the PLLA/PLA-lignin nanofibers by tensile test.

Figure S6 DSC curves of PLA-lignin copolymers

Figure S7 DSC curves of PLLA/lignin-PLA nanofibers