Supporting Information

B7H3 Targeting Gold Nanocage pH-Sensitive Conjugates for Precise and Synergistic Chemo-Photothermal Therapy against NSCLC

Bing Chen 1,2†, Kaifan Zheng 1,2†, Shubin Fang 1,2†, Kangping Huang 1, Chengchao Chu 4, Junyang Zhuang 1,2, Jin Lin 2, Shaoguang Li 1,2, Hong Yao 1,2, Ailin Liu 1,2, Gang Liu 4*, Jizhen Lin 1,3,5*, Xinhua Lin 1,2*

1 Key Laboratory of Nanomedical Technology (Education Department of Fujian Province), School of Pharmacy, Fujian Medical University, Fuzhou 350122, China.

2 Department of Pharmaceutical Analysis, School of Pharmacy, Fujian Medical University, Fuzhou 350122, China.

3 The Cancer Center, Union Hospital, Fujian Medical University, Fuzhou 350122, China.

4 State Key Laboratory of Molecular Vaccinology and Molecular Diagnostics & Center for Molecular Imaging and Translational Medicine, School of Public Health, Xiamen University, Xiamen 361102, China.

5 The Department of Otolaryngology, Head and Neck Surgery, University of Minnesota Medical School, Minneapolis 55404, United States.

*Correspondence: 13906939638@163.com; linjizhen@fimu.edu.cn; Gangliu.cmitm@xmu.edu.cn.

† These authors contributed equally to this work.

Keywords: B7H3/CD276, Gold nanocage, Doxorubicin conjugates, Chemo-photothermal therapy, NSCLC

Figure S1. Synthesis and characterization of silver nanocubes and gold nanocages. A) The photo, B) Hydrodynamic diameters, and C) Zeta potentials of silver nanocubes. D) The UV-Vis spectra of silver nanocubes, E) gold nanocages, and F) B7H3/Dox@GNCs. G) The photo, H) Hydrodynamic diameters, and I) Zeta potentials of gold nanocages.

Figure S2. The synthetic procedures of LA-Dox-mPEG.

Figure S3. Characterization of LAOEt and LA-NHNH2. A) HPLC chromatograms, B) FT-IR, C) MS spectra, G) 1H-NMR (DMSO-d6) and H) 13C-NMR (DMSO-d6) of LAOEt. D) HPLC chromatograms, E) FT-IR, F) MS spectra, H) 1H-NMR (DMSO-d6) and J) 13C-NMR (DMSO-d6) of LA-NHNH2.

Figure S4. Characterization of LA-Dox and mPEG-NPC. A) HPLC chromatograms, B) FT-IR, C) MS spectra, G) 1H-NMR (DMSO-d6) and H) 13C-NMR (DMSO-d6) of LA-Dox. D) HPLC chromatograms, E) FT-IR, F) MS spectra, H) 1H-NMR (DMSO-d6) and J) 13C-NMR (DMSO-d6) of mPEG-NPC.

Figure S5. Characterization of LA-Dox-mPEG. A) HPLC chromatograms, B) FT-IR, C) MS spectra, D) 1H-NMR (DMSO-d6) of LA-Dox-mPEG.

Figure S6. In vivo biodistribution of Dox, Dox@GNCs, and B7H3/Dox@GNCs. B) Biodistribution profiles of Dox in A) heart, B) Lung, C) Liver, D) Spleen, and E) Kindey of NSCLCs tumor-bearing mice following intravenous injection of Dox·HCl, Dox@GNCs, and B7H3/Dox@GNCs at Dox dose of 3 mg/kg for different time. Data are Mean ± SD (n=3), *P ﹤0.05 and **P ﹤0.01, (one-sample t-test) versus Dox group.