Supporting Information

Bi2S3/Ti3C2-TPP Nano-Heterostructures Induced by Near-Infrared for Photodynamic Therapy Combined with Photothermal Therapy on Hypoxic Tumors

Hanwen Jiang1,2, Jingxian Sun3,5, Fucong Liu1, Yuanjiao Zhao1, Xin Chen3, Changsong Dai4, and Zhaohui Wen1*.

1 Department of Neurology, Brain Ultrasound, The First Afﬁliated Hospital of Harbin Medical University, Harbin 150001, Heilongjiang Province, China

2 Department of Cardiology, Cardiac Ultrasound, The First Afﬁliated Hospital of Harbin Medical University, Harbin 150001, Heilongjiang Province, China

3 Key Colleges and Universities Laboratory of Neurosurgery in Heilongjiang Province, Harbin 150001, Heilongjiang Province, China

4 MIIT Key Laboratory of Critical Materials Technology for New Energy Conversion and Storage, School of Chemistry and Chemical Engineering, Harbin Institute of Technology, Harbin 150001 China

5 Department of Neurosurgery, the Affiliated Hospital of Qingdao University, Qingdao 266005, Shandong Province, China

Email: wenzhaohui1968@163.com

A: Calculation of Photothermal Conversion Efficiency

Following the Roper report [1], the total energy balance for the system is

imiCp,idTdt = QNMs + QDis – Qsurr

in which mi and  Cp,i represent the mass and heat capacity of system components, respectively. T represents the solution temperature, QDis represents the basic energy input of the quartz cuvette cell containing pure water without samples, and Qsurr represents the heat conducted away from the system surface by air. For the heat output:

Qsurr = hS(T - Tsurr)

Where h is the heat transfer coefficient, S is the surface area of the container, and Tsurr is the ambient temperature of the surroundings. The system temperature will rise to a maximum when the heat input is equal to the heat output:

QNMs + QDis = Qsurr - max = hS(Tmax - Tsurr)

In the above equation, Qsurr -max is heat conduction away from the system surface by air when the sample cell reaches the equilibrium temperature, and Tmax is the maximum system temperature.

The photothermal conversion efficiency is calculated from the following equation:

η = hS(Tmax - Tsurr) - QDisI(1- 10-A808)

Where I is the laser power and A808 is the absorbance of the samples at the wavelength of 808 nm.

In order to get the hS, a dimensionless driving force temperature, θ is introduced as follows:

θ = T- TsurrTmax- Tsurr

And a sample system time constant τs,

τs = imiCp,ihS

Thus, dθdt = 1τsQNMs + QDishS(Tmax - Tsurr) – θτs, dθdt = – θτs, t = –τslnθ

So hS could be calculated from the slope of cooling time vs. lnθ.

Reference:

1.	Roper DK, Ahn W, Hoepfner M. Microscale Heat Transfer Transduced by Surface Plasmon Resonant Gold Nanoparticles. J Phys Chem C Nanomater Interfaces 2007, 111:3636-3641.

B: Reaction Equations

Equation 1  O2 + e- → ·O2-

Equation 2  2H2O + 4h+ → O2 + 4H+

Equation 3  ·O2- + e- + 2H+ → H2O2

Equation 4  ·O2- + H2O2 + 2h+ → ·OH + OH- + O2

C: Supplementary Figures

Fig. S1 XRD patterns of Bi2S3 NPs, Ti3C2 NSs, and Bi2S3/Ti3C2 NHs.

Fig. S2 XPS results of Bi2S3/Ti3C2 NHs for the regions of interest.

Fig. S3 Tauc plot diagram of Bi2S3 NPs.

Fig. S4 PL spectra of Bi2S3 NPs and Bi2S3/Ti3C2 NHs with different ratios.

Fig. S5 a DLS and b Zeta potential of Ti3C2, Bi2S3/Ti3C2, Bi2S3/Ti3C2-PEG, and Bi2S3/Ti3C2-TPP. c Size distributions of Bi2S3/Ti3C2-TPP in water and DMEM; inset: corresponding image of Bi2S3/Ti3C2-TPP in DI and DMEM after 48 h storage.

Fig. S6 a Hydrodynamic size and polydispersity index, and the corresponding b digital and c TEM images of Bi2S3/Ti3C2-TPP under different conditions. The sequence of the experimental group in pictures b and c from left to right is consistent with that in picture a.

Fig. S7 UV-vis absorption patterns of a Bi2S3/Ti3C2 and Bi2S3/Ti3C2-TPP, and b TPP aqueous solutions with various concentrations. c The standard curve of TPP concentrations (y = 0.0797x + 0.08123, R2 = 0.994).

Fig. S8 a Mott-Schottky plot of Bi2S3. b XPS spectrum of VB in Bi2S3.

Fig. S9 The UV–vis absorption spectra of a Bi2S3 and b Ti3C2 with various concentrations. The absorptions of c Bi2S3/Ti3C2, d Bi2S3, and e Ti3C2 aqueous suspensions with various concentrations at 808 nm.

Fig. S10 Heating and cooling profiles of a Bi2S3/Ti3C2, c Bi2S3, and e Ti3C2 (100 µg mL-1) under 808 nm laser irradiation (1 W cm-2, 10 min). Plot and linear fit of time vs. negative log of increased temperature for b Bi2S3/Ti3C2, d Bi2S3, and f Ti3C2 cooling rates.

Fig. S11 a The inhibition effect of low temperature (4 ℃), colchicine, and CPZ on the cellular uptake of Bi2S3/Ti3C2-TPP. The contents of b Bi and c Ti in U251 cells incubated with Bi2S3/Ti3C2-TPP or Bi2S3/Ti3C2 measured by ICP-MS; ***P < 0.001.

Fig. S12 a Flow cytometry analysis of JC-1-based MMP change in U251 cells. b DCF-based cellular ROS level of U251 cells analyzed by flow cytometry. B-Bi2S3, M-Ti3C2, T-TPP, sample concentration - 100 µg mL-1, and NIR - an 808 nm laser, 1 W cm-2, 10 min.

Fig. S13 Quantification of Nrf2, Hsp70, and HO-1 expressions in U251 cells following various treatments; the intensities of Nrf2, Hsp70, and HO-1 were normalized to those of β-actin using Image J software.

Fig. S14 Quantification of HIF-1α expressions in tumors after various treatments, the intensities of HIF-1α were standardized to those of β-actin using Image J software.

Fig. S15 Plots of temperature values of U251 tumor-bearing mice after being injected with PBS (pH=7.4, 10 mM) or Bi2S3/Ti3C2-TPP (20 mg kg-1).