Attenuation of osteoarthritis progression via locoregional delivery of Klotho-expressing plasmid DNA and Tanshinon IIA through a stem cell-homing hydrogel

Peng Wang1 †, Zhibo Zhao1 †, Xiao Li1, Ziyang Li5, Benzhao Huang2 ,Xiaoqing Lu2, Shimin Dai2, Shishuo Li2, Zhentao Man1,2,3,4* and Wei Li1,2,3*

†Peng Wang and Zhibo Zhao are contributed equally to this work

* Correspondence: Zhentao Man mztqd1984@163.com, Wei Li greatli2000@163.com

1Department of Joint Surgery, Shandong Provincial Hospital, Shandong University, Jinan, Shandong 250021, P. R. China

2Department of Joint Surgery, Shandong Provincial Hospital Affiliated to Shandong First Medical University, Jinan, Shandong 250021, P. R. China

3College of Sports Medicine and Rehabilitation, Shandong First Medical University & Shandong Academy of Medical Sciences, Jinan, Shandong 250021, P. R. China

4Endocrine and Metabolic Diseases Hospital of Shandong First Medical University, Shandong Institute of Endocrine and Metabolic Diseases, Jinan, Shandong 250062, P. R. China

5Department of Sports Medicine, Zhejiang University School of Medicine, Hangzhou, Zhejiang 310058, P. R. China

Figure S1. Characterization of the amphiphilic peptide-SA monomer. (A) The purity of the peptide as confirmed by HPLC. (B) The molecular weight of the peptide-SA monomer as certified by ESI-MS.

Figure S2. Gel retardation assay of pPNP stability. (A) The stability of pPNP at a weight ratio of peptide-SA monomers to pDNA of 10:1. DNase I digestion and FBS treatment were performed at 37°C for 1 h.(B) Gel retardation assay showing the stability of pPNP after 14 days. The experiments were repeated three times independently.

Figure S3. Raman spectra of freeze-dried KLDL/PFS hydrogel.

Figure S4. Characterization of the self-assembling peptide hydrogel. (A, B) The purity of KLDL-PFS (A) and KLDL (B) as confirmed by HPLC. (C, D) The molecular weight of KLDL-PFS (C) and KLDL (D) as certified by ESI-MS.

Figure S5. Stability and release profile of NP-pKlotho in vitro. (A) Degradation of the blank hydrogel in phosphate-buffered saline, with or without proteinase K digestion. (B) The release profile of pKlotho from the hydrogel. Data expressed as means ± SD (n = 3).

Figure S6. Immunofluorescence staining showing that pPNPs (red) in rat knee

cartilage after surgery. Scale bar, 75μm.

Figure S7. Col2 promoter-driven, chondrocyte-specific KL transgene expression. Transduction of rat BMSCs and RAW264.7 cells with pDNA including the Col2 promoter. (A, C) Percentage of EGFP-positive BMSCs (A) and RAW264.7 cells (C) after treatment with free pDNA or pPNPs. (B, D) Quantitative analysis of the flow cytometry data. Data expressed as means ± SD (n = 3 independent experiments per group).

Figure S8. Immunofluorescence staining of Klotho in interleukin (IL)-1β-treated chondrocytes and chondrocytes at passage 1 (P1). Scale bar, 200 µm.

Figure S9. qPCR evaluation of the expression of P21, MMP3, and Adamts5 at 2 days post-transfection of rat chondrocytes with different cultures (n = 3).

Figure S10. (A) CCK-8 viability assay of BMSC cultured under normal conditions, or in the presence of KLDL, PFS, or pPNP+TIIA@PFS (n = 3). (B) Representative fluorescence images of the proliferation of BMSC cultured for 3 days on different culture. Scale bar, 50 µm.

Figure S11. Cytotoxicity assays of pPNPs in chondrocytes (n = 3). NS, not significant.

Figure S12. (A) CCK-8 viability assay of chondrocytes cultured under normal conditions, or in the presence of KLDL, PFS, or pPNP+TIIA@PFS (n = 3). (B) Representative fluorescence images of the proliferation of chondrocytes cultured for 3 days on different culture. Scale bar, 50 µm.

Figure S13. Systemic toxicity evaluation of the pPNP+TIIA@PFS. (A) Complete blood counts and blood chemistry analyses of healthy control rats (without surgery) and pPNP-hydrogel-injected rats. WBC, white blood cell; LYMPH, lymphocyte; RBC, red blood cell; HCT, hematocrit; PLT, platelet; ALB, albumin; GLU, glucose; BUN, blood urea nitrogen; ALT, alanine transaminase; AST, aspartate transaminase (n = 3). (B) Histological analysis of the major organs from healthy control rats (without surgery) and pPNP-hydrogel-injected rats. Scale bar, 500 µm. NS, not significant.

Table S1. Osteoarthritis Research Society International (OARSI) scores

| Grade (key feature) | Subgrade (optional) | Associated criteria (tissue reaction) |
| --- | --- | --- |
| Grade 0: surface intact, cartilage intact | No subgrade | Intact, uninvolved cartilage |
| Grade 1: surface intact | 1.0 Cells intact | Matrix: superficial zone intact, edema and/or fibrillation |
|  | 1.5 Cells death | Cells: proliferation (clusters), hypertrophy Reaction must be more than superficial fibrillation only |
| Grade 2: surface discontinuity | 2.0 Fibrillation through superficial zone | As above |
|  | 2.5 Surface abrasion with matrix loss within superficial zone | +Discontinuity at superficial zone ±Cationic stain matrix depletion (Safranin O or Toluidine Blue) upper 1/3 of cartilage (mid zone) ±Disorientation of chondron columns |
| Grade 3: vertical fissures | 3.0 Simple fissures | As above |
|  | 3.5 Branched/complex fissures | ±Cationic stain depletion (Safranin O or Toluidine Blue) into lower 2/3 of cartilage (deep zone) ±New collagen formation (polarized light microscopy, Picro Sirius Red stain) |
| Grade 4: erosion | 4.0 Superficial zone delamination | Cartilage matrix loss, cyst formation within cartilage matrix |
|  | 4.5 Mid zone excavation |  |
| Grade 5: denudation | 5.0 Bone surface intact | Surface is sclerotic bone or reparative tissue including fibrocartilage |
|  | 5.5 Reparative tissue surface present |  |
| Grade 6: deformation | 6.0 Joint margin osteophytes | Bone remodelling. Deformation of articular surface contour (more than osteophyte formation only) |
|  | 6.5 Joint margin and central osteophytes | Includes: microfracture and repair |

Table S2. Related information about primary antibodies

| Product name | Species Reactivity | Molecular weight | Source |
| --- | --- | --- | --- |
| GAPDH | Rabbit | 37 kDa | CST, America |
| β-actin | Rabbit | 45 kDa | CST, America |
| Mmp13 | Rabbit | 54 kDa | Abcam, England |
| Sox 9 | Rabbit | 56 kDa | Abcam, England |
| Col2A1 | Rabbit | 142 kDa | Abcam, England |
| Aggrecan | Rabbit | 250 kDa | Proteintech, China |
| Klotho | Mouse | 116 kDa | Proteintech, China |
| P21 | Rabbit | 21 kDa | CST, America |
| P16ink4a | Rabbit | 16 kDa | CST, America |
| Adamts5 | Rabbit | 73 kDa | ABclonal, China |
| CCN1 | Rabbit | 41 kDa | Abcam, England |

Table S3. Sequences of the primers used in this study

| Gene | Forward primer (5′-3′) | Reverse primer (5′-3′) |
| --- | --- | --- |
| Mmp13 | CATCATCTGGGAGCATGAAA | GCAGCTCCAAAGGCTACAA |
| Mmp3 | AGTGCTTCTGAATGTCCTTCG | TCTTCCTCTGAAACTTGGCG |
| Adamts5 | TCGTGGCCGCGTTCTTGCTCAC | ACGCGGGACCTCAGACGTGGTG |
| P16ink4a | GCGTTGCCAGAAGTGAAGCCA | CGTCGTGCGGTATTTGCGGTAT |
| P21 | GCTCTGGACGGTACGCTTAGGT | CTGCCTGGTTCCTTGCCACTTC |
| Sox9 | GCACCAGGGTCCAGTCATA | TAAATTCCCAGTGTGCATCC |
| Col2A1 | CCTGGACCCCGTGGCAGAGA | GCAGGGCCAGAAGTACCCTGATC |
| Aggrecan | TGGGGTCCGTGGGCTCACAA | CATTCGCACGGGAGCAGCCA |
| Klotho | CTCTGAAAGCCTACGTGTTGG | TAGAAACGAGATGAAGGCCAG |
| β-actin | TGTCACCAACTGGGACGATA | GGGGTGTTGAAGGTCTCAAA |