Figure S1 ALP staining and Transwell Assay

(A) Alizarin red (lower) staining of control and treated groups;(B) by Transwell Assay and crystal violet dying, migration was observed in Control, Exo-MSC, Exo-Yoda1, and Yoda1 groups, the scale was 50um; (C) the statistical analysis of migration, * p<0.5, **p<0.01, *** p<0.001, **** p<0.0001

Figure S2 KEGG and GO analysis of Exo-Yoda1 and Yoda1 treated BMSCs

(A) and (B) KEGG analysis of Exo-Yoda1 and Yoda1; (C) andd (D) GO analysis of Exo-Yoda1 and Yoda1

Figure S3 OCN and CD31(marker of vessels) staining in subcutaneous ectopic osteogenesis nude mice models

Figure S4 OCN and CD31(marker of vessels) staining in bone defect of rat skull models

| Primers | Sequence (5’-3’) |
| --- | --- |
| OPN-RAT-F | AGCTTGGCTTACGGACTGAG |
| OPN- RAT-R | AGGTCCTCATCTGTGGCATC |
| COL1A1-RAT-F | GTCATCGTGGCTTCTCTGGT |
| COL1A1- RAT-R | ACCGTTGAGTCCATCTTTGC |
| OCN-RAT-F | AATAGACTCCGGCGCTACCT |
| OCN- RAT-R | GAGCTCACACACCTCCCTGT |
| ALP-RAT-F | GCACAACATCAAGGACATCG |
| ALP- RAT-R | TCAGTTCTGTTCTTGGGGTACAT |
| BMP2-RAT-F | TGAACACAGCTGGTCTCAGG |
| BMP2- RAT-R | GCTGTTTGTGTTTGGCTTGA |
| Gapdh-Rat-F | TGGAGTCTACTGGCGTCTT |
| Gapdh-Rat-R | TGTCATATTTCTCGTGGTTCA |

Table S1 primers used in this study

Table S2 GO analysis of MAPK-ERK1/2 pathway

| Groups | Term | P value and q value | Genes |
| --- | --- | --- | --- |
| Exo-Yoda1 VS Con | GO:0070372 regulation of ERK1 and ERK2 cascade | p= 0.0000013, q= 0.000037066969282284 | Ackr3¦Angpt1¦Bmp4¦Ccl2¦Ccl7¦Ccr1¦Ceacam1¦Ceacam4¦Clcf1¦Cx3cl1¦Ednra¦Errfi1¦Fgf2¦Fgfr3¦Gcnt2¦Gcnt6¦Gper1¦Gpr183¦Kdr¦LOC100909750¦Nox4¦Pdgfd¦Pkhd1¦Spry2¦Xcl1 |
| Exo-Yoda1 VS Con | GO:0000165 MAPK cascade | p= 0.000011, q= 0.0001675958094383 | Ackr3¦Adra1b¦Angpt1¦Bmp4¦Bmp6¦Camk2a¦Ccl2¦Ccl7¦Ccr1¦Ceacam1¦Ceacam4¦Clcf1¦Cx3cl1¦Dact1¦Diras2¦Dusp2¦Dusp5¦Ednra¦Errfi1¦Fgd2¦Fgf2¦Fgfr3¦Gcnt2¦Gcnt6¦Gdf6¦Gper1¦Gpr183¦Grem1¦Grik2¦Id1¦Igfbp3¦Ighv¦Il1rn¦Inhbb¦Kdr¦LOC100909750¦LOC102549344¦Lpar2¦Lpar3¦Map3k7¦Mdfi¦Nox4¦Pdgfd¦Pkhd1¦Sfrp1¦Sh2d3c¦Spry2¦Xcl1¦Zfp622 |
| Yoda1 VS Con | GO:0070372 regulation of ERK1 and ERK2 cascade | p= 0.000000022, q= 7.89162481170248E-07 | Ackr3¦Angpt1¦Atf3¦Bmp4¦Btn2a2¦C5ar1¦C5ar2¦Ccl2¦Ccl7¦Ccr1¦Ceacam4¦Clcf1¦Cx3cl1¦Dusp1¦Ednra¦Epha7¦Errfi1¦Fgf10¦Fgf18¦Fgf2¦Fgfr3¦Gcnt2¦Gcnt6¦Gper1¦Gpr183¦Klf4¦LOC103689974¦Lgals9¦Mif¦Ndrg2¦Nox4¦P2ry1¦Pdgfd¦Rasgrp1¦Scimp¦Spry1¦Spry2¦Tgfbr3¦Trem2¦Wnk2¦Xcl1 |
| Yoda1 VS Con | GO:0000165 MAPK cascade | P= 0.0000000087, q= 3.61201261899261E-07 | Ackr3¦Actn2¦Adra1b¦Angpt1¦Atf3¦Bdnf¦Bmp3¦Bmp4¦Bmp6¦Btn2a2¦C5ar1¦C5ar2¦Cav2¦Ccl2¦Ccl7¦Ccr1¦Cd24¦Ceacam4¦Clcf1¦Cx3cl1¦Dact1¦Dusp1¦Dusp2¦Dusp5¦Dusp9¦Ednra¦Epha4¦Epha7¦Errfi1¦Fgf10¦Fgf14¦Fgf18¦Fgf2¦Fgfr3¦Flt1¦Fzd5¦Gcnt2¦Gcnt6¦Gdf6¦Gdnf¦Gper1¦Gpr183¦Grem1¦Id1¦Igfbp3¦Ighv¦Il11¦Il17rd¦Il1rn¦Inhba¦Inhbb¦Itga1¦Kit¦Klf4¦Kng1l1¦LOC100910021¦LOC100912585¦LOC102549344¦LOC103689974¦Lemd2¦Lgals9¦Lpar2¦Lpar3¦Map3k7¦Map3k7cl¦Mapk11¦Mdfi¦Mif¦Ndrg2¦Nox4¦Nrg1¦Nrk¦P2ry1¦Pdgfd¦Peli2¦Pik3r5¦Plce1¦Rasgrp1¦Rgs3¦Scimp¦Sfrp4¦Sh2d3c¦Spry1¦Spry2¦Tgfbr3¦Tnfrsf25¦Trem2¦Wnk2¦Wnt5a¦Xcl1 |