Enzyme/ROS dual-sensitive nanoplatform with on-demand Celastrol release capacity for enhanced ulcerative colitis therapy by ROS scavenging, microbiota rebalancing, inflammation alleviating

Jinfeng Shi1, Jiahui Zhou1, Bo Liu1, Kezhou Lin1, Xingliang Xie1, Xue Han1, Yanmei Sheng1, Yihan Liu1, Congjian He1, Yujin Zhou1, Nan Zhu1, Qian Yang1, Ruifeng Luo2*, Yi Li1*

1 College of Pharmacy, Chengdu Medical College, Chengdu 610500, China

2 State Key Laboratory of Quality Research in Chinese Medicine, Institute of Chinese Medical Sciences, University of Macau, Taipa, Macau 999078, China

*Corresponding authors

Dr. Yi Li, No.783 Xindu Avenue, Xindu District, Chengdu city, College of Pharmacy, Chengdu Medical College, Chengdu, China

Tel.: +86 13688305707

E-mail address: liyichengdu29@126.com

Dr. Ruifeng Luo, State Key Laboratory of Quality Research in Chinese Medicine, Institute of Chinese Medical Sciences, University of Macau, Taipa, Macau SAR, China

Tel.: +86 18482114736

E-mail address: ruifengluo128@163.com

Experimental Section

1. Synthesis of PAPE-SA

PAPE (1 g, 4.26 mmol), succinic anhydride (0.73 g, 7.3 mmol), DMAP (20 mg, 0.163 mmol) were dissolved in anhydrous THF (20 mL), and to the resulting solution, 1 mL of pyridine was added. The resulting solution was stirred at room temperature for 36 h. 1 mL of methanol was then added and continuously stirred for an additional 1 h to hydrolyze the excess succinic anhydride. The solvents were evaporated under vacuum to remove THF and 30 mL of chloroform was added to dissolve the evaporation residue. The solution was washed with 0.1 M HCl (2 × 30 mL) and water (1 × 30 mL). The organic phase was dried over MgSO4 overnight and then evaporated to give the product as colorless oil.

Supplementary Figures

Figure S1 Characteristic properties of various NPs

Figure S2 The zeta potential results of Cel/NPs at different days

Figure S3 The safety evaluation of Cel/NPs. (A) The representative images of H&E staining of main organs (the scale bar = 100 μm). (B) The level of ALT, AST, BUN and CRE in serum. Data are mean±SD (n=6). *p<0.05.