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Figure S1. The 1H NMR spectra of ATK-CDI in DMSO-d6. δ 1.59 (4H, -CH2-CH2-CH2-S-), δ 2.36 (4H, -CH2-CH2-CH2-S-), δ 2.94 (4H, -CH2-CH2-CH2-S-), δ 7.04 (2H, -CH=CH- from imidazole), δ 7.33-7.41 (4H, Ar-H), δ 7.61-7.86 (6H, -CH=CH- from imidazole, and Ar-H), δ 8.32 (2H, Ar-H).
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Figure S2. The ESI-MS spectrum of ATK-CDI. ESI-MS m/z: calculated for ATK-CDI [M+H]+ 503.15, found: 503.1.
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Figure S3. The HPLC chromatograms. A, F2A incubated in PBS for different times. From top to bottom are 72 hours, 24 hours, 12 hours, and 0 hours, respectively. B, From top to bottom are FA, 9-fluorenone, and gamma thiobutyrolactone, respectively. C, F2A was incubated in 1 mM H2O2 for different times. From top to bottom are 15 mins, 30 mins, and 60 mins, respectively. 
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Figure S4. The photograph of TPSA in PBS solution.

[image: ]
Figure S5. Flow cytometry (A) and data analysis (B) of CD22 expression in RAW264.7, THP-1, Ramos, and Raji cell lines. All data are presented the mean ± SD (n = 6).
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Figure S6. Flow cytometry was used to detect and analyze the fluorescence intensity (FI) of Cy5-labeled F@PLGA or F@TPSA incubated with RAW264.7 cells. All data are presented the mean ± SD (n = 6).
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Figure S7. The cell viability of Raji cells after incubation with different dose of TPSA for 24 h. All data are presented the mean ± SD (n = 6).
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