Supplementary Materials for

Reduced graphene oxide loaded with tetrahedral framework nucleic acids for combating orthodontically induced root resorption

Authors: Wenxiu Yuan 1, 3, Maotuan Huang 4, Wenqian Chen 2, Sihang Chen 3, Jingwen Cai 3, Linxin Chen 3, Hanyu Lin 2, Kaixun He 2, Huachen Chen 2, Wenting Jiang 2, Yanjing Ou 2, Jiang Chen 2, *

Supplementary Figures

Fig. S1. The schedule of orthodontically induced root resorption models.

Fig. S2. Palatal root was marked by green dashed line whereas the resorption area was represented by red.

Fig. S3. tFNAs-rGO suppresses M1, promotes M2 polarization, and boosts the migration ability in vitro. (A) Quantitative RT-PCR analysis of the mRNA levels of M1-like macrophages related genes of RAW264.7 cells after indicated treatment. (B) Quantitative RT-PCR analysis of the mRNA levels of M2-like macrophages related genes of RAW264.7 cells after indicated treatment. (C) Immunofluorescence staining showing the iNOS+ or CD86+ RAW264.7 cells. Scale bar: 100 μm. (D) Immunofluorescence staining showing the CD163+ or CD206+ RAW264.7 cells after indicated treatment. Scale bar: 100 μm. (E) Crystal violet staining showing the migration ability of RAW264.7 cells after indicated treatment. Scale bar: 200 μm. Data are represented as mean ± SEM. * P < 0.05, ** P < 0.01, *** P < 0.001.

Supplementary Tables

Table S1. The sequences of each single-stranded DNA (ssDNA).

| ssDNA | Sequences (from 5′ to 3′) |
| --- | --- |
| S1 | ATTTATCACCCGCCATAGTAGACGTATCACCAGGCAGTTGAGACGAACATTCCTAAGTCTGAA |
| S2 | ACATGCGAGGGTCCAATACCGACGATTACAGCTTGCTACACGATTCAGACTTAGGAATGTTCG |
| S3 | ACTACTATGGCGGGTGATAAAACGTGTAGCAAGCTGTAATCGAGGGAAGAGCATGCCCATCC |
| S4 | ACGGTATTGGACCCTCGCATGACTCAACTGCCTGGTGATACGAGGATGGGCATGCTCTTCCCG |

Table S2. Sequences of forward and reverse primers of the housekeeper gene and related genes designed for qRT-PCR.

| Gene | Primer Sequence (from 5′ to 3′) |
| --- | --- |
| Gapdh (Murine) | F 5’- TGTTTCCTCGTCCCGTAGA -3’ R 5’- ATCTCCACTTTGCCACTGC -3’ |
| Gapdh (human) | F 5’- GCCAACGTGTCAGTGGTG -3’ R 5’- AAGGTGGAGGAGTGGGTGT -3’ |
| Ocn (human) | F 5’- GGCGCTACCTGTATCAATGG -3’ R 5’- GTGGTCAGCCAACTCGTCA -3’ |
| Opn (human) | F 5’- CTCCATTGACTCGAACGACTC -3’ R 5’- CAGGTCTGCGAAACTTCTTAGAT -3’ |
| Runx-2 (human) | F 5’- TGGTTACTGTCATGGCGGGTA -3’ R 5’- TCTCAGATCGTTGAACCTGCTA -3’ |
| Osterix (human) | F 5’- CTCCTTTCACCTGCAGGCAG -3’ R 5’- CAGACAGTCAGAAGAGCTGT -3’ |
| Alp (human) | F 5’- ACTGGTACTCAGACAACGAGAT -3’ R 5’- ACGTCAATGTCCCTGATGTTATG -3’ |
| Tnf-α (Murine) | F 5’- CCCTCACACTCAGATCATCTTCT -3’ R 5’- GCTACGACGTGGGCTACAG -3’ |
| Inos (Murine) | F 5’- GTTCTCAGCCCAACAATACAAGA -3’ R 5’- GTGGACGGGTCGATGTCAC -3’ |
| Arg-1 (Murine) | F 5’- ACATTGGCTTGCGAGACGTA -3’ R 5’- ATCACCTTGCCAATCCCCAG -3’ |
| Tgf-β (Murine) | F 5’- CTCCCGTGGCTTCTAGTGC -3’ R 5’- GCCTTAGTTTGGACAGGATCTG -3’ |
| Cd206 (Murine) | F 5’- ATGGATTGCCCTGAACAGCA -3’ R 5’- CTCGTCAGCACCCCAGTTAG -3’ |
| Il-1β (Murine) | F 5’- GTATGGGCTGGACTGTTTC -3’ R 5’- GCTGTCTGCTCATTCACG -3’ |

Table S3. Comparison of the tFNAs-rGO complex with previously published biomaterials in root bone related diseases.

| Biomaterial | Component | Preparation method | Main results | Advantages | Disadvantages | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| tFNAs-rGO complex | tFNAs, rGO | Self-assembly | Enhanced osteogenic differentiation of PDLCs and facilitated M2-phenotype polarization of macrophages to ameliorate OIRR | Simple synthesis, high reproducibility, relatively stability, and dual functionality | Metabolism, immunoreaction unknown | Our study |
| Melt electrowriting scaffolds | 3D printed bone compartment, melt electrospun PDL compartment | Melt electrowriting | Guided periodontal ligament fiber attachment to the tooth root and alveolar bone interfaces, achieved periodontal regeneration | Porous, highly adaptable | Complex preparation, high equipment requirements | [1] |
| Nanofibrous membrane | Magnesium oxide nanoparticles, pol/gelatin | Electrospun | Guided periodontal tissue regeneration | Early antibacterial activity, elevated tensile strength | Short antibacterial time limit, broad spectrum antibacterial activity unknown | [2] |
| 3D matrix | Collagen, sodium alginate and titanium oxide | Fibrin precipitation, freeze-drying | Supported the differentiation of the HPLF cells into osteoblastogenic lineage cells in-vitro | High porosity, stiffness | Effect in vivo remains to be confirmed | [3] |
| Acerogenin peptide | Tyrosine, enamel matrix derivative | High performance liquid chromatography | Stimulated migration of human periodontal ligament cells and HUVECs | Commercialization of basic materials | Complex and unclear composition | [4] |
| Nanoparticle | Fibrin chitosan matrices, ε-aminocaproic acid | Fibrin precipitation, tripolyphosphate initiated ionic gelation | Developed structural integrations of the cementum-periodontal ligament-bone complex | Feasibility of tooth roof-of-furcation defects regeneration | Complex composition | [5] |
| Platelet-derived growth factor | Chitosan/coral composites, platelet-derived growth factor B | Freeze-drying | Promoted HPLCs proliferation and periodontal regeneration | Large internal surface, easy plasticity | Transient effectiveness, immunogenicity | [6] |
| Hydrogel | β-glycerophosphate, chitosan | Steam sterilization, aggregation induced self-assembly | Promoted periodontal tissue regeneration class III furcation defects | Temperature control, biocompatibility | Unclear immunological response, poor mechanical performance | [7] |
| Scaffold/hydrogel membrane | Wollastonite scaffolds, gelatin hydrogel | Digital light processing, photo-crosslinked technique | Exhibited favorable cell viability and osteogenic ability, a strong periodontal regeneration capability | Precise tissue regeneration | Complicated technology, high-level equipment | [8] |

Reference

1.	Staples R, Ivanovski S, Vaswani K, Vaquette C: Melt electrowriting scaffolds with fibre-guiding features for periodontal attachment. Acta Biomaterialia 2024, 180:337-357.

2.	Liu X, He X, Jin D, Wu S, Wang H, Yin M, Aldalbahi A, El-Newehy M, Mo X, Wu J: A biodegradable multifunctional nanofibrous membrane for periodontal tissue regeneration. Acta Biomaterialia 2020, 108:207-222.

3.	Elango J, Selvaganapathy PR, Lazzari G, Bao B, Wenhui W: Biomimetic collagen-sodium alginate-titanium oxide (TiO2) 3D matrix supports differentiated periodontal ligament fibroblasts growth for periodontal tissue regeneration. International Journal of Biological Macromolecules 2020, 163.

4.	Jonke E, Gemperli AC, Zhang T, Özdemir B, Dard M, Rausch-Fan X, Andrukhov O: Effect of tyrosine-rich amelogenin peptide on behavior and differentiation of endothelial cells. Clinical Oral Investigations 2016, 20:2275-2284.

5.	Park CH, Oh J-H, Jung H-M, Choi Y, Rahman SU, Kim S, Kim T-I, Shin H-I, Lee Y-S, Yu FH, et al: Effects of the incorporation of ε-aminocaproic acid/chitosan particles to fibrin on cementoblast differentiation and cementum regeneration. Acta Biomaterialia 2017, 61:134-143.

6.	Zhang Y, Wang Y, Shi B, Cheng X: A platelet-derived growth factor releasing chitosan/coral composite scaffold for periodontal tissue engineering. Biomaterials 2007, 28:1515-1522.

7.	Zang S, Dong G, Peng B, Xu J, Ma Z, Wang X, Liu L, Wang Q: A comparison of physicochemical properties of sterilized chitosan hydrogel and its applicability in a canine model of periodontal regeneration. Carbohydrate Polymers 2014, 113:240-248.

8.	Wei Y, Wang Z, Han J, Jiang X, Lei L, Yang X, Sun W, Gou Z, Chen L: Modularized bioceramic scaffold/hydrogel membrane hierarchical architecture beneficial for periodontal tissue regeneration in dogs. Biomaterials Research 2022, 26:68.