Supporting Information

Recent advances in self-targeting natural product-based nanomedicines

Haifan Liua,b,†, Xingyue Jina,c,†, Suyi Liua,c, Xinyue Liua,b, Xiao Peia, Kunhui Suna,c, Meifang Lia, Ping Wanga, Yanxu Changc, Tiejie Wanga,b, *, Bing Wanga,b, *, Xie-an Yua, *

a NMPA Key Laboratory for Bioequivalence Research of Generic Drug Evaluation, NMPA Key Laboratory for Quality Research and Evaluation of Traditional Chinese Medicine, Shenzhen Institute for Drug Control, Shenzhen 518057, China

b School of Pharmacy, Shenyang Pharmaceutical University, Shenyang 110016, China

c State Key Laboratory of Component-based Chinese Medicine, Tianjin University of Traditional Chinese Medicine, Tianjin 301617, China

† These authors contributed equally.

* Corresponding author.

E-mail address: szyjwtj@163.com (T.W.); wangbingszyj@163.com (B.W.); yuxieanalj@126.com (X.Y.).

Table S1. Summary of Nano TCM applications in different diseases

| No. | TCM | Type | Disadvantage | Targeting Module | Synthesizing Methods | Size | Electric Potential | NPs | Targeted Areas | Targeted Strategy | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Gypenosides (Gyp) | terpenoid | Low solubility and bioavailability | PLGA | a modified nano-precipitation technique combined with self-assembly | 128 ± 5.89 | -35.6 ± 3.18 | PLGA-Gyp XLIX NPs | unilateral ureteral occlusion Kidney | / | [167] |
| 2 | Triptolide | terpenoid | Highly hydrophobic, poor bioavailability, weak targeting ability | DSPE-tk-PEG | Ultrasound, stirring, etc. | 98.000 | -23.60 | (TP+A)@TkPEG NPs | tumour | / | [181] |
| 3 | Ursolic acid (UA) and Astragaloside IV (AS-IV) | terpenoid | weak water solubility and targeting | HA | three-step synthetic procedure (Polymerization and Coating) | 200-240 | -38.1 or -41.2 | UA/ (AS-IV) @PDA-HA | tumour | HA specifically binds to cluster of differentiation 44 (CD44), which was overexpressed on the surface of most cancer cells. | [157] |
| 4 | EGCG | phenolics | / | PEG-EGCG | SU and PEG-EGCG self-assembled into the MNC through the SU−EGCG interaction by hydrating a film of SU and PEG-EGCG mixture | 167.4 ± 2.4 | 5.4 ± 1.3 | SU-MNC | tumour | ERP | [166] |
| 5 | Dihydroartemisinin and tetrandrine | terpenoid | Solubility differences and instability | 1,2-Dioleoyl-n-glycero-3-phosphoethanolamine (DOPE)(liposome) | / | 112.20 ± 4.80 | -8.63 ± 0.74 | DHA-TET pH-sensitive LPs | tumour | / | [215] |
| 6 | Diosgenin | steroids | Low intracellular permeability, rapid in vivo clearance, poor targeting | polyethylene glycol (PEG) | stirring | 165.4 ± 5.4 | / | DOX/NPs | tumour | EPR | [209] |
| 7 | Triptolide | terpenoid | liver and kidney impairment | HER2 antibodies | magnetic stirring | 73.4 ± 5.2 | -57.3 ± 6.69 – -21.1 ± 4.73 | TPLNP | tumour | Specific targeting was clearly demonstrated in cell lines overexpressing HER2 | [192] |
| 8 | Paclitaxel | terpenoid | May cause bone marrow depression and liver and kidney toxicity | albumin nanoparticles | stirred, homogenized and emulsified, ultrafiltration, lyophilize | 87.63 ± 1.15 | 11.7 ± 0.61 | Nab-PTX-PA | tumour | Active targeting mediated by gp60 cytosolic protein-SPARC | [175] |
| 9 | Quercetin (Qu) | flavonoids | Poor targeting ability and water solubility | outer cancer cell membranes (CM) | mechanical mixing method | 115.2 ± 6.4 | -10 | CQM | tumour | Nanoparticles coated with tumour cell membranes have good tumour tissue targeting properties | [176] |
| 10 | Paclitaxel (Ptx) combined with tanshinone IIA (TanIIA) | terpenoid | Low solubility | folic acid | stirring | 298.8 ± 10.5 | -51.6 ± 0.6 | (Ptx + TanIIA)@FA-LB-MSNs | tumour | Bioadhesion between FA and its receptors | [210] |
| 11 | Angelica polysaccharides | polysaccharides | / | angelica polysaccharide | self-assembly method | 129.00 ± 3.32 | -28.45 ± 0.22 | AP-PP-DOX | tumour | Angelica sinensis polysaccharide targets tumours | [207] |
| 12 | Emodin | anthraquinones | / | R8GD | Thin film dispersion method | 103.33 ± 2.49 | 2.88 ± 0.47 | R8GD modified emodin liposomes | tumour | R8GD significantly enhanced liposome targeting | [182] |
| 13 | Ginsenoside Rh2 | terpenoid | / | Liposomes + ginsenoside Rh2 | thin-flm hydration method | 99.03 | / | PTX-Rh2-lipo | tumour | Ginsenoside Rh2 strongly enhanced liposome accumulation in tumours by interacting with tumour cell glucose transporters | [183] |
| 14 | astragaloside IV | terpenoid | Poor water solubility | Liposomes + Folic Acid | Ethanol injection-ammonium sulphate gradient method | 100 | / | FA-R8-LPs-DOX/AS | tumour | Folate receptor (FR) expressed at high levels on the surface of many malignant tumour cells | [173] |
| 15 | Andrographolide | terpenoid | Poor water solubility, short half-life, low permeability | liposome | Melt-emulsification and ultrasound | 193.840 | -22.80 | AND-SLN | spleen and thymus | EPR | [147] |
| 16 | Glabridin (Gla) | flavonoids | Poor water solubility and stability | Polyethylene glycol-distearoyl phosphatidylethanolamine (PEG-DSPE) | double-emulsion method (Dual Emulsion Method) | 80.67 ± 5.71 | -3.57 ± 0.12 | Cy5-NP(Gla) -5k | spleen | EPR | [148] |
| 17 | Tanshinone | quinone | Side effects and non-selectivity | PSMA targeting ligand | emulsification and solvent-diffusion method | 139.7 ± 4.1 | 11.2 ± 1.6 | P-N-DOX/TAN | PSMA on prostate cancer cells | Prostate-specific membrane antigen targeting | [208] |
| 18 | Triptolide | terpenoid | Severe acute cytotoxicity | liposome | / | 137 | / | PEG-TRX-TP-LP/ CA IX-TP-Lips | mesangial cells (MCs)/tumour | Anti-carbonic anhydrase IX antibody (CA IX) significantly recognised carbonic anhydrase IX overexpressed on the surface of lung cancer cells | [159] |
| 19 | Curcumin | phenolics | Low solubility and bioavailability | D-mannose（Man） | Combined electrostatically driven self-deposition and solvent hydration/lyophilization | 3322 ± 14.697 | / | Man-CUR NYPs | macrophage | By binding to macrophage-associated receptors | [191] |
| 20 | Melittin | amino acid derivatives | Narrow safe dose range and haemolytic side effects | Lipid nanoparticles | Vortex, ultrasound, etc. | 10–20 | / | α-melittin-NPs | lymphatic node (LNs) | Size required for optimal lymph nodes with targeted nanovaccines | [146] |
| 21 | Baicalin | flavonoids | Poor bioavailability and solubility | nanoliposomes | / | / | / | / | lung | / | [156] |
| 22 | Curcumin and Platycodon grandiflorum polysaccharides(PGP) | polysaccharides/phenolics | weak water solubility and targeting | Platycodon grandiflorum polysaccharides and macrophage membranes | Membrane hydration method | 91.100 | / | MNPs@Cur | lung | Inherent affinity of macrophages for sites of inflammation | [153] |
| 23 | Arctiin (ARC) | phenylpropanoid | weak water solubility and targeting | / | the solvent precursor method | 185.5 ± 22.3 | -31.8 ± 8.36 | ARC@DPBNPs | lung | Pulmonary route of administration. | [161] |
| 24 | Quercetin (Qu) | flavonoids | low solubility and bioavailability | / | the emulsion polymerization method | 61.870 | approximately -30 | QU-Nanogel | lung | Ultrasonic aerosol inhalation administration. | [154] |
| 25 | Daphnoretin | phenylpropanoid | Poor solubility | Glycyrrhetinic acid | Film hydration method | 151.9 | -13.82 ± 0.66 | GPP/PP-DAP | liver tumour | glycyrrhizic acid specifically bound to the glycyrrhizic acid receptor (GA-R) and targeted to the hepatocyte membrane | [96] |
| 26 | Angelica Polysaccharide | polysaccharides/phenolics | Poor water solubility | Angelica Polysaccharide (ASP) | the self-assembly method | 194.5 | -28.23 | AAAF@Cur | liver | ASP has a high affinity for salivary glycoprotein receptors (ASGPR), and polymeric micelles can be used as an instinctive liver-targeted drug delivery vehicle due to ASP liver targeting. | [40] |
| 27 | Mulberry leaf polysaccharides (MP) and luteolin | polysaccharides/flavonoids | Poor water solubility and non-targeted release | Gal-NH2 | magnetically stirred | 77.8 ± 2.6 | 0.22 ± 0.06 | Gal-MPL/Lut nanoparticles | liver | The nanoparticles enhanced the effect on liver tissue by specifically recognising the asialoglycoprotein receptor (ASGPR) | [85] |
| 28 | Rhein | anthraquinones | Poor solubility, short half-life, low renal accumulation, low bioavailability | kidney targeting peptide | / | 59.5 ± 6.2 | -3.7 ± 4.3 | KLPPR | kidney | KTP (Sequence: CSAVPLC) decorated with KTP could promote uptake and endocytosis by renal cells via non-lysosomal pathways and could enter the kidney through the glomerular filtration membrane in the particle size range of 30 ~ 80 nm. | [165] |
| 29 | Glycyrrhetinic acid/Curcumin | terpenoid/phenolics | Low solubility and bioavailability | GA | / | 110 | -25.27 ± 0.57 | MSN-GA-CUR | hepatocellular carcinoma cell | Mammalian hepatocytes had GA receptor expression | [84] |
| 30 | Glycyrrhetinic acid | terpenoid | / | GA | / | 200 | -15.2 – -23.5 | DOX/GCDPu NPs | hepatocellular carcinoma cell | GA receptor expressed highly in hepatocytes and hepatocellular carcinoma cells | [90] |
| 31 | Glycyrrhetinic acid | terpenoid | / | GA | / | 170 | / | GA-CS-PEI-HBA-DOX | hepatocellular carcinoma cell | GA receptors primarily found on the surface of mammalian hepatocytes recognise GA ligands | [92] |
| 32 | Glycyrrhizic acid (GA) | terpenoid | / | GA | Solvent evaporation method | 126.47 ± 3.74 | -14.72 ± 2.47 | AGP-GA-PPP | hepatocellular carcinoma cell | Targeted binding sites of GA expressed highly in HCC cells | [91] |
| 33 | Glycyrrhizic acid (GA) | terpenoid | / | GA | Solvent evaporation method | 133.6 ± 1.2 | -16.3 | ETO-TGA PMs | hepatocellular carcinoma cell | GA receptor expressed abundantly on the surface of hepatocytes | [93] |
| 34 | Glycyrrhizic acid (GA) | terpenoid | / | GA | / | 100 | -25 | GPND/siRNA | hepatocellular carcinoma cell | GA selectively targeted to hepatocytes | [95] |
| 35 | Triptolide | terpenoid | Poor solubility and bioavailability, adverse side effects | transferrin (a protein that transforms ironmongery and reproduces ferritin in blood) | Thin film hydration method | 130.33 ± 1.89 | -23.20 ± 0.90 | TF-TP@LIP | hepatocellular carcinoma cell | HepG2 could over-express transferrin receptor (TFR) | [100] |
| 36 | Echinacoside | phenethyl alcohol | Malabsorption and low bioavailability | ECH | sol–gel method/ stirring magnetically | approximately 200 | / | ECH@ Au@MSN-PEGDE-GAL/ECH@AMPG | hepatocellular carcinoma (UBR5) | ECH is targeting UBR5 expressed in HCC | [86] |
| 37 | Notoginsenoside R1 | terpenoid | Very poor oral utilisation | CD11b monoclonal antibody | / | 83.000 | -32.50 | MSN-NGR1-CD11b antibody nanoparticles | heart | In the early stages of myocardial infarction, CD11b-expressing monocytes and neutrophils accumulate at the infarct site | [136] |
| 38 | Muscone/Docetaxel | ketones/terpenoid | / | Muscarinone/Mouse Monoclonal Antibody RI7217 | / | 155.2 ± 5.8 | -32.0 ± 1.9 | RI-LP-M | glioma | Musk ketone could change the permeability of the blood-brain barrier, transferrin receptor (TfR) was overexpressed in brain capillary endothelial cells (hCMEC/D3) and glioma cells, and the mouse monoclonal antibody, RI7217, had a high affinity and selectivity for TfR | [124] |
| 39 | Tanshinone IIA/Glycyrrhizic acid (GA) | terpenoid | Bad water solubility, excessive metabolism in vivo, poor targeting, some degree of haemolysis | transferrin (Tf) | Ultrasonic degradation method | 153.5 ± 10.2 | -4.69 ± 1.31 | CpG-EXO/TGM | glioblastoma cells | Serum-derived EXO also has expressed abundant TfR, which can be targeted to the brain by binding to free Tf in the bloodstream | [116] |
| 40 | Fat-soluble contents were extracted from Lycium barbarum (LB) | / | / | / | vortex, etc. | 189.200 | -34.90 | LB lipid-derived NPs | colonic tissue (inflammatory) | Effective taken up by UC treatment-associated target cells (macrophages) | [190] |
| 41 | Emodin | anthraquinones | Poor water solubility, low bioavailability, poor targeting ability | lactoferrin and yeast cell wall particles (YPs) | Novel solvent hydration/freeze-drying electrostatic-driven self-deposition technique, dialysis | 157.99 ± 0.13 | approximately 5.70 | EMO-NYPs | colonic epithelial cells/macrophages | EMO-NPs and EMO-NYPs targeted Lf and dection-1 receptors on the cell membrane of Caco-2 cells and macrophages respectively | [188] |
| 42 | Paris saponin VII | steroids | Poor solubility, no selective distribution in the body, causing severe haemolysis | Modified citrus pectin nanoparticles | stirred, ultrasound, lyophilization | 104 | -29.62 | PSVII@MCP-CaP | colon Cancer Cells | Galactose lectin-3 (Gal-3) expressed highly on the cell membrane of drug-resistant colon cancer cells and modified citrus pectin (MCP) selectively binds to Gal-3 | [187] |
| 43 | Tangeretin (TAGE) | flavonoids | / | RGD | / | 156.9 ± 4.1 | -17.1 | RGD-ATST/TAGE CNPs | colon cancer | Several synthetic peptide-containing cyclised arginine-glycine (RGD) sequences have high affinity for the αvβ3 integrin receptor, which is specifically overexpressed in selected tumour cells | [189] |
| 44 | Resveratrol and salidroside (Sal) | phenolics | Bad specificity, low solubility, insufficient blood-brain barrier penetration | apolipoprotein E | Liposome membrane hydration method | 95–140 | -1.00 | ApoE-Res/Sal-Lips | central nervous system | ApoE could target both LRP1 and LDLR receptors that were highly expressed in the blood-brain barrier | [114] |
| 45 | Curcumin/Astragalus Polysacharin/Quercetin | phenolics/polysaccharides/flavonoids | Low water solubility, poor solubility, low bioavailability | Folic Acid (FA) | Methods of dialysis | 132.2 ± 9.4 | -33.71 ± 4.8 | QDAF@Cur | breast tumour | Folic acid (FA) associates specifically with folate receptors on the surface of tumour cells | [174] |
| 46 | Docetaxel | terpenoid | Insoluble in water, serious side effects | Brief peptide composed of arginine-glycine-aspartic acid (RGD) | stirred | 16.44 ± 1.35 | -19.24 ± 1.24 | RGD-DTX-M | breast cancer cells | αVβ3 expression is higher in breast cancer cells than in normal cells, especially in metastatic breast tumours, and RGD peptides recognise αvβ3 receptors expressed on the surface of tumour cells and tumour blood vessels | [178] |
| 47 | Docetaxel | terpenoid | Low solubility, low osmolality, non-targeting and toxic effects | Folic acid receptor (FR) | improved emulsification-solvent evaporation method | 182.38 ± 1.57 | -1.18 ± 0.01 | FA-PEG-DA-PAE-Chol nanoparticles/ DTX, FPDPCNPs/DTX | breast cancer cells | Folate receptors specifically overexpressed on the surface of malignant tumour cells and so have an FR-mediated targeting effect | [179] |
| 48 | Muscone/Docetaxel | ketones/terpenoid | / | Lf | thin film dispersion | 144.6 ± 3.1 | -30.3 ± 1.6 mV | Lf-LP-Mu-DTX | brain/blood-brain barrier | Lactoferrin receptors were overexpressed in both brain endothelial cells and glioma cells, and muscimol ketone allowed liposomes to enter the brain | [126] |
| 49 | Dihydroartemisinin | terpenoid | Poor water solubility, short retention time in blood | lactoferrin | Nano-coprecipitation method | 120.5 | -28.2 | L-D-I/NPs | brain/blood-brain barrier | Lactoferrin could interact with low-density lipoprotein receptor-related protein-1 (LRP1) | [112] |
| 50 | Baicalin | flavonoids | Low solubility | macrophage membrane | squeezing method | 182.33 | / | MM-BA-LP | brain/blood-brain barrier | Macrophage Cell Membrane Modifications Easier to Cross the Blood-Brain Barrier | [113] |
| 51 | Icariin/Tanshinone IIA | flavonoids/terpenoid | Poor water solubility and bioavailability | Aniopep-2/liposome | Thin film hydration method | 111.26 ± 11.65 | -1.53 ± 0.38 | Ang2-ICA/TSIIA | brain/blood-brain barrier | Low-density lipoprotein receptor-related protein-1 (LRP1) was overexpressed on the blood-brain barrier and Angiopep-2 had a high binding efficiency to LRP1 | [129] |
| 52 | Emodin | anthraquinones | Low targeting | PEGylation and cRGD modifcation | thin film dispersion method | 92 | / | Em-Lip | brain | Cyclic Arg-Gly-Asp (cRGD) peptide ligand given liposomes access to brain targeting | [119] |
| 53 | Cannabidiol | phenolics | Low water solubility, poor bioavailability, slow brain targeting | Bionic macrophage membrane vesicles | Liposome extruders | 224 | / | CMNV | blood-brain barrier | Macrophage membranes could deliver drugs across the blood-brain barrier | [123] |
| 54 | (-)-Borneol/Baicalin | terpenoid/flavonoids | Low solubility and bioavailability, difficult to penetrate the blood-brain barrier | borneol | / | / | / | BO-BA-LP | blood-brain barrier | borneol | [111] |
| 55 | Rhynchophylline | alkaloids | Low water solubility, bioavailability and blood-brain barrier penetration | Tween 80 | nanoprecipitation method | 145.2 | / | T80-NPS-RIN | blood-brain barrier | Tween 80-coated nanoparticles crossed the blood-brain barrier by LRPs-mediated cytosis | [121] |
| 56 | Curcumin | phenolics | Poor bioavailability and water solubility | Bioperine and PLGA | the single emulsion-solvent evaporation method | 293 ± 4.15 or 181 ± 8.63 | −21 ± 0.88 or −17.6 ± 0.33 | Cur-Bio PLGA NPs | Atherosclerotic plaque sites | / | [138] |
| 57 | Curcumin | phenolics | Low water solubility and poor bioavailability | / | in situ synthesis | aperture 63.020 Å | / | CCM@SBA-15/PDA/Ag | / | / | [152] |
| 58 | Puerarin | flavonoids | Poor water and fat solubility | / | in situ self-assembly | approximately 170 | / | CHP@Si | / | / | [137] |
| 59 | Glycyrrhizic acid (GA) | terpenoid | / | / | One-pot hydrothermal method and self-assembly | approximately 20–200 | / | GA/WS-CQDs hydrogels | / | / | [213] |
| 60 | Curcumin | phenolics | Difficult water solubility, low gastrointestinal absorption rate | / | nanoprecipitation | approximately 150 | / | Cur@SF NPs | / | / | [141] |
| 61 | Pterostilbene | styrenics | Easily oxidised, poorly soluble in water, and low oral bioavailability | / | one-pot synthesis | 150 - 250 | -15–-30 | p (AAPBA-b-PTE) NPs | / | / | [216] |
| 62 | Emodin | anthraquinones | Low solubility | Erythrocytes and macrophages fused into a mixed membrane (EMHM) | / | 170 ± 20 | / | EG@EMHM NPs | / | / | [212] |
| 63 | Baicalein | flavonoids | low solubility and bioavailability | / | / | 285 ± 25 | -2.50 | L-B-NP and E-B-NP | / | / | [155] |
| 64 | Methanolic extracts from Ocimum basilicum, Rosemarinus officinalis, and Thymus vulgaris | / | / | Silicon dioxide nanocarriers | stirring | 48.000 | / | SNBs | / | Particle size less than 50nm | [211] |
| 65 | Triptolide | terpenoid | Narrow therapeutic window, poor water solubility, rapid metabolism | / | / | ＜100 | / | / | / | Targeted drug delivery systems (TDDS) and EPR and binding to specific receptors in the tumour tissue microenvironment or on the cell surface alone | [8] |
| 66 | Shikonine | quinone | / | / | / | / | / | / | / | / | [77] |

Table S2. List of abbreviations and sources of natural product active ingredients

| No. | TCM | Abbreviation | Type | Source |
| --- | --- | --- | --- | --- |
| 1 | Rhein | - | anthraquinones | Radix Rhei Et Rhizome, Sennae Folium, Polygoni Cuspidati Rhizoma Et Radix and etc. |
| 2 | Hypericin | - | quinone | Sedi Herba, Hyperici Japonici Herber and etc. |
| 3 | Saikosaponin | - | saponins | Radix Bupleuri |
| 4 | Platycodon saponin | - | saponins | Platycodon grandiflorum |
| 5 | Liquorice proteins | - | terpenoid | Licorice |
| 6 | Angelica protein | - | - | Chinese angelica |
| 7 | Danpi polysaccharide | - | polysaccharides | Moutan Cortex |
| 8 | Berberine | BBR | alkaloids | Phellodendri Amurensis Cortex, Phellodendri Chinrnsis Cortex, Coptidis Rhizoma and etc. |
| 9 | Hesperetin | - | flavonoids | Lobeliae Chinensis Herba, Stephaniae Tetrandrae Radix, Lysimachiae Herba and etc. |
| 10 | Ursolic acid | UA | terpenoid | Ligustrum lucidum Ait., Eriobotrya japonica (Thunb.) Lindl., Prunella vulgaris L. and etc. |
| 11 | Lentinan | - | polysaccharides | Lentinus edodes |
| 12 | Baicalin | - | flavonoids | Arum Ternatum Thunb., Scutellariae Barbatae Herba, Radix Bupleuri and etc. |
| 13 | Celastrol | - | terpenoid | Tripterygii Radix and Celastri Orbiculati Fructus |
| 14 | Erianin | - | aromatic | Dendrobii Caulis |
| 15 | Glycyrrhetinic acid | GA | terpenoids | licorice and Abri Herba |
| 16 | Daphnoretin | DAP | phenylpropanoids | Wikstroemiae Indicae Rasix |
| 17 | Angelica sinensis polysaccharide | ASP | polysaccharides | Angelicae Sinensis Radix |
| 18 | Gambogic acid | - | flavonoids | Garcinia hanburyiHook.f. |
| 19 | Leonurine | - | alkaloids | Cistanches Herba and Leonuri Herba |
| 20 | Ginsenoside Rg3 | - | terpenoid | Ginsen Radix Et Rhizoma Rubra |
| 21 | Silybin | - | flavonoids | Silybum Marianum |
| 22 | Paclitaxel | - | alkaloids | Taxus chinensis |
| 23 | Glycyrrhizic Acid | GL | terpenoids | Licorice, Puerariae Flos, Amygdalus Communis Vas and etc. |
| 24 | Andrographolide | AGP | terpenoids | Andrographis Herba |
| 25 | Oleanolic acid | OA | terpenoid | Fructus Ligustri Lucidi |
| 26 | Curcumin | CUR | phenols | Alpiniae Officinarum Rhizome, Momordicae Fructus and Curcumae Radix |
| 27 | Echinacoside | ECH | phenethyl | Rehmanniae Radix Praeparata |
| 28 | Triptolide | TP | terpenoids | Tripterygii Radix |
| 29 | Matrine | - | alkaloids | Sophorae Flavescentis Radix |
| 30 | Camptothecin | CPT | alkaloids | Sesami Nigrum Semen |
| 31 | Resveratrol | Res | phenols | Veratrum album |
| 32 | Salidroside | Sal | phenols | Sargentodoxae Caulis, Scutellariae Radix, Sedum Aizoon L. and etc. |
| 33 | Tanshinone IIA | TanIIA | terpenoid | Radix Salviae and Peucedani Radix |
| 34 | Emodin | EMO | anthraquinones | Ampelopsis Japonica, Lilii Bulbus, Isatidis Radix and etc. |
| 35 | Rhynchophylline | RIN | alkaloids | Uncariae Ramulus Cumuncis |
| 36 | Cannabidiol | CBD | phenolics | Cannabis Sativa L. |
| 37 | Muscone | - | ketones | Moschus |
| 38 | Docetaxel | DTX | terpenoid | Synthesized from extracts of Taxus baccata L. |
| 39 | Borneol | BO | terpenoid | Borneolum Syntheticum |
| 40 | Icariin | - | flavonoids | Epimrdii Herba |
| 41 | Dihydroartemisinin | DHA | terpenoid | Artemisia Annua L. |
| 42 | Vinpocetine | - | alkaloids | Synthesized from extracts of Vincamajor |
| 43 | Notoginsenoside R1 | NGR1 | terpenoid | Panacis Japonici Rhizoma |
| 44 | Puerarin | - | flavonoids | Radix Bupleuri, Cyathulae Radix, Puerariae Flos and etc. |
| 45 | Glabridin | Gla | flavonoids | Licorice and Amygdalus Communis Vas |
| 46 | Quercetin | Qu | flavonoids | Platycladi Cacumen, Farfarae Flos, Ginkgo Folium and etc. |
| 47 | Platycodonopsis polysaccharide | PGP | polysaccharides | Platycodon Grandiforus |
| 48 | Baicalein | BA | flavonoids | Scutellariae Radix, Phellodendri Amurensis Cortex, Scutellariae Barbatae Herba and etc. |
| 49 | Astragaloside IV | AS-IV | terpenoid | Hedysarum Multijugum Maxim. |
| 50 | Arctiin | ARC | phenylpropanoid | Fructus Arctii, Trachelospermumjasminoides and Forsythiae Fructus |
| 51 | Podophyllotoxin | PPT | - | Dysosmae Verspiellis Rhixoma Et Radix |
| 52 | Ginsenoside Rb1 | GRb1 | terpenoid | Panax Ginseng C. A. Mey., Ginsen Radix Et Rhizoma Rubra and Panacis Japonici Rhizoma |
| 53 | Epigallocatechin-3-O-gallate | EGCG | phenolics | Ginkgo Semen, Eriobotryae Folium and Phyllanthi Fructus |
| 54 | Astragalus polysaccharide | APS | polysaccharides | Astragali Radix |
| 55 | Ginsenoside Rh2 | - | terpenoid | Ginsen Radix Et Rhizoma Rubra |
| 56 | Lycium barbarum | LB | - | Lycii Fructus |
| 57 | Paris saponin VII | PSVII | saponins | Trillium tschonoskii |
| 58 | Tangeretin | TAGE | flavonoids | Citrus Reticulata, Citri Grandis Exocarpium and Citri Reticulatae Pericarpium Viride |
| 59 | Magnoliol | MAG | phenolics | Magnolia Officinalis Rehd Et Wils. |
| 60 | Gallic acid | - | phenolics | Ampelopsis Japonica, Radix Aconiti Kusnezoffii and Cortex Hibisci |
| 61 | Cinnamic acid | - | organic Acid | Cinnanmomi Cortex |
| 62 | Rhamnoolipid | RHL | polysaccharide | Rhamnus davurica Pall |
| 63 | Chlorogenic acid | CGA | phenylpropanoids | Anisi Stellati Fructus, Imperatae Rhizoma, Stemonae Radix and Glehniae Radix |
| 64 | Diosgenin | - | steroids | Anemarrhenae Rhizoma and Rhizoma Dioscoreae Nipponicae |
| 65 | Glycyrrhizin | - | terpenoid | licorice |
| 66 | Tetrahydroartemisinin | TET | terpenoid | Artemisia Annua L. |
| 67 | pterostilbene | - | styrenics | Notopterygii Rhizoma Et Radix |
| 68 | Luteolin | - | flavonoids | Ajugae Decumbentis Herba |
| 69 | Ellagic acid | - | phenolics | Rubi Fructus, Euphorbiae Humifusae Herba and Radix Paeoniae Rubra |

Table S3. Abbreviated table

| No. | Full Name | Abbreviation |
| --- | --- | --- |
| 1 | Traditional Chinese medicine | TCM |
| 2 | Folic acid | FA |
| 3 | Colorectal cancer | CRC |
| 4 | Alzheimer’s disease | AD |
| 5 | Cyclodextrin | CD |
| 6 | Prussian blue | Pu |
| 7 | Graphene oxide | GO |
| 8 | PEGyl-block poly (D, L-lactic acid) | PEG-PLA |
| 9 | Mesoporous silica nanoparticles | MSN |
| 10 | Glycyrrhetinic acid receptor | GA-R |
| 11 | Asialoglycoprotein receptor | ASGP-R |
| 12 | Hepatocellular carcinoma | HCC |
| 13 | Blood-brain barrier | BBB |
| 14 | Doxorubicin | DOX |
| 15 | Enhanced permeability and retention | EPR |
| 16 | Transferrin receptor | TfR |
| 17 | Lipoprotein receptor-associated protein 1 | LRP1 |
| 18 | Post-traumatic stress disorder | PTSD |
| 19 | Cerebral ischaemia-reperfusion injury | CIRI |
| 20 | Indocyanine green | ICG |
| 21 | Myocardial infarction | MI |
| 22 | Friedreich's ataxia | FRDA |
| 23 | Acute lung injury | ALI |
| 24 | Reactive oxygen species | ROS |
| 25 | Non-small cell lung cancer | NSCLC |
| 26 | Polydopamine | PDA |
| 27 | Carbonic anhydrase IX | CAIX |
| 28 | Idiopathic pulmonary fibrosis | IPF |
| 29 | Alveolar epithelial type 2 | AEC2 |
| 30 | Acute kidney injury | AKI |
| 31 | Iodine contrast media | ICM |
| 32 | Polylactic acid-glycolic acid | PLGA |
| 33 | Kidney-targeting peptide | KTP |
| 34 | Gibberellin | Gyp |
| 35 | Unilateral ureteral occlusion | UUO |
| 36 | Folate receptor | FR |
| 37 | Cell membranes | CM |
| 38 | Human epidermal growth factor receptor 2 | HER2 |
| 39 | Modified citrus pectin | MCP |
| 40 | Inflammatory bowel disease | IBD |
| 41 | Ulcerative colitis | UC |
| 42 | Multidrug-resistant Staphylococcus aureus | MRSA |
| 43 | Acute promyelocytic leukaemia | APL |
| 44 | Carboxymethyl cellulose | CMC |
| 45 | White blood cell | WBC |
| 46 | Erythrocytes and macrophages fused into hybrid membranes | EMHM |
| 47 | Nanoparticles | NPs |
| 48 | Nanofibers | NFs |