Supplementary Table 1: Summary of some reported phase-transition nanoparticles

| Platform | Composition | Drug | Core | Main method | Size（nm） | Stimulus mode | Condition | Transition temperature | Target strategy | Imaging platform | Monitoring time | Functional disease | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| PFP@PDM-PEG | PLGA-COOH, PEG3000-COOH, MMP-2 peptide | DSF | PFP | ultrasonic emulsification (100 W, on:off=1:1, 3 min) | 343 | LIFU | 2 W/cm2， 3 min | / | MMP-2 | USI | 24 h | breast cancer (4T1) | [1] |
| Lip-ICG-PFP-cRGD | DPPC, DSPG, DSPE-PEG-cRGD, cholesterol | ICG | PFP | ultrasonic emulsification (5 min) | 300 | LIFU | 2 W/cm2， 10 min | / | cRGD | USI | 24 h | ovarian cancer (TC-1) | [2] |
| fPFP/ICG/DOX@LIP | DPPC, DSPE-PEG2000, ICG | DOX | PFP | ultrasonic emulsification (1 min/2 min) | 362.23 | NIR | 1 W/cm2, 10 min | 43 °C | EPR | USI | 5 min | MDA-MB-231 | [3] |
| DPP-R | PLGA-COOH, RGD | DOX | PFH | microtip probe of the sonicator (25% intensity, 2 min/5 min, on:off=3:5) | 367 | LIFU | 8 W/cm2， 5 min | / | integrin αvβ3 | / | 6 h | gastric cancer (MGC-803) | [4] |
| DHPL | OMP, HAuNS, SA, DSPE-PEG2000 | DOX | PFP/PFH | ultrasonic emulsification | 196.6±17.6 | NIR | 2 W/cm2 | ＞60 °C | EPR | USI | 48 h | breast cancer- (4T1) | [5] |
| HA/CPPs-10-HCPT-NPs | DPPC, DC-Chol, DSPE-PEG-COOH, 10-HCPT, CPPs, HA | / | PFP | microtip probe of the sonicator（125W，6min，on:off=3:5） | 284.2±13.3 | LIFU | 3.2 W/cm2，2 min | / | CD44 | / | / | liver cancer (SMMC-7721) | [6] |
| FA-NDs | HSPC, DSPE-PEG-Folate, DPPG | / | PFP | microtip probe of the sonicator（130 W，5 min，on:off=5:5） | 321±67 | LIFU | 3.2 W/cm2, 2 min | 50 °C | folate | USI | 1h | ovarian cancer (SKOV3) | [7] |
| PFH@PLGA/Fe3O4 | PLGA, oleic-acid-coated Fe3O4 | / | PFH | microtip probe of the sonicator （50% intensity， 6 min） | 347 | NIR | 3 W/cm2 | 50 °C | intratumor injection | USI | ~5 min | ovarian cancer (SKOV3) | [8] |

Abbreviations. CPPs: cell-penetrating peptides; DPPC: 1,2-dipalmitoyl-sn-glycero-3-Phosphocholine; DPPG: 1,2-dipalmitoyl-sn-glycero-3-phospho- (1′-rac-glycerol); DSF: disulfram; DSPG: 1, 2-distearoyl-sn-glycero-3-phospho- (1′-rac-glycerol) ; DSPE-PEG2000: 1,2-distearoyl-sn-glycero-3-phosphoethanolamine-N-[methoxy(polyethyleneglycol)-2000]; DC-Chol: 3-(N-(N',N'-Dimethylaminoethane) carbamoyl) cholesterol; DOX: doxorubicin; DTX: docetaxel； EPR: enhanced permeability and retention; HA: hyaluronic acid; HAuNS:  hydrophobization of hollow gold nanoparticles; HSPC: 1-palmitoyl-2-stearoyl-snglycero-3-phosphocholine; ICG: indocyanine green; LIFU: low-intensity focused ultrasound; MMP-2: matrix metalloproteinase-2; NIR: near infrared; OMP: octadecyl 3-mercaptopionate; PLGA-COOH: poly (lactic-co-glycolic acid)-carboxylic acid; PFP: perfluoropropane; PFH: perfluorohexanes; SA: stearic acid; USI: ultrasonic imaging; UTMD: ultrasound-targeted microbubble destruction;  10-HCPT: 10-hydroxy camptothecin

Reference

1.	Liu Y, Tang R, Cao Y, Wu N, Qin Q, Chen Y, et al. LIFU/MMP-2 dual-responsive release of repurposed drug disulfiram from nanodroplets for inhibiting vasculogenic mimicry and lung metastasis in triple-negative breast cancer. Journal of Nanobiotechnology. 2024; 22: 209.

2.	Li M, Zhu Y, Yang C, Yang M, Ran H, Zhu Y, et al. Acoustic triggered nanobomb for US imaging guided sonodynamic therapy and activating antitumor immunity. Drug Delivery. 2022; 29: 2177-89.

3.	Sheng D, Deng L, Li P, Wang Z, Zhang Q. Perfluorocarbon Nanodroplets with Deep Tumor Penetration and Controlled Drug Delivery for Ultrasound/Fluorescence Imaging Guided Breast Cancer Therapy. ACS Biomaterials Science & Engineering. 2021; 7: 605-16.

4.	Liu Z, Ran H, Wang Z, Zhou S, Wang Y. Targeted and pH-facilitated theranostic of orthotopic gastric cancer via phase-transformation doxorubicin-encapsulated nanoparticles enhanced by low-intensity focused ultrasound (LIFU) with reduced side effect. Int J Nanomedicine. 2019; 14: 7627-42.

5.	Li W, Hou W, Guo X, Luo L, Li Q, Zhu C, et al. Temperature-controlled, phase-transition ultrasound imaging-guided photothermal-chemotherapy triggered by NIR light. Theranostics. 2018; 8: 3059-73.

6.	Zhao H, Wu M, Zhu L, Tian Y, Wu M, Li Y, et al. Cell-penetrating Peptide-modified Targeted Drug-loaded Phase-transformation Lipid Nanoparticles Combined with Low-intensity Focused Ultrasound for Precision Theranostics against Hepatocellular Carcinoma. Theranostics. 2018; 8: 1892-910.

7.	Liu J, Shang T, Wang F, Cao Y, Hao L, Ren J, et al. Low-intensity focused ultrasound (LIFU)-induced acoustic droplet vaporization in phase-transition perfluoropentane nanodroplets modified by folate for ultrasound molecular imaging. Int J Nanomedicine. 2017; 12: 911-23.

8.	Zhao Y, Song W, Wang D, Ran H, Wang R, Yao Y, et al. Phase-Shifted PFH@PLGA/Fe3O4 Nanocapsules for MRI/US Imaging and Photothermal Therapy with near-Infrared Irradiation. ACS Appl Mater Interfaces. 2015; 7: 14231-42.