Supplementary Material

Comprehensive wound healing using ETN@Fe7S8 complex by positively regulating multiple programmed phases

Mengxia Chen1,2, †, Ting Liu1,3, †, Xiaonan Wang4,5, †, Lizeng Gao4,6, Yunqing Cheng2*, Jing Jiang4*, Jinhua Zhang1*

1College of Life Science and Bioengineering, Beijing Jiaotong University, Beijing 100044, China

2School of Life Sciences, Jilin Normal University, Jilin 136000, China

3School of Life Science and Technology, Jinan University, Guangdong 510632, China

4CAS Engineering Laboratory for Nanozyme, Key Laboratory of Biomacromolecules, Institute of Biophysics, Chinese Academy of Sciences, Beijing 100101, China

5School of Life Sciences, University of Chinese Academy of Sciences, Beijing 101408, China

6Nanozyme Laboratory in Zhongyuan, School of Basic Medical Sciences, Zhengzhou University, Zhengzhou 450001, China

†These authors contributed equally to this work.

E-mail addresses: zhangjh@bjtu.edu.cn (JH. Zhang); jiangjing@ibp.ac.cn (J.Jing); chengyunqing1977@163.com (YQ. Cheng)

Supplementary Figure 1. The SEM and HAADF image of ETN.

Supplementary Figure 2. The SEM and HAADF image of Fe1-xS.

Supplementary Figure 3. (A) EDS mapping images of ETN. (B) EDS analysis of ETN elements.

Supplementary Figure 4. (A) EDS mapping images of Fe1-xS. (B) EDS analysis of Fe1-xS elements.

Supplementary Figure 5. (A) Photographs of bacterial colonies of MRSA with different concentrations (0, 125, 250, 500 µg/mL). (B) Bacterial viability of MRSA based on (A). ****P < 0.0001.

Supplementary Figure 6. Body weight of mice with different treatments. ns: no significant.

Supplementary Figure 7. (A) IF staining of CK10 for the wounds on days 3 and 7, and (B) quantitative analysis. (C) IF staining of CK14 for the wounds on days 3 and 7, and (D) quantitative analysis. **P<0.01, ****P < 0.001.

Supplementary Figure 8. (A) IF staining of Ki67 for the wounds on days 3 and 7, and (B) quantitative analysis. **P<0.01, ***P < 0.001.

Supplementary Figure 9. (A) Images of HaCaT migration with different treatments for 0, 12, 24, and 48 hours, and (B) quantitative analysis. ns: no significant，*P<0.05，***P<0.001

Supplementary Figure 10. (A) Optimal concentration of ETN@Fe7S8 to Raw264.7. (B) Optimal concentration of Na2S4 to Raw264.7. (C) Optimal concentration of FeCl2 to Raw264.7. *P < 0.05, ***P < 0.001, ****P < 0.001.

Supplementary Figure 11 (A) Images of HUVECs migration with different treatments in the Trans-well migration assay, and (B) quantitative analysis. **P < 0.01

Supplementary Figure 12. (A) Optimal concentration of ETN@Fe7S8 to HUVEC. (B) Optimal concentration of Na2S4 to HUVEC. (C) Optimal concentration of FeCl2 to HUVEC. *P < 0.05, **P<0.01, ***P < 0.001, ****P < 0.0001.

Supplementary Tables

Table S1. Details of primary materials and antibodies used in the study.

| REAGENT Or RESOURCE | SOURCE | IDENTIFIER |
| --- | --- | --- |
| Materials |  |  |
| DMEM | BI | 06-1055-57-1ACS-1 |
| Pen-Strep Solution | BI | 03-031-1B |
| FBS | Gibco | A31608-02 |
| Ferric chloride (FeCl3) | Sigma-Aldrich | 7705-08-0 |
| Ferrous chloride (FeCl2) | Sigma-Aldrich | 7758-94-3 |
| Cysteine | Sigma-Aldrich | 3374-22-9 |
| Sodium acetate trihydrate | Sigma-Aldrich | 6131-90-4 |
| Ethylene glycol | Sigma-Aldrich | 107-21-1 |
| NaCl | Sigma-Aldrich | 7647-14-5 |
| SulfoBiotics-SSP4 | DOJINDO | SB10 |
| Cell counting kit-8 | Aladdin Chemistry | C266180 |
| Iron content kit | Solarbio | BC5315 |
| ATP kit | Solarbio | BC0300 |
| Malondialdehyde kit | Nanjing Jiancheng | A003-1-2 |
| GSH and glutathione disulfide (GSSG) assay kit | Beyotime | S0053 |
| NAD/NADH kit | Beyotime | S0175 |
| Propidium iodide (PI) | Beyotime | C1075M |
| Mouse anticoagulant whole-blood | Bersee | B1057 |
| Agar | Sangon Biotech | A505255 |
| FastKing RT Kit (With gDNase) | TIANGEN | KR116 |
| Fixation & Permeabilization Buffer | Invitrogen | 88-8824-00 |
| IFN-γ ELISA kit | Cloud-Clone | SEA049Mu |
| TNF-α ELISA kit | Cloud-Clone | SEA133Mu |
| SYBR Green qPCR Master Mix | MCE | HY-K0501-5 |
| SYTO 9 | Thermo Fisher Scientific | S34854 |
| Antibodies |  |  |
| anti-Mouse CD11b | BD Biosciences | 550282 |
| anti-Mouse F4/80 | Bio Legend | 123101 |
| anti-Mouse Gr1 | BD Biosciences | 550291 |
| Mouse monoclonal anti-Ki67 | BD Biosciences | 550609 |
| anti-Mouse CK10 | Affinity | AF0197 |
| anti-Mouse CK14 | Affinity | AF5370 |
| anti-Mouse CD31 | Affinity | AF6191 |
| Phospho-PI3K Antibody | Affinity | AF3242 |
| PI3K Antibody | Affinity | AF6242 |
| anti-p-p65 | ProteinTech | 82335-1 |
| anti-p65 | ProteinTech | 10745-1 |
| VEGFA | Affinity | AF5131 |
| Mouse monoclonal anti-β-actin | Santa Cruz | sc-47778 |
| Cell lines |  |  |
| Raw264.7 | ATCC | TIB-71 |
| HUVEC | ATCC | PCS-100-013 |
| Bacteria |  |  |
| MRSA | ATCC | F-182 |
| Experimental models: organisms/strains |  |  |
| Balb/c | Hfkbio |  |

Table S2. The primer sequences of pro-inflammatory and anti-inflammatory factors.

| Gene | Primer sequence (5’-3’) |
| --- | --- |
| IL-6 Forward | TTCTTGGGACTGATGCTGGT |
| IL-6 Reverse | CTGTGAAGTCTCCTCTCCGG |
| TNF-α Forward | TGAGGTCAATCTGCCCAAGT |
| TNF-α Reverse | GGGGTCAGAGTAAAGGGGTC |
| IL-12 Forward | GTCCTCAGAAGCTAACCATCTCC |
| IL-12 Reverse | CCAGAGCCTATGACTCCATGTC |
| IL-10 Forward | CAGGGATCTTAGCTAACGGAAA |
| IL-10 Reverse | GCTCAGTGAATAAATAGAATGGGAAC |
| Arg-1 Forward | CAATCCCCAGCTTGTCTACTTCA |
| Arg-1 Reverse | GCATATCTGCCAAAGACATCGT |
| YM-1 Forward | GGCAAAGGTCATGGAGATGT |
| YM-1 Reverse | CTGCAGTCTCCATCACGAAA |
| β-actin Forward | GGCYGYAYYCCCCYCCAYCG |
| β-actin Reverse | CCAGTTGGTAACAATGCCATGT |

Table S3. Raman data of D band, G band and ID/IG of ETN and ETN@Fe7S8.

| Samples | D band (cm-1) | G band (cm-1) | ID/IG |
| --- | --- | --- | --- |
| ETN | 1722.66 | 1824.91 | 0.94 |
| ETN@Fe7S8 | 1204.05 | 1186.87 | 1.01 |

Table S4. BET-specific surface area, pore volume and pore size of ETN@Fe7S8.

| Samples | BET specific surface area (m2/g) | Pore volume (cm3/g) | Pore size (nm) |
| --- | --- | --- | --- |
| ETN | 20.72 | 0.05 | 10.28 |
| Fe1-xS | 16.25 | 0.05 | 16.17 |
| ETN@Fe7S8 | 10.17 | 0.03 | 11.63 |

Table S5. Comparison of ETN@Fe7S8 with other materials.

|  | Nanozybiotics/ others | Antibacterial properties | Microorganism | Antibacterial applications | Other Functions | Refs. |
| --- | --- | --- | --- | --- | --- | --- |
| Single-atom nanozybiotics | ETN | PODa | MRSAb | Wound healing | Hemostasis | [1] |
|  | CuL/PHI | POD, OXDc | E. colid, MRSA | Wound healing | _ | [2] |
|  | Mn/Fe SACs | POD, GOxe, CATf | S. aureusg, E. coli | Wound healing | _ | [3] |
| Carbon-based nanozybiotics | ETN@Fe7S8 | Fe2+, polysulfide release | MRSA | Wound healing | Hemostasis， angiogenesis |  |
|  | Cu SASs/NPC | POD, GPx, PTT | MRSA | Wound healing | _ | [4] |
|  | CeO2 NPs | OXD | S. aureus, E. coli |  | _ | [5] |
|  | H-CDs | POD | S. aureus, E. coli, P. aeruginosah, MRSA | Infection,、wound healing | _ | [6] |
|  | CS@Fe-N CDs | POD | S. aureus, E. coli | S. aureus, E. coli | _ | [7] |
|  | Fe-γ-CD | POD | ESBL- E. colii , MRSA | Antibacterial agent in foodstuﬀs | _ | [8] |
| Metal-based nanozybiotics | Cu ND/CG | POD | MRSA, E. coli | Wound healing | Angiogenesis | [9] |
|  | PtCo@G@H2A | OXD | H. pylorij | Gastric diseases | _ | [10] |
|  | Zn-Nx-C | Lactonase | P. aeruginosak | Antifouling nanocoating | _ | [11] |
|  | V-Fe2O3 | POD | MRSA | Wound healing | _ | [12] |
|  | Fe-SAC | POD | MRSA | Wound healing | _ | [13] |
| MOF-based nanozybiotics | FeCD | FeCD | E. coli, MRSA | Treatment of abscess | _ | [14] |
|  | Ni-MOF | POD, SOD | MRSA, E. coli | Wound healing | _ | [15] |
|  | Fe3O4@MOF@Au NPs | POD | S. aureus, E. coli | Wound healing | _ | [16] |
|  | Cu-CNNDs | POD | S. aureus, E. coli | Surface antibacterial coatings | _ | [17] |
|  | Bi-PCN-222 MOF | POD, OXD | S. aureus | Wound healing | _ | [18] |
| Others | Ferrous· iron | Ferroptosis | MRSA | Mouse keratitis model | _ | [19] |
|  | Polysulfide | Synergistic ferrousiron | MRSA | Infection model | _ | [20] |

Reference

1.	Wang X, Liu T, Chen M, Liang Q, Jiang J, Chen L, Fan K, Zhang J, Gao L: An Erythrocyte-Templated Iron Single-Atom Nanozyme for Wound Healing. Adv Sci (Weinh) 2024, 11:e2307844.

2.	Ou H, Qian Y, Yuan L, Li H, Zhang L, Chen S, Zhou M, Yang G, Wang D, Wang Y: Spatial Position Regulation of Cu Single Atom Site Realizes Efficient Nanozyme Photocatalytic Bactericidal Activity. Adv Mater 2023, 35:e2305077.

3.	Zhang M, Xu W, Gao Y, Zhou N, Wang W: Manganese-Iron Dual Single-Atom Catalyst with Enhanced Nanozyme Activity for Wound and Pustule Disinfection. ACS Appl Mater Interfaces 2023, 15:42227-42240.

4.	Wang X, Shi Q, Zha Z, Zhu D, Zheng L, Shi L, Wei X, Lian L, Wu K, Cheng L: Copper single-atom catalysts with photothermal performance and enhanced nanozyme activity for bacteria-infected wound therapy. Bioact Mater 2021, 6:4389-4401.

5.	Mehta D, Sharma P, Singh S: ATP-triggered, selective superoxide radical generating oxidase-mimetic cerium oxide nanozyme exhibiting efficient antibacterial activity at physiological pH. Colloids Surf B Biointerfaces 2023, 231:113531.

6.	Cheng K, Wang H, Sun S, Wu M, Shen H, Chen K, Zhang Z, Li S, Lin H: Specific Chemiluminescence Imaging and Enhanced Photodynamic Therapy of Bacterial Infections by Hemin-Modified Carbon Dots. Small 2023, 19:e2207868.

7.	Li L, Wang D, Ren L, Wang T, Tan X, Cui F, Li T, Li J: Chitosan-chelated carbon dots-based nanozyme of extreme stability with super peroxidase activity and antibacterial ability for wound healing. Int J Biol Macromol 2024, 258:129098.

8.	Liu X, Zhao Y, Xu Y, Liu C: Synthesis of γ-Cyclodextrin-Reduced Fe(III) Nanoparticles with Peroxidase-like Catalytic Activity for Bacteriostasis of Food. Nano Lett 2023, 23:9995-10003.

9.	Cui Y, Zhang W, Shan J, He J, Niu Q, Zhu C, Wang W, Chen XL, Wang X: Copper Nanodots-Based Hybrid Hydrogels with Multiple Enzyme Activities for Acute and Infected Wound Repair. Adv Healthc Mater 2024, 13:e2302566.

10.	Deng H, Zhang Y, Cai X, Yin Z, Yang Y, Dong Q, Qiu Y, Chen Z: Dual-Targeted Graphitic Cascade Nanozymes for Recognition and Treatment of Helicobacter pylori. Small 2024, 20:e2306155.

11.	Gao M, Xu B, Huang Y, Cao J, Yang L, Liu X, Djumaev A, Wu D, Shoxiddinova M, Cai X, et al: Nano-enabled Quenching of Bacterial Communications for the Prevention of Biofilm Formation. Angew Chem Int Ed Engl 2023, 62:e202305485.

12.	Huang H, Geng W, Wu X, Zhang Y, Xie L, Ma T, Cheng C: Spiky Artificial Peroxidases with V-O-Fe Pair Sites for Combating Antibiotic-Resistant Pathogens. Angew Chem Int Ed Engl 2024, 63:e202310811.

13.	Liu Q, Liu X, He X, Wang D, Zheng C, Jin L, Shen J: Iron-Single-Atom Nanozyme with NIR Enhanced Catalytic Activities for Facilitating MRSA-Infected Wound Therapy. Adv Sci (Weinh) 2024, 11:e2308684.

14.	Xu G, Liu K, Jia B, Dong Z, Zhang C, Liu X, Qu Y, Li W, Zhao M, Zhou H, Li YQ: Electron Lock Manipulates the Catalytic Selectivity of Nanozyme. ACS Nano 2024, 18:3814-3825.

15.	Chen Z, Shan J, Niu Q, Chen H, Zhang W, Cao D, Wang X: pH-responsive double-enzyme active metal-organic framework for promoting the healing of infected wounds. J Colloid Interface Sci 2024, 657:250-262.

16.	Liu C, Zhao X, Wang Z, Zhao Y, Li R, Chen X, Chen H, Wan M, Wang X: Metal-organic framework-modulated Fe(3)O(4) composite au nanoparticles for antibacterial wound healing via synergistic peroxidase-like nanozymatic catalysis. J Nanobiotechnology 2023, 21:427.

17.	Dai X, Liu H, Cai B, Liu Y, Song K, Chen J, Ni SQ, Kong L, Zhan J: A Bioinspired Atomically Thin Nanodot Supported Single-Atom Nanozyme for Antibacterial Textile Coating. Small 2023, 19:e2303901.

18.	Wu L, Luo Y, Wang C, Wu S, Zheng Y, Li Z, Cui Z, Liang Y, Zhu S, Shen J, Liu X: Self-Driven Electron Transfer Biomimetic Enzymatic Catalysis of Bismuth-Doped PCN-222 MOF for Rapid Therapy of Bacteria-Infected Wounds. ACS Nano 2023.

19.	Wang Z, Li H, Zhou W, Lee J, Liu Z, An Z, Xu D, Mo H, Hu L, Zhou X: Ferrous sulfate-loaded hydrogel cures Staphylococcus aureus infection via facilitating a ferroptosis-like bacterial cell death in a mouse keratitis model. Biomaterials 2022, 290:121842.

20.	Shen X, Ma R, Huang Y, Chen L, Xu Z, Li D, Meng X, Fan K, Xi J, Yan X, et al: Nano-decocted ferrous polysulfide coordinates ferroptosis-like death in bacteria for anti-infection therapy. Nano Today 2020, 35:100981.