Supporting Information

Macrophage-Mimetic Liposomes Co-delivering Ceria and Ac2-26 Peptide for Penumbra Protection in Ischemic Stroke

Lingyun Bai 1†, Na Li 2†, Huiqin Li 3†, Yuxuan Dai 3, Yi Bai 1, Feiyu Ma 1, Dujuan Sha 4, Shengnan Xia 3, Yun Xu 3,5*, Xiang Cao 1,3,5*

1 Department of Neurology, Nanjing Drum Tower Hospital, Drum Tower Hospital Life and Health Research Institute, Nanjing Normal University, Nanjing, 210008, China

2 Department of Blood Transfusion Medicine, Jinling Hospital, Affiliated Hospital of Medical School, Nanjing University, Nanjing, 210002, China

3 Department of Neurology, Nanjing Drum Tower Hospital, Affiliated Hospital of Medical School, Nanjing University, Nanjing, 210008, China

4 Department of General Practice, Nanjing Drum Tower Hospital, Affiliated Hospital of Medical School, Nanjing University, Nanjing, 210008, China

5 Nanjing Neurology Clinical Medical Center, Nanjing, 210008, China

† Lingyun Bai, Na Li and Huiqin Li contributed equally to this work.

*Correspondence:

Yun Xu

xuyun20042001@aliyun.com

Xiang Cao

caoxiang@njglyy.com

Fig. S1 Characterization of CeO2. (A) Size distribution of CeO2 nanoparticles measured by DLS. (B) Zeta potential of CeO2 nanoparticles measured by DLS. (C) Elemental mapping of CeO2 nanoparticles. Scale bar = 50 nm. (D) EDX spectrum of CeO2 nanoparticles.

Fig. S2 (A) TEM image of CeO2-Ac2-26@MM-LPs. Scale bar = 50 nm. (B) Magnified TEM images of CeO2 nanoparticles encapsulated within CeO2-Ac2-26@MM-LPs. Scale bar = 10 nm. (C) EDX spectrum of CeO2-Ac2-26@MM-LPs.

Fig. S3 (A) Viability of HT22 cells co-cultured with MM-LPs at different concentrations, measured by CCK-8 assay (n = 3). (B) Viability of HBMECs co-cultured with MM-LPs at different concentrations, measured by CCK-8 assay (n = 3).

Fig. S4 Hemolysis assay of CeO2-Ac2-26@MM-LPs (n = 6). “ns” means no significance (P > 0.05), ***P<0.001 versus the pure water group.

Fig. S5 H&E staining of major organs (heart, liver, spleen, lungs, and kidneys) from different treatment groups. Scale bar = 50 μm.

Fig. S6 In vivo biocompatibility of CeO2-Ac2-26@MM-LPs measured by (A) hematology and (B) blood chemistry tests (n = 5).

Fig. S7 Representative fluorescence images of major organs including heart, liver, spleen, lung and kidney from tMCAO mice at different timepoints post i.v. injection of DiR-labeled LPs and MM-LPs.

Fig. S8 (A-B) The Nrf2 inhibitor ML385 abolished the ROS-scavenging capacity of CeO2-Ac2-26@MM-LPs in OGD/R-treated HT22 cells (n = 3). **P<0.01, ***P<0.001versus the control group; ##P<0.01 versus the OGD/R group; &P<0.05 versus the OGD/R + CeO2-Ac2-26@MM-LPs group.

Fig. S9 (A-B) ML385 (Nrf2 inhibitor) blocked CeO2-Ac2-26@MM-LPs-mediated reduction of apoptosis in OGD/R-injured HT22 cells (n = 3). *P<0.05, ***P<0.001 versus the control group; ###P<0.001 versus the OGD/R group; &&&P<0.001 versus the OGD/R + CeO2-Ac2-26@MM-LPs group.

Fig. S10 TEER measurements revealed that CeO2-Ac2-26@MM-LPs and the NF-κB inhibitor PDTC produced comparable effects in reducing endothelial permeability (n = 3). **P<0.01, ***P<0.001 versus the control group; ##P<0.01, ###P<0.001 versus the OGD/R group.