Supporting Information

Tungsten disulfide atomic crystals with RONS scavenging and liver targeting capabilities for acetaminophen-induced acute liver injury therapy

Ziwen Xiao a,#, Yu Liu a,#, Zhenchao Tao b,#, Yu Zhang a, Qian Chen a, Zhaohua Miao a, Zhengbao Zha a, Yan Ma c*, Hua Wang d*, Deyan Gong a*

a School of Food and Biological Engineering, Hefei University of Technology, Hefei 230009, China

b Department of Radiation Oncology, Anhui Provincial Cancer Hospital, Hefei 230031, China

c School of Biomedical Engineering, Anhui Medical University, Hefei, 230022 China

d Department of Oncology, The First Affiliated Hospital of Anhui Medical University, Hefei 230032, China

#These authors contributed equally

*Corresponding authors: may@ahmu.edu.cn (Yan Ma); wanghua@ahmu.edu.cn (Hua Wang); gongdy@hfut.edu.cn (Deyan Gong)

Figure S1. (a) TEM image of WS2 NSs. (b) AFM image and (c) the corresponding thickness profiles of WS2 NSs.

Figure S2. Hydrated particle size of WS2 NSs and WS2@TA NSs.

Figure S3. (a) The variation of hydration particle size of WS2 NSs in different media. (b)The variation of hydration particle size of WS2@TA NSs in different media.

Figure S4. UV−vis spectra of WS2@TA NSs, WS2 NSs, and TA.

Figure S5. Fourier transform infrared (FTIR) spectra of WS2@TA NSs, WS2 NSs, and TA.

Figure S6. Thermogravimetric (TG) analysis of WS2@TA NSs, WS2 NSs, and TA.

Figure S7. (a) Core XPS spectra of C element. (b) Core XPS spectra of O element.

Figure S8. The clearance kinetics curve of DPPH.

Figure S9. H2O2 scavenging efficiencies.

Figure S10. (a) Core XPS spectra of S element and (b) W element in WS2@TA after H2O2 treatment.

Figure S11. Cell viability of Raw 264.7 cells treated with WS2 NSs or WS2@TA NSs of different concentrations (n = 3).

Figure S12. (a-c) Downregulation of LPS-induced proinflammatory cytokine (TNF-α, IL-1β, and IL-6) levels.

Figure S13. Quantitative analysis of the fluorescence intensity of intracellular Cy5.5-labeled WS2@TA NSs (n = 3).

Figure S14. Endotoxin activity in 0.5mg/mL WS2@TA solution.

Figure S15. Hemolysis test of WS2@TA NSs.

Figure S16. Distribution of W element in organs of AILI mice after intravenous injection of WS2 NSs (n=3).

Figure S17. Blood biochemistry index tests. (a) Serum levels of ALT, (b) AST, (c) UREA, (d) UA and (e) TP.

Figure S18. Representative images of TUNEL fluorescence imaging of liver tissue sections.