Supporting Information

Single-atom Ca Nanozyme Induces Glioma Death Through Ca2+-Overload-Enhanced Catalytic Tumor Nanotherapy, Ferroptosis and Synergistic Remodeling of the Immune Microenvironment

Zhizhong Jina,1, Xinqiao Lib,1, Xiaoyu Houc,1, Jinpeng Hua, Yue Zhuoa, Jianghua Shia, Tao Xud***, Qi Zhaoe,f,1**, Zhitao Jinga,*

aDepartment of Neurosurgery, The First Hospital of China Medical University, Nanjing Street 155, Heping District, Shenyang 110001, P. R. China

bDepartment of Neurosurgery, Liaoning Cancer Hospital and Institute, Cancer Hospital of China Medical University, Shenyang 110042, P. R. China

cDepartment of Rheumatology and Immunology, The First Hospital of China Medical University, Shenyang 110001, P. R. China

dCenter for Bio-intelligent Manufacturing and Living Matter Bioprinting, Research Institute of Tsinghua University in Shenzhen, Tsinghua University, Shenzhen, 518057, People's

Republic of China

eCenter of Super-Diamond and Advanced Films (COSDAF), Department of Chemistry, City University of Hong Kong, 83 Tat Chee Avenue, Kowloon, Hong Kong SAR, P. R. China

fDepartment of Chemistry and the Institute for Sustainability and Energy, Northwestern University, 2145 Sheridan Road, Evanston, IL 60208-3113, USA

Supplementary Figure 1.

Supplementary Figure 1.

- The TEM image of ZIF-8 and the images of elemental mapping of C, N, and O.

- The TEM image of Ca/ZIF-8 and the images of elemental mapping of C, N, and Ca.

Supplementary Figure 2.

Supplementary Figure 2.

- SEM image of (a) ZIF-8 and (b) Ca/ZIF-8.

- Simulated XRD patterns of ZIF-8 and experimental XRD patterns of ZIF-8 and Ca-ZIF 8.

- Ca-CN electron energy loss spectroscopy (EELs）

Supplementary Figure 3.

Supplementary Figure 3.

- Comparison of the peroxidase-like activity between CaCN and HRP.

- Photothermal analysis of Ca/CN-SAzyme.

Supplementary Figure 4.

Supplementary Figure 4.

- The cytotoxicity between ZIF-8 after calcination and CaCN in LN229 cell line.

- Viability curves of LN229 and NHA cells treated with different concentrations of TF-CaCN.

- WB results show that in LN229 and GSC23 cell lines, H2O2 influences the catalytic efficiency of CaCN, thereby promoting cell apoptosis.

Supplementary Figure 5.

Supplementary Figure 5. Immune infiltration in CaCN-treated glioma cells versus controls was calculated using the cibersort algorithm.

Supplementary Figure 6.

Supplementary Figure 6.

- PCR results demonstrate the effects of CaCN and TF-CaCN on M1 markers (IL-6 and iNOS) in RAW and THP-1 cell lines.

- Dynamic light scattering (DLS) analysis for measuring the particle size of TF-CaCN.

- The cytotoxicity between CaCN and TF-CaCN in LN229 cell line.

- WB results compare the effects of CaCN and TF-CaCN on calcium ion channels in LN229 and GSC23 cell lines.

Supplementary Figure 7.

Supplementary Figure 7. Immunohistochemistry was used to detect the expression of peritumoral immune-related indicators (CD4, CD8) in mice after injection of TF-CaCN and CaCN.

Supplementary Figure 8.

Supplementary Figure 8. Histological examination of major organs (heart, liver, spleen, lung and kidney)from G261 tumor-bearing mice in various treatment groups.

| GEO | https://www.ncbi.nlm.nih.gov/geo/ |
| --- | --- |
| TCGA | https://portal.gdc.cancer.gov/ |
| CGGA | http://www.cgga.org.cn/ |
| GSEA | https://www.gsea-msigdb.org/gsea/msigdb/index.jsp |

Table S1. The database website.

| Primer | Forward (5’-3’) | Reverse (5’-3’) |
| --- | --- | --- |
| Caspase1 | AAATCTCACTGCTTCGGACA | GGCTGCTCAAATGAAAATCGAAC |
| GPX4 | CGCCTTTGCCGCCTACTGA | CTGGCTCCTGCTTCCCGAAC |
| Il6 | AACAAATTCGGTACATCCTCGAC | ATTTTCACCAGGCAAGTCTCC |
| iNOS | TCCCACCTGACCTTGTGCTT | CAGGGCGTACCACTTTAGCTC |
| PMCA4 | ATTAACACATTCCAGACGGGAG | CTATGGAACGCTTTGACCACT |
| TNF-α | TCGAACCCCGAGTGACAAGCC | GTTCTTATACTCGGGCCACAC |
| GAPDH | ACGACCACTTTGTCAAGCTC | CTGTTGCTGTAGCCAAATTCGTT |
| ACSL4 | ACTTAAGCTAAATGTGCTCACC | ATTCTCTTTGCCATAGCGTTT |

Table S2. PCR Primers sequences.

Refrence:

[1]	M. E. Ritchie, B. Phipson, D. Wu, Y. Hu, C. W. Law, W. Shi, G. K. Smyth, Nucleic Acids Res. 2015, 43, e47.

[2]	T. Wu, E. Hu, S. Xu, M. Chen, P. Guo, Z. Dai, T. Feng, L. Zhou, W. Tang, L. Zhan, X. Fu, S. Liu, X. Bo, G. Yu, Innov. Camb. Mass 2021, 2, 100141.

[3]	Y. Jiang, J. Zhou, J. Zhao, D. Hou, H. Zhang, L. Li, D. Zou, J. Hu, Y. Zhang, Z. Jing, EBioMedicine 2020, 52, 102651.

[4]	J. Zhao, Y. Jiang, H. Zhang, J. Zhou, L. Chen, H. Li, J. Xu, G. Zhang, Z. Jing, J. Exp. Clin. Cancer Res. CR 2021, 40, 134.