Fig. S1. Two DHA prodrug candidates: DHA-S-CA1 (A) and DHA-S-CA2 (B).

Fig. S2. The structures of DHA-PRO were determined by HR MS.

Fig. S3. Release curves of DHA from DHA-PRO in different concentrations of H2O2 (n =3).

Fig. S4. Stability and release curves of DHA-PRO@NMs. (A) The stability of DHA-PRO@NMs was visually assessed in four solutions—H₂O, NS, PBS, and DMEM—at pH 5.5 and pH 7, at day 1 and day 7. (B-E) SIZE and PDI of DHA-PRO@NMs in H₂O, NS, PBS, and DMEM over 7 days. (F) Release curves of DHA from DHA-PRO@NMs in different concentrations of H₂O₂. (G) Release curves of DHA from DHA-PRO and DHA-PRO@NMs in 10 mM H₂O₂ (n=3).

1: The sol-gel transition temperatures of different ratios of P188/P407 in Blank@TSH

| P407 P188 | 18 % | 20 % | 23 % | 25 % |
| --- | --- | --- | --- | --- |
| 0 % | 29℃ | 25℃ | 22℃ | 20℃ |
| 2 % | 31℃ | 27℃ | 23℃ | 21℃ |
| 3 % | 35℃ | 29℃ | 25℃ | 23℃ |
| 5 % | 37℃ | 31℃ | 27℃ | 25℃ |

2: The sol-gel transition temperatures of different ratios of P188/P407 in DHA-PRO@NMs@TSH

| P407 P188 | 18 % | 20 % | 23 % | 25 % |
| --- | --- | --- | --- | --- |
| 0 % | 28℃ | 24℃ | 21℃ | 19℃ |
| 2 % | 30℃ | 26℃ | 22℃ | 20℃ |
| 3 % | 34℃ | 28℃ | 24℃ | 22℃ |
| 5 % | 36℃ | 30℃ | 26℃ | 24℃ |

Table 1 and 2. The sol-gel transition temperatures of different ratios of P188/P407 in Blank@TSH (Table 1) and DHA-PRO@NMs@TSH (Table 2).

Fig. S5. Properties of DHA-PRO@NMs@TSH. (A) Viscosity (η) changes of DHA-PRO@NMs@TSH at day 1 and day 7. (B) Erosion and release cumulative rate of DHA-PRO@NMs@TSH.

Fig. S6. The levels of inflammatory cytokines IL-1β (A) and TNF-α (B) in ATDC5 cells with different treatments. Data are shown as mean ± SD (n = 3), and *p < 0.05, **p < 0.01, ***p < 0.001, ****p < 0.0001, ns means not significant.

Fig. S7. DHA-PRO@NMs@TSH attenuated OA progression in vivo. (A-F) Quantification analysis of corresponding bone parameters from micro-CT: Bone mineral content (BMC), Bone mineral density (BMD), Bone surface density (BS/TV), Percent bone volume (BV/TV), Trabecular number (Tb. N), and Trabecular separation (Tb. Sp). (G) The histological severity in each group was evaluated by Mankin scoring system. Data are shown as mean ± SD (n = 3), and *p < 0.05, **p < 0.01, ***p < 0.001, ****p < 0.0001, ns means not significant.

Fig. S8. The levels of inflammatory cytokines IL-1β (A) and TNF-α (B) in rat joints with different treatments. Data are shown as mean ± SD (n = 3), and *p < 0.05, **p < 0.01, ***p < 0.001, ****p <0.0001, ns means not significant.