Pathogen-microenvironment-responsive and antioxidant-buffered propiconazole nanofungicide for safe and effective fungal disease control

Xin Shi1, Qizhen Zhang1, Xunian Chang2, Tingting Wang4, Feifei Tian2, Xiaolin Li3, Anyu Gu3, Xili Liu1*, Pengfei Liu1*

1College of Plant Protection, China Agricultural University, Beijing 100193, China

2Shimadzu (China) Co. LTD, Beijing 100020, China

3Institute of Food Crops, Yunnan Academy of Agricultural Sciences, Kunming 650205, China

4Institute of Medicinal Plant Development, Chinese Academy of Medical Sciences and Peking Union Medical College, Beijing 100193, China

*Corresponding authors: Pengfei Liu (pengfeiliu@cau.edu.cn) and X. Liu (seedling@cau.edu.cn)

Supplemental document S1. Detailed Materials and Reagents

Technical-grade propiconazole was provided by Andor (Beijing) Agricultural Technology Co., Ltd., Beijing, China. Sodium tripolyphosphate (TPP) was purchased from Sinopharm Chemical Reagent Co., Ltd., Shanghai, China. Quercetin hydrate, epichlorohydrin (ECH, 97%), and fluorescein isothiocyanate (FITC, 95%) were obtained from Tianjin Heowns Biochemical Technology Co., Ltd., Tianjin, China. Chitosan (CS, Mw = 200 kDa, degree of deacetylation 90%) and pectin (from citrus peel, Mw = 20-30 kDa, galacturonic acid ≥ 74%, degree of methylation ≥ 45%) were purchased from Shanghai Macklin Biochemical Technology Co., Ltd., Shanghai, China. Polysorbate 80 (Tween 80), sodium hydroxide, ethanol, dichloromethane, acetate, and other analytical grade reagents were purchased from Tianjin Zhiyuan Chemical Reagent Co., Ltd., Tianjin, China. Dialysis bags (MD77 mm, Mw: 12,000 Da; MD44 mm, Mw: 4000 Da) were purchased from Beijing Biotopped Science & Technology Co., Ltd., Beijing, China. Ultrapure Milli-Q water (resistivity > 18 MΩ·cm) used for all experiments was obtained from an experimental water system. The strain Rhizoctonia solani X19 was maintained in the Laboratory of Fungicide Pharmacology and Pathogen Resistance at China Agricultural University, Beijing, China. The rice seeds (variety 9801#) were provided by Yunnan Academy of Agricultural Science, Kunming, Yunna, China.

Supplemental document S2. Sample characterization

The hydrated particle size, polydispersity index (PDI), and zeta potential of the nanoparticles were measured at 25 °C using a BeNano 180 Zeta analyzer (Bettersize Instruments Ltd., Dandong, China). Particle size and PDI were determined by dynamic light scattering (DLS) at a scattering angle of 173°, while zeta potential was measured by electrophoretic light scattering (ELS). All measurements were conducted in triplicate.

Fourier-transform infrared (FTIR) spectra were obtained using a Nicolet iS20 spectrometer (Thermo Fisher Scientific, Waltham, USA). Dried samples were finely ground, mixed with potassium bromide (KBr), and pressed into pellets. Spectra were recorded in the range of 400–4000 cm⁻¹.

Scanning electron microscopy (SEM) images of nanoparticles and rice leaves were captured using a GeminiSEM 300 instrument (ZEISS, Oberkochen, Germany).

Transmission electron microscopy (TEM) was performed using a JEM-F200 microscope (JEOL Ltd., Tokyo, Japan) to examine nanoparticle morphology.

Thermogravimetric analysis (TGA) was carried out using a Hitachi 7300 analyzer (Hitachi, Tokyo, Japan). Samples were heated from 30 °C to 550 °C at a rate of 10 °C/min, under nitrogen, and weight loss was continuously recorded.

Proton nuclear magnetic resonance (¹H NMR) spectra of pectin, quercetin, and the quercetin–pectin conjugate (PQ) were recorded on a Bruker Ascend 500 MHz spectrometer (Bruker, Karlsruhe, Germany) to confirm structural features.

UV–visible (UV–vis) absorption spectra were measured using a Genesys180 spectrophotometer (Thermo Fisher Scientific, Waltham, USA).

Supplemental document S3. Determination of fungicide loading

Chromatographic separation was achieved using a ZORBAX SB-C18 column (4.6 mm × 150 mm, 5 μm). The mobile phase consisted of acetonitrile and water (75:25, v/v), delivered at a flow rate of 1.0 mL/min. The detection wavelength was set at 220 nm, with the column maintained at 25 °C. The injection volume was 5 μL. Each sample was analyzed in triplicate.

Supplemental document S4. Evaluation of antifungal activity

The antifungal activity of Pro@CS/PQ and a propiconazole commercial emulsifiable concentrate (Pro-EC) was evaluated against Rhizoctonia solani using the mycelial growth rate method. Pro was incorporated into potato dextrose agar (PDA) at concentrations ranging from 0.05 to 4 mg/L. Fungal plugs (5 mm in diameter) were excised from the actively growing edge of each colony and transferred to Pro-amended PDA plates. Plates containing sterile water served as blank controls. Mycelial diameters were measured in two perpendicular directions after incubation, and inhibition rates were used to calculate the EC₅₀ values. All experiments were performed in triplicate. The composition of the Pro-EC formulation was as follows: 20% Pro, 70% xylene, 8% solvent 500#, and 2% emulsifier 600#.

The protective and curative efficacy of Pro@CS/PQ was further assessed using a detached leaf assay. Rice leaves at the tillering stage were harvested from greenhouse-grown plants and wrapped with moist cotton at both ends. Pro@CS/PQ and Pro-EC suspensions were prepared at concentrations of 50 and 100 mg/L, and 10 mL of each suspension was evenly sprayed onto the leaves. For the protective assay, fungal plugs of R. solani were inoculated 24 h after spraying. For the curative assay, inoculation occurred 24 h prior to spraying. Lesion areas were imaged at 5 days post-inoculation and quantified using ImageJ software (version 1.54d, NIH, USA). Water-treated leaves were used as controls. Each treatment group included 9 leaves and was replicated three times. The control efficacy (CE, %) was calculated using the following equation (3).

CE %=(C-L)C×100% 	(3)

Here, C (mm) represents the lesion area of the rice leaves treated with water (blank control), while L (mm) denotes the lesion area of the rice leaves treated with Pro.

Supplemental document S5. Wettability and adhesion properties of Pro@CS/PQ

Determination of liquid holding capacity

The retention capacity of Pro@CS/PQ on rice leaves was evaluated following a previously reported method. Both Pro@CS/PQ and Pro-EC were diluted to a concentration of 100 mg/L using deionized water. Fresh rice leaves were cut into 1 cm × 3 cm segments and immersed in the test suspensions for 30 s. After immersion, leaves were vertically lifted with forceps and held for 20 s to allow excess liquid to drip off. The weight of each leaf was measured before and after immersion using an analytical balance (Sartorius, Germany). Distilled water served as the control. Each treatment included 20 replicates and was performed in triplicate. The LHC (mg/cm²) was calculated using the following equation (4).

LHC mgcm2=(m1-m0)2S 	(4)

Where m0 (mg) is the weight of the leaf, m1 (mg) is the weight of the leaf after immersion in the drug solution, and S (cm2) is the area of the leaf.

Determination of surface tension and contact angle

Surface tension of the Pro@CS/PQ and Pro-EC suspensions (100 mg/L) was measured using a surface tensiometer (DCAT21, Germany). Contact angle measurements were performed using a video optical contact angle system (OCA 20, Germany). A 4 μL droplet of each suspension was applied to the surface of rice leaves using a microsyringe, and the contact angle was recorded over a 0–90 s interval. All measurements were conducted in triplicate.

Determination of rainwash resistance

Rainwash resistance was evaluated using fluorescein isothiocyanate (FITC) as a fluorescent tracer. FITC-labeled Pro@CS/PQ and Pro-EC formulations were prepared by adding FITC ethanol solution (0.5 mg/mL, 2 mL) to the oil phase during nanoparticle preparation (Section 2.3). Fresh rice leaves (1 cm × 5 cm) were positioned on a 40° inclined surface and evenly sprayed with 5 mL of test suspension.

After air-drying, each leaf was halved along the main vein. One half was directly imaged under a fluorescence inverted microscope (Nikon Ti-E, Japan) to observe pre-rinse distribution, while the other half was rinsed with 10 mL deionized water before imaging. Fluorescence intensity and coverage area were analyzed using ImageJ (v1.54d, NIH, USA). Pre-rinse fluorescence values were normalized to 100%, and post-rinse values were expressed as percentages. Each treatment was performed in five replicates.

Supplemental document S6. Safety assessment of Pro@CS/PQ

Impact of Pro@CS/PQ on rice growth

The safety of Pro@CS/PQ on rice seedlings was assessed under greenhouse conditions. Four concentrations were selected based on the recommended dosage of Pro (active ingredient: 22.5 mg/m²) and different spraying approaches: 1×S (300 mg/L, representing high-volume spraying), 1×F, 2×F, and 4×F (where F = 7500 mg/L, representing low-volume spraying). Experiments were conducted in the greenhouse facility of China Agricultural University. Rice seedlings were grown in nutrient-rich soil within plastic pots until the tillering stage (30 days). On the day of treatment, the greenhouse temperature and relative humidity averaged 27 °C and 70%, respectively. Each formulation was uniformly sprayed onto the rice leaves. Water-treated plants served as the control group. After 21 days, plant height, fresh and dry weight, and chlorophyll content were measured. Each treatment included three replicates, with 30 plants per replicate.

Determination of antioxidant enzyme activity

Oxidative stress and the activity of antioxidant enzymes were assessed in rice leaves treated with Pro@CS/PQ. Superoxide dismutase (SOD), catalase (CAT), peroxidase (POD), and malondialdehyde (MDA) levels were determined. Briefly, 0.1 g of fresh rice leaves was flash-frozen in liquid nitrogen and ground into fine powder. The powder was resuspended in 1 mL of phosphate-buffered saline (PBS, 50 mM, pH 7.8), centrifuged at 8000 g for 10 min at 4 °C, and the supernatant was collected.

Enzyme activities were measured using commercial assay kits (Solarbio, Beijing, China), following manufacturer protocols. MDA content was determined via the thiobarbituric acid (TBA) method. All assays were performed in triplicate.

Metabolomic Analysis of Rice Seedlings

Fresh rice leaves were ground into a fine powder using liquid nitrogen to preserve their metabolic integrity. A 100 mg sample of the powder was transferred to a 2 mL centrifuge tube and mixed with 1.8 mL of a methanol-chloroform-water solution (3:2:1, v/v/v) containing ribitol (10 µg/mL) as an internal standard. The mixture was sonicated at 25°C for 20 minutes to ensure thorough extraction and then centrifuged at 12,000 rpm for 15 minutes. A 0.1 mL portion of the supernatant was dried at 45°C to remove the solvent. The dried residue was dissolved in 100 µL of a methoxyamine hydrochloride solution (20 mg/mL) and sonicated for 20 minutes at 25°C. After vortexing briefly and centrifuging, the solution was incubated at 30°C for 2 hours. Subsequently, 100 µL of Bis(trimethylsilyl)trifluoroacetamide was added, and the mixture was sonicated again for 20 minutes under the same conditions. The sample was then vortexed, briefly centrifuged, and incubated for 6 hours at 30°C. After a final centrifugation at 12,000 rpm for 15 minutes, 120 µL of the supernatant was transferred to a sample vial for analysis.

For untargeted metabolomics, fresh rice leaves were ground under liquid nitrogen to preserve metabolic integrity. A 100 mg aliquot of the powder was extracted using 1.8 mL of a methanol–chloroform–water mixture (3:2:1, v/v/v) containing ribitol (10 μg/mL) as an internal standard. Samples were sonicated at 25 °C for 20 min and centrifuged at 12,000 rpm for 15 min. A 0.1 mL aliquot of the supernatant was dried at 45 °C, derivatized with 100 μL methoxyamine hydrochloride (20 mg/mL), and sonicated again at 25 °C for 20 min. After brief vortexing and centrifugation, the solution was incubated at 30 °C for 2 h.

Next, 100 μL of BSTFA [N,O-Bis(trimethylsilyl)trifluoroacetamide] was added, followed by sonication for 20 min and a final incubation at 30 °C for 6 h. The derivatized sample was centrifuged at 12,000 rpm for 15 min, and 120 μL of supernatant was transferred to GC-MS vials for analysis.

Metabolomic profiling was performed using a GCMS-TQ8050 NX system (Shimadzu, Japan). Data processing was conducted with GCMS solution 4.53SP1 software. Peak alignment and metabolite identification were performed using an integrated library and cross-referenced with the Human Metabolome Database (HMDB) and the KEGG database for pathway mapping.

Principal component analysis (PCA) and statistical analysis were performed on the MetaboAnalyst 6.0 platform (https://www.metaboanalyst.ca/), following data normalization and log transformation. Differentially accumulated metabolites (DAMs) were defined as those with variable importance in projection (VIP) ≥ 1 and |log₂(fold change)| ≥ 1. Six biological replicates were used per treatment to ensure statistical reliability.

Fig. S1. In vitro antifungal activity of Pro EC and Pro@CS/PQ against three plant pathogenic fungi. (a) Magnaporthe oryzae, (b) Botrytis cinerea, and (c) Fusarium fujikuroi.

Table S1. Method conditions for rice metabolites detection

| Instrument Model | GCMS-TQ8050 NX (shimadzu) |
| --- | --- |
| Carrier Gas | 99.999% Helium |
| Injection Volume | 1 µL |
| Injection Mode | Split Injection |
| Column | DB-5 (30 m × 0.25 mm × 1.00 μm) |
| Column Temperature Program | Initial Temp: 100°C, hold for 4 min; ramp to 320°C at 4°C/min, hold for 8 min |
| Solvent Delay Time | 3.5 min |
| Interface Temperature | 280°C |
| Ion Source | Electron Ionization (EI) |
| Ion Source Temperature | 250°C |
| Electron Energy | 70 eV |
| Scan Range | m/z 45–600 |
| Scan Speed | 0.3 s/scan |
| Detection Mode | FASST Mode (SCAN+MRM) |
| Data Acquisition Software | GCMS solution 4.53SP1 (Shimadzu) |

Table S2. Fitting results for the various release kinetics models

| Model | pH | Kinetic equation | R2 |
| --- | --- | --- | --- |
| Zero-order | 4.5 | y = 0.6993 x + 22.4556 | 0.62 |
|  | 7.0 | y = 0.59867 x + 22.2892 | 0.57 |
|  | 9.2 | y = 0.5904 x + 14.4611 | 0.67 |
|  | 7.0 (with pectinase ) | y = 1.1544 x + 18.6552 | 0.83 |
| First-order | 4.5 | y = 55.9752 (1 - e-0.186 x) | 0.98 |
|  | 7.0 | y = 50.8099 (1 - e-0.2174 x) | 0.98 |
|  | 9.2 | y = 43.9139 (1 - e-0.1330 x) | 0.97 |
|  | 7.0 (with pectinase ) | y = 81.6719 (1 - e-0.0711 x) | 0.98 |
| Higuchi | 4.5 | y = 7.1042 x1/2 + 10.9064 | 0.83 |
|  | 7.0 | y = 6.1938 x1/2 + 12.0151 | 0.79 |
|  | 9.2 | y = 5.8682 x1/2 + 5.1585 | 0.86 |
|  | 7.0 (with pectinase ) | y = 10.9377 x1/2 + 2.2298 | 0.97 |
| Ritger-Peppa | 4.5 | y = 18.9503 x0.2930 | 0.91 |
|  | 7.0 | y = 19.2401 x0.2653 | 0.90 |
|  | 9.2 | y = 11.6605 x0.3491 | 0.90 |
|  | 7.0 (with pectinase ) | y = 14.2773 x0.4363 | 0.98 |
| Weibull | 4.5 | y = 100 (1-e-(0.016 x) ^0.40) | 0.93 |
|  | 7.0 | y = 100 (1-e-(0.01 x) ^0.36) | 0.91 |
|  | 9.2 | y = 100 (1-e-(0.01 x) ^0.43) | 0.91 |
|  | 7.0 (with pectinase ) | y = 100 (1-e-(0.046 x) ^0.70) | 0.99 |

Table S3. Metabolite information and Log2FC value of each metabolite in rice leaves

| Compound Name | RT (min) | Compound CID | Super class | log2(fold change) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Pro@CS/PQ |  |  |  | Pro EC |  |  |  |
|  |  |  |  | 1×S | 1×F | 2×F | 4×F | 1×S | 1×F | 2×F | 4×F |
| Pyruvic acid | 8.92 | 1060 | Organic acids and derivatives | -0.7 | -1.0 | -0.9 | -1.2 | -1.1 | -1.6 | -1.1 | -0.7 |
| Glycolic acid | 9.79 | 757 | Organic acids and derivatives | 0.7 | 0.6 | 1.1 | 1.5 | 1.5 | 1.1 | 2.1 | 1.9 |
| Hydroxylamine | 11.60 | 787 | Homogeneous non-metal compounds | 1.4 | 1.5 | 1.5 | 1.9 | 1.8 | 2.1 | 2.5 | 1.9 |
| Acetoacetic acid | 11.84 | 96 | Organic acids and derivatives | 1.0 | 1.0 | 1.3 | 2.0 | 2.0 | 1.8 | 2.3 | 1.7 |
| Hydroxypropionic acid | 12.23 | 68152 | Organic acids and derivatives | 0.5 | 0.4 | 0.9 | 1.1 | 1.0 | 0.7 | 1.6 | 1.6 |
| 3-Hydroxybutyric acid | 12.82 | 441 | Organic acids and derivatives | 0.3 | 0.5 | 1.2 | 1.3 | 1.1 | 1.0 | 1.6 | 1.9 |
| (S)-3-Hydroxyisobutyric acid | 12.89 | 440873 | Organic acids and derivatives | 0.6 | 0.5 | 0.9 | 1.0 | 1.1 | 1.0 | 1.6 | 1.7 |
| L-Valine | 14.94 | 6287 | Organic acids and derivatives | 1.0 | 1.2 | 2.4 | 2.0 | 1.8 | 1.7 | 2.4 | 3.0 |
| Urea | 15.54 | 1176 | Organic acids and derivatives | 1.9 | 1.7 | 3.0 | 3.5 | 3.8 | 3.6 | 4.1 | 3.6 |
| Leucine | 16.94 | 6106 | Organic acids and derivatives | 1.4 | 1.7 | 3.5 | 3.3 | 3.1 | 2.6 | 3.2 | 3.7 |
| Nicotinic acid | 17.71 | 938 | Organoheterocyclic compounds | 0.5 | 0.2 | 0.5 | 0.9 | 0.6 | 0.2 | 1.0 | 1.1 |
| Isoleucine | 17.74 | 6306 | Organic acids and derivatives | 1.0 | 1.1 | 3.0 | 3.1 | 2.4 | 2.2 | 3.0 | 3.7 |
| Proline | 17.95 | 145742 | Organic acids and derivatives | 1.1 | 2.2 | 4.0 | 4.9 | 4.4 | 3.8 | 5.0 | 5.5 |
| Methylsuccinic acid | 18.66 | 6950476 | Lipids and lipid-like molecules | 0.6 | 0.8 | 0.8 | 1.0 | 1.0 | 1.2 | 1.3 | 1.5 |
| Glyceric acid | 19.06 | 439194 | Organic oxygen compounds | -0.8 | -1.0 | -1.2 | -1.2 | -0.6 | -1.2 | -0.1 | -0.7 |
| Fumaric acid | 19.27 | 444972 | Organic acids and derivatives | 0.0 | -0.1 | 0.2 | 0.5 | 0.6 | 0.0 | 1.3 | 1.2 |
| Uracil | 19.30 | 1174 | Organoheterocyclic compounds | 0.9 | 0.8 | 4.8 | 6.7 | 7.1 | 6.5 | 8.0 | 8.5 |
| Serine | 20.01 | 5951 | Organic acids and derivatives | 1.7 | 1.5 | 2.7 | 2.9 | 2.7 | 2.4 | 3.2 | 3.9 |
| L-Threonine | 20.99 | 6288 | Organic acids and derivatives | 0.9 | 0.6 | 1.9 | 2.2 | 1.4 | 1.4 | 2.3 | 3.0 |
| Glutaric acid | 21.22 | 743 | Organic acids and derivatives | 0.7 | 0.6 | 0.8 | 1.5 | 1.7 | 1.3 | 2.5 | 2.3 |
| Thymine | 21.42 | 1135 | Organoheterocyclic compounds | 0.6 | 0.5 | 0.8 | 1.2 | 5.5 | 5.6 | 7.4 | 7.8 |
| beta-Alanine | 22.29 | 239 | Organic acids and derivatives | 0.9 | 0.7 | 1.0 | 1.1 | 0.7 | 0.9 | 2.6 | 3.0 |
| L-Erythrulose | 23.68 | 5460032 | Organic oxygen compounds | -1.5 | -0.6 | -1.2 | -2.0 | -2.5 | -1.7 | -0.8 | -1.9 |
| Citramalic acid | 23.87 | 1081 | Lipids and lipid-like molecules | 0.6 | 0.6 | 0.4 | 1.1 | 1.2 | 1.1 | 1.7 | 1.5 |
| Adipic acid | 24.57 | 196 | Lipids and lipid-like molecules | 0.9 | 0.9 | 1.3 | 1.5 | 1.9 | 1.2 | 2.0 | 1.9 |
| N-Acetylserine | 24.76 | 65249 | Organic acids and derivatives | -0.2 | -0.5 | -1.4 | 0.2 | 0.5 | 0.3 | 1.5 | 1.9 |
| L-Aspartic acid | 25.25 | 5960 | Organic acids and derivatives | 0.8 | 1.4 | 1.8 | 1.9 | 2.3 | 2.2 | 2.4 | 2.5 |
| Methionine | 25.28 | 6137 | Organic acids and derivatives | 0.9 | 0.8 | 7.3 | 7.6 | 5.3 | 7.8 | 9.2 | 10.3 |
| Cytosine | 25.40 | 597 | Organoheterocyclic compounds | 1.8 | 0.1 | 2.0 | 2.7 | 3.1 | 0.7 | 1.9 | 2.0 |
| Threonic acid | 26.63 | 5460407 | Organic acids and derivatives | 0.0 | 0.1 | 0.3 | 0.2 | 0.2 | 0.3 | 1.3 | 1.2 |
| D-2-Hydroxyglutaric acid | 26.91 | 439391 | Organic acids and derivatives | -0.2 | -0.4 | 0.5 | 0.4 | 0.4 | 0.3 | 1.4 | 1.6 |
| 3-Hydroxymethylglutaric acid | 27.81 | 1662 | Lipids and lipid-like molecules | 0.4 | 0.2 | 0.4 | 0.4 | 0.3 | 0.3 | 1.6 | 1.3 |
| Glutamic acid | 28.25 | 33032 | Organic acids and derivatives | 0.5 | 0.7 | 2.2 | 2.0 | 1.4 | 1.7 | 2.1 | 2.4 |
| Triethanolamine | 28.40 | 7618 | Organic nitrogen compounds | 0.9 | 1.0 | 1.5 | 1.6 | 2.7 | 1.6 | 3.2 | 2.2 |
| 4-Hydroxybenzoic acid | 28.48 | 135 | Benzenoids | 0.0 | 0.2 | 0.7 | 1.1 | 1.3 | 0.8 | 2.4 | 2.3 |
| Phenylalanine | 28.66 | 6140 | Organic acids and derivatives | 3.1 | 4.1 | 6.6 | 6.6 | 5.8 | 6.4 | 7.6 | 8.4 |
| Tartaric acid | 29.01 | 444305 | Organic oxygen compounds | 1.3 | 1.3 | 1.6 | 2.2 | 2.0 | 1.7 | 3.3 | 3.1 |
| L-Asparagine | 29.80 | 6267 | Organic acids and derivatives | 0.9 | 0.8 | 1.1 | 10.4 | 1.4 | 11.0 | 15.3 | 14.6 |
| L-Arabinose | 29.83 | 439764 | Organic oxygen compounds | -0.2 | 0.3 | 0.4 | 0.3 | 0.8 | 0.1 | 1.6 | 1.0 |
| D-Ribose | 30.30 | 5779 | Organic oxygen compounds | 0.3 | 0.2 | 0.3 | 0.2 | 0.4 | 0.0 | 1.5 | 1.4 |
| Ribonolactone | 30.32 | 111064 | Organic oxygen compounds | -0.3 | -0.3 | -0.2 | -0.4 | 0.0 | -0.1 | 1.1 | 1.3 |
| Suberic acid | 30.35 | 10457 | Lipids and lipid-like molecules | 0.9 | 6.1 | 6.0 | 7.9 | 1.4 | 5.7 | 10.7 | 11.0 |
| Levoglucosan | 31.04 | 2724705 | Organoheterocyclic compounds | 0.6 | 0.5 | 1.1 | 1.3 | 1.7 | 1.0 | 1.8 | 1.3 |
| Aminoadipic acid | 31.07 | 92136 | Organic acids and derivatives | 0.9 | 0.8 | 1.1 | 1.5 | 9.3 | 9.2 | 11.6 | 12.4 |
| Aconitic acid | 31.85 | 309 | Organic acids and derivatives | -1.4 | -1.4 | -0.5 | -0.1 | -0.8 | -2.1 | -1.6 | -0.8 |
| Putrescine | 31.98 | 1045 | Organic nitrogen compounds | 0.4 | 0.4 | 0.6 | 1.1 | 0.6 | 0.2 | 1.1 | 1.1 |
| L-Fucose | 32.23 | 17106 | Organic oxygen compounds | 0.2 | 0.2 | 0.5 | 0.4 | 0.9 | 0.5 | 1.3 | 1.0 |
| Vanillic acid | 32.43 | 8468 | Benzenoids | 0.6 | 0.9 | 0.9 | 1.1 | 1.0 | 0.9 | 1.6 | 1.3 |
| Azelaic acid | 33.09 | 2266 | Lipids and lipid-like molecules | 0.4 | 0.8 | 1.1 | 1.9 | 2.1 | 1.6 | 3.6 | 4.0 |
| Shikimic acid | 33.62 | 8742 | Organic oxygen compounds | 0.4 | -0.5 | -1.9 | -2.0 | -0.8 | -1.1 | -0.3 | -1.0 |
| 3-Phosphoglyceric acid | 33.78 | 724 | Organic oxygen compounds | 0.9 | 0.1 | 0.5 | 0.9 | 1.6 | 1.6 | 1.8 | 0.0 |
| Ornithine | 34.07 | 6262 | Organic acids and derivatives | 0.0 | 0.1 | 1.1 | 1.4 | 1.7 | 1.3 | 1.8 | 2.0 |
| D-Tagatose | 35.20 | 14408225 | Organic oxygen compounds | 0.9 | 0.8 | 1.1 | 1.5 | 1.4 | 1.0 | 12.5 | 11.8 |
| Sebacic acid | 35.65 | 5192 | Lipids and lipid-like molecules | 3.8 | 4.1 | 4.5 | 5.0 | 5.7 | 5.4 | 6.2 | 6.6 |
| D-Fructose | 35.86 | 439709 | Organic oxygen compounds | -0.8 | -0.8 | -0.7 | -0.7 | -0.7 | -1.8 | -0.7 | -1.0 |
| L-Sorbose | 35.96 | 441484 | Organic oxygen compounds | -0.7 | -0.6 | -0.6 | -0.7 | -0.6 | -1.7 | -0.7 | -1.0 |
| Tyramine | 36.62 | 5610 | Benzenoids | 0.3 | 0.4 | 0.2 | 0.7 | -0.2 | 0.7 | 0.9 | 1.5 |
| Lysine | 36.74 | 5962 | Organic acids and derivatives | 0.9 | 8.3 | 12.6 | 12.5 | 12.2 | 12.4 | 13.2 | 14.0 |
| L-Tyrosine | 37.22 | 6057 | Organic acids and derivatives | 0.9 | 9.9 | 13.7 | 13.3 | 12.5 | 13.3 | 14.3 | 15.5 |
| D-Glucuronic acid | 37.60 | 444791 | Organic oxygen compounds | 0.2 | 0.3 | 0.4 | 0.2 | 1.0 | 0.7 | 1.7 | 1.2 |
| Galacturonic acid | 37.77 | 84740 | Organic oxygen compounds | 0.6 | 0.1 | 0.4 | 0.6 | 0.9 | 0.7 | 1.7 | 1.3 |
| Pantothenic acid | 38.61 | 6613 | Organic acids and derivatives | 0.3 | 0.4 | 1.0 | 1.1 | 0.4 | 1.1 | 1.6 | 1.3 |
| Palmitoleic acid | 38.95 | 445638 | Lipids and lipid-like molecules | 1.1 | 1.0 | 1.6 | 1.8 | 3.1 | 2.3 | 3.6 | 3.1 |
| Palmitic acid | 39.38 | 985 | Lipids and lipid-like molecules | 1.1 | 0.6 | 1.4 | 1.6 | 2.5 | 1.6 | 2.8 | 2.1 |
| Glucaric acid | 39.70 | 33037 | Organic acids and derivatives | 0.5 | 0.5 | 0.6 | 0.8 | 0.6 | 0.8 | 1.1 | 0.6 |
| N-Acetylmannosamine | 41.01 | 11096158 | Organic oxygen compounds | 0.1 | 0.0 | -0.2 | -0.8 | 0.4 | -0.5 | 1.4 | 0.9 |
| Heptadecanoic acid | 41.74 | 10465 | Lipids and lipid-like molecules | 1.0 | 0.9 | 1.4 | 1.6 | 1.6 | 1.0 | 1.8 | 1.9 |
| Linoleic acid | 43.38 | 5280450 | Lipids and lipid-like molecules | 1.0 | 1.1 | 1.6 | 1.4 | 2.1 | 1.3 | 2.4 | 2.3 |
| Oleic acid | 43.47 | 445639 | Lipids and lipid-like molecules | 1.3 | 1.1 | 1.8 | 1.6 | 2.6 | 1.7 | 3.1 | 2.6 |
| Stearic acid | 43.96 | 5281 | Lipids and lipid-like molecules | 1.1 | 0.7 | 1.5 | 1.8 | 2.4 | 1.6 | 2.5 | 2.0 |
| Tryptamine | 44.26 | 1150 | Organoheterocyclic compounds | -9.7 | -0.5 | -9.5 | -9.1 | 0.8 | 1.0 | 1.7 | 0.2 |
| Thymidine | 47.87 | 5789 | Nucleosides, nucleotides, and analogues | 0.9 | 0.8 | 1.1 | 1.5 | 1.4 | 1.0 | 7.3 | 7.1 |
| 5-Methoxytryptamine | 48.63 | 1833 | Organoheterocyclic compounds | 0.9 | 7.4 | 8.7 | 8.6 | 7.2 | 8.8 | 11.6 | 11.2 |
| Uridine | 48.99 | 6029 | Nucleosides, nucleotides, and analogues | 0.3 | 0.4 | 1.1 | 0.9 | 0.9 | 0.4 | 1.9 | 1.7 |
| Docosahexaenoic acid | 50.83 | 445580 | Lipids and lipid-like molecules | 1.0 | 0.9 | 1.6 | 1.7 | 1.6 | 1.2 | 1.9 | 1.6 |
| Adenosine | 52.62 | 60961 | Nucleosides, nucleotides, and analogues | 0.0 | -0.1 | 1.1 | 0.8 | 0.8 | 0.1 | 0.2 | 0.6 |
| Trehalose | 55.21 | 7427 | Organic oxygen compounds | -0.2 | 2.0 | -0.1 | 2.4 | 0.1 | 0.1 | 6.4 | 5.7 |
| D-Maltose | 55.30 | 10991489 | Organic oxygen compounds | -0.1 | 1.9 | -0.1 | 2.3 | -0.1 | -0.1 | 6.3 | 5.6 |

Table S4. Analysis of metabolic pathways

| Metabolic pathway | Total | Expected | Hits | p-values | Impact | Match compound |
| --- | --- | --- | --- | --- | --- | --- |
| Linoleic acid metabolism | 4 | 0.14397 | 1 | 0.137 | 1 | L-Aspartate, L-Asparagine, L-Glutamate, Fumarate, Pyruvate |
| Alanine, aspartate and glutamate metabolism | 22 | 0.79181 | 5 | 0.001 | 0.45324 | L-Phenylalanine |
| Phenylalanine metabolism | 12 | 0.4319 | 1 | 0.357 | 0.42308 | L-Tyrosine, Tyramine |
| Isoquinoline alkaloid biosynthesis | 6 | 0.21595 | 2 | 0.017 | 0.41176 | Putrescine, L-Proline, L-Glutamate, Ornithine |
| Arginine and proline metabolism | 28 | 1.0078 | 4 | 0.016 | 0.38532 | 3-Hydroxypropanoate, beta-Alanine, L-Aspartate, Pantothenate, Uracil |
| beta-Alanine metabolism | 18 | 0.64785 | 5 | 0.000 | 0.3254 | L-Serine, D-Glycerate, L-Aspartate, Threonine, Pyruvate |
| Glycine, serine and threonine metabolism | 33 | 1.1877 | 5 | 0.005 | 0.32415 | L-Tyrosine, Tyramine, Pyruvate, Fumarate, Acetoacetate |
| Tyrosine metabolism | 18 | 0.64785 | 5 | 0.000 | 0.27568 | L-Glutamate, Urea, L-Aspartate, L-Ornithine, Fumarate |
| Arginine biosynthesis | 18 | 0.64785 | 5 | 0.000 | 0.25632 | Pantothenate, beta-Alanine, Pyruvate, L-Valine, Uracil |
| Pantothenate and CoA biosynthesis | 25 | 0.89979 | 5 | 0.002 | 0.25329 | Tryptamine |
| Tryptophan metabolism | 23 | 0.82781 | 1 | 0.573 | 0.18605 | (9Z)-Octadecenoic acid, Hexadecanoic acid |
| Cutin, suberine and wax biosynthesis | 15 | 0.53987 | 2 | 0.099 | 0.16667 | Pyruvate, Fumarate |
| Pyruvate metabolism | 23 | 0.82781 | 2 | 0.199 | 0.14854 | L-Methionine, L-Serine, L-Aspartate, Pyruvate |
| Cysteine and methionine metabolism | 47 | 1.6916 | 4 | 0.085 | 0.13978 | D-Fructose, Trehalose, Maltose |
| Starch and sucrose metabolism | 22 | 0.79181 | 3 | 0.042 | 0.12545 | Pyruvate |
| Glycolysis / Gluconeogenesis | 26 | 0.93578 | 1 | 0.618 | 0.11665 | D-Glycerate, L-Serine, L-Glutamate |
| Glyoxylate and dicarboxylate metabolism | 29 | 1.0438 | 3 | 0.083 | 0.11602 | L-Threonine, L-Leucine, Pyruvate, L-Isoleucine, L-Valine |
| Valine, leucine and isoleucine biosynthesis | 22 | 0.79181 | 5 | 0.001 | 0.10727 | L-Tyrosine, Shikimate, L-Phenylalanine |
| Phenylalanine, tyrosine and tryptophan biosynthesis | 22 | 0.79181 | 3 | 0.042 | 0.1016 | Uracil, Uridine, Thymidine, Thymine, beta-Alanine |
| Pyrimidine metabolism | 40 | 1.4397 | 5 | 0.013 | 0.10143 | 3-Hydroxypropanoate |
| Propanoate metabolism | 19 | 0.68384 | 1 | 0.504 | 0.09653 | D-Glucuronate, D-Galacturonate |
| Pentose and glucuronate interconversions | 17 | 0.61186 | 2 | 0.123 | 0.09524 | D-Glucuronate, D-Glucarate |
| Ascorbate and aldarate metabolism | 20 | 0.71983 | 2 | 0.160 | 0.09184 | D-Fructose |
| Fructose and mannose metabolism | 18 | 0.64785 | 1 | 0.485 | 0.06695 | L-Glutamate, L-Ornithine, Putrescine |
| Glutathione metabolism | 27 | 0.97177 | 3 | 0.070 | 0.05622 | D-Glycerate |
| Glycerolipid metabolism | 19 | 0.68384 | 1 | 0.504 | 0.04 | L-Aspartate, Pyruvate |
| Carbon fixation in photosynthetic organisms | 21 | 0.75582 | 2 | 0.173 | 0.03627 | Pyruvate, Fumarate, (S)-3-Hydroxyisobutyrate |
| Citrate cycle (TCA cycle) | 20 | 0.71983 | 2 | 0.160 | 0.0295 | L-Valine, L-Isoleucine, L-Leucine, Acetoacetate |
| Valine, leucine and isoleucine degradation | 37 | 1.3317 | 5 | 0.009 | 0.02802 | Hexadecanoic acid, (9Z)-Hexadecenoic acid, Octadecanoic acid; (9Z)-Octadecenoic acid |
| Fatty acid biosynthesis | 56 | 2.0155 | 4 | 0.139 | 0.01123 | D-Glucuronate, 6-Deoxy-L-galactose, L-Arabinose, D-Fructose, D-Galacturonate |
| Amino sugar and nucleotide sugar metabolism | 52 | 1.8716 | 5 | 0.036 | 0.00927 | Adenosine, Urea |
| Purine metabolism | 70 | 2.5194 | 2 | 0.730 | 0.00823 | Hexadecanoic acid, Octadecanoic acid, (9Z)-Octadecenoic acid, Linoleate, (4Z,7Z,10Z,13Z,16Z,19Z)-Docosahexaenoic acid |
| Biosynthesis of unsaturated fatty acids | 22 | 0.79181 | 5 | 0.001 | 0 | L-Serine, Pyruvate, L-Lysine |
| D-Amino acid metabolism | 7 | 0.25194 | 3 | 0.001 | 0 | Glutamate, Pyruvate, Acetoacetate |
| Butanoate metabolism | 17 | 0.61186 | 3 | 0.021 | 0 | L-Aspartate, Pyruvate |
| Monobactam biosynthesis | 8 | 0.28793 | 2 | 0.031 | 0 | L-Aspartate, Lysine |
| Lysine biosynthesis | 9 | 0.32392 | 2 | 0.039 | 0 | Asparagine, L-Aspartate, L-Serine |
| Cyanoamino acid metabolism | 22 | 0.79181 | 3 | 0.042 | 0 | L-Valine, L-Leucine, L-Isoleucine |
| Glucosinolate biosynthesis | 22 | 0.79181 | 3 | 0.042 | 0 | L-Aspartate, Nicotinate |
| Nicotinate and nicotinamide metabolism | 13 | 0.46789 | 2 | 0.077 | 0 | L-Lysine, L-2-Aminoadipate |
| Lysine degradation | 20 | 0.71983 | 2 | 0.160 | 0 | Pyruvate |
| C5-Branched dibasic acid metabolism | 6 | 0.21595 | 1 | 0.198 | 0 | L-Phenylalanine |
| Tropane, piperidine and pyridine alkaloid biosynthesis | 9 | 0.32392 | 1 | 0.282 | 0 | L-Glutamate |
| Nitrogen metabolism | 11 | 0.39591 | 1 | 0.333 | 0 | L-Tyrosine, L-Phenylalanine |
| Phenylpropanoid biosynthesis | 33 | 1.1877 | 2 | 0.335 | 0 | Hexadecanoic acid, omega-Hydroxy fatty acid |
| Fatty acid degradation | 37 | 1.3317 | 2 | 0.388 | 0 | L-Serine |
| Sulfur metabolism | 15 | 0.53987 | 1 | 0.425 | 0 | D-Ribose |
| Pentose phosphate pathway | 19 | 0.68384 | 1 | 0.504 | 0 | 4-Hydroxybenzoate, L-Tyrosine |
| Ubiquinone and other terpenoid-quinone biosynthesis | 47 | 1.6916 | 2 | 0.512 | 0 | Pyruvate |
| Thiamine metabolism | 22 | 0.79181 | 1 | 0.556 | 0 | L-Methionine |
| Biosynthesis of various plant secondary metabolites | 22 | 0.79181 | 1 | 0.556 | 0 | Hexadecanoic acid |
| Fatty acid elongation | 23 | 0.82781 | 1 | 0.573 | 0 | Pyruvate |
| Lipoic acid metabolism | 24 | 0.8638 | 1 | 0.588 | 0 | D-Fructose |
| Galactose metabolism | 27 | 0.97177 | 1 | 0.632 | 0 | L-Serine |
| Sphingolipid metabolism | 27 | 0.97177 | 1 | 0.632 | 0 | D-Glucuronate |
| Inositol phosphate metabolism | 28 | 1.0078 | 1 | 0.645 | 0 | Pyruvate |
| Terpenoid backbone biosynthesis | 29 | 1.0438 | 1 | 0.658 | 0 | L-Serine |
| Glycerophospholipid metabolism | 38 | 1.3677 | 1 | 0.756 | 0 | Glutamate |
| Porphyrin metabolism | 47 | 1.6916 | 1 | 0.827 | 0 | L-Aspartate, L-Asparagine, L-Glutamate, Fumarate, Pyruvate |
| Linoleic acid metabolism | 4 | 0.14397 | 1 | 0.137 | 1 | L-Phenylalanine |