Fig. S1 In vivo safety evaluation of FZRL hydrogel. (A) H&E staining results of heart, liver, spleen, lung, and kidney treated with FZRL hydrogel (scale bar: 1000 μm). (B) H&E staining results of skin tissues in Control group and FZRL group (scale bar: 200 μm). (C) Quantitative detection of ALT, AST, BUN, and CREA in serum of Control group and FZRL group (n = 5).

Table. S1 Mathematical models of the regression for in vitro release profiles of 5Fu@ZIF-8

|  | Function | Equation | R2 |
| --- | --- | --- | --- |
| pH 7.4 | Zero order | y = 1.9723 + 0.25038x | 0.9734 |
|  | First order | y = 21.61444 × (1 - e-0.02599x) | 0.9773 |
|  | Higuchi | y = 2.31955x1/2 - 1.3913 | 0.993 |
|  | Ritger-Peppas | y = 1.28692x0.62785 | 0.9972 |
| pH 6.8 | Zero order | y = 18.12558 + 0.65239x | 0.7122 |
|  | First order | y = 52.15814 × (1 - e-0.13727x) | 0.9766 |
|  | Higuchi | y = 6.66074x1/2 + 7.2127 | 0.8827 |
|  | Ritger-Peppas | y = 13.81034x0.34767 | 0.9285 |
| pH 5.5 | Zero order | y = 37.87008 + 0.80604x | 0.5753 |
|  | First order | y = 78.45245 × (1 - e- 0.23492x) | 0.9677 |
|  | Higuchi | y = 8.57451x1/2+ 23.18511 | 0.7740 |
|  | Ritger-Peppas | y = 29.97282x0.26223 | 0.8751 |

Table S2 Mathematical models of the regression for in vitro release profiles of FZRL hydrogel

|  | Function | Equation | R2 |
| --- | --- | --- | --- |
| pH 7.4 | Zero order | y = -0.92491 + 3.28807x | 0.98709 |
|  | First order | y = -29.67012 × (1 - e0.07974x) | 0.99437 |
|  | Higuchi | y = 9.18829x1/2 - 4.25901 | 0.86715 |
|  | Ritger-Peppas | y = 2.17308x1.19662 | 0.99256 |
| pH 6.8 | Zero order | y = 14.67673 + 7.17649x | 0.84438 |
|  | First order | y = 63.99046 × (1 - e-0.45782x) | 0.99592 |
|  | Higuchi | y = 23.12472x1/2 + 2.43981 | 0.98633 |
|  | Ritger-Peppas | y = 27.96799x0.41202 | 0.99447 |
| pH 5.5 | Zero order | y = 25.67377 + 8.3467x | 0.72304 |
|  | First order | y = 77.95702 × (1 - e-0.72995x) | 0.99302 |
|  | Higuchi | y = 28.28496x1/2+ 9.19696 | 0.7740 |
|  | Ritger-Peppas | y = 46.00639x0.2834 | 0.99246 |