Supporting Information

For

Electrospun Dressing promotes diabetic-infected wound healing via Rapid and Sustained Antibacterial, ROS Scavenging, and Immune Modulation Ability

Hao Li1#, Haibing Liu2#, Rong Chen11#, Siqi Zheng1, Yixin Xu1, Mingyuan Lei1, Huaming Mai1, Hongyu Wang1, Taotao Cao3, Li Li4*, Yang Zhang1*, Jian Wang1*, Hao Cheng1*

1Department of Orthopedics, Nanfang Hospital, Southern Medical University, Guangzhou, 510515, China

2Department of Orthopedics, Affiliated Hengyang Hospital of Hunan Normal University & Hengyang Central Hospital, Hengyang, 421001, Hunan, China

3School of Basic Medical Sciences, Southern Medical University, Guangzhou, 510515, China

4State Key Laboratory of Multi-organ Injury Prevention and Treatment, National Clinical Research Center of Kidney Disease, Division of Nephrology, Nanfang Hospital, Southern Medical University, Guangzhou, 510515, China

#These authors contributed equally to this work

Correspondence: Li Li4, Yang Zhang1, Jian Wang 1, Hao Cheng1

Tel +86-020-62787191

Fax 020-61641961

Prof. Li Li, E-mail: guilinlily3@i.smu.edu.cn

Prof. Yang Zhang, E-mail: nfgjzy@126.com

Prof. Jian Wang, E-mail: wangjiannanfanghospital@gmail.com

Dr. Hao Cheng, E-mail: haocool317@gmail.com

Figure. S1 Interfacial and degradation properties of PC-based nanofiber membranes: (a) The diameter distribution of the PC-based nanofibers; (b,c) Particle size distribution of BPNSs and PDA@ZnO as determined by dynamic light scattering (DLS); (d) The cumulative Zn2+ release profiles of the PCZ and PCPZ were measured on days 1 to 21; (e) Degradation profiles of PC, PCB, PCPZ and PCBPZ nanofiber membranes; (f) Degree of swelling (%) of nanofiber mats with different weight ratios.

Figure. S2 Transcriptomic analysis of L929 cells treated with PCBPZ nanofiber membranes. (a) Bar chart showing the number of significantly upregulated (red) and downregulated (blue) genes between the PCBPZ and NC groups; (b) Volcano plot illustrating differentially expressed genes (DEGs) between the two groups. A total of 2,720 DEGs were identified, including 767 upregulated and 1,953 downregulated genes (|log₂Fold Change| > 1, p < 0.05). Representative genes with the most significant expression changes are labeled.

Table1: Primers used for qRT-PCR

| Primer | Sequence (5'-3') |
| --- | --- |
| CD206-F | AGCCAACACCAGCTCCTCAAGA |
| CD206-R | CAAAACGCTCGCGCATTGTCCA |
| CD86-F | CCATCAGCTTGTCTGTTTCATTCC |
| CD86-R | GCTGTAATCCAAGGAATGTGGTC |
| IL-10-F | TCTCCGAGATGCCTTCAGCAGA |
| IL-10-R | TCAGACAAGGCTTGGCAACCCA |
| IL-Iβ-F | CCACAGACCTTCCAGGAGAATG |
| IL-Iβ-R | GTGCAGTTCAGTGATCGTACAGG |
| iNOS2-F | GCTCTACACCTCCAATGTGACC |
| iNOS2-R | CTGCCGAGATTTGAGCCTCATG |
| TNF-α-F | CTCTTCTGCCTGCTGCACTTTG |
| TNF-α-R | ATGGGCTACAGGCTTGTCACTC |
| GAPDH-F | GTCTCCTCTGACTTCAACAGCG |
| GAPDH-R | ACCACCCTGTTGCTGTAGCCAA |

Table 2: NIR Irradiation Parameters

| Parameter | Value |
| --- | --- |
| Wavelength | 808 nm |
| Power density | 1.0 W/cm2 |
| Spot diameter | 0.9 cm (area ≈ 0.64 cm2) |

Table 3: Photothermal Performance of PCBPZ Under Different Power Densities

| Power density | Temperature at 5 min |
| --- | --- |
| 0.50 W/cm2 | 42.2 ℃ |
| 0.75 W/cm2 | 46.2 ℃ |
| 1.00 W/cm2 | 60.7 ℃ |
| 1.25 W/cm2 | 79.7 ℃ |

Table 4: Photothermal Heating Kinetics of Different Nanofiber Formulations (1.0 W/cm2) (Temperature rise at 0–120 s)

| Time (s) | PC | PCB | PCPZ | PCBPZ |
| --- | --- | --- | --- | --- |
| 0 | 22.0 | 22.0 | 22.0 | 22.0 |
| 10 | 22.1 | 33.6 | 29.3 | 38.9 |
| 20 | 22.2 | 40.3 | 33.5 | 45.1 |
| 30 | 22.3 | 45.8 | 37.8 | 52.4 |
| 40 | 22.4 | 49.1 | 40.5 | 54.1 |
| 50 | 22.3 | 51.7 | 41.5 | 56.2 |
| 60 | 22.4 | 52.6 | 42.4 | 57.2 |
| 70 | 22.1 | 52.9 | 43.2 | 58.0 |
| 80 | 22.4 | 53.5 | 43.8 | 58.9 |
| 90 | 22.2 | 53.5 | 44.6 | 58.7 |
| 100 | 22.1 | 53.4 | 44.9 | 58.9 |
| 110 | 22.3 | 53.5 | 44.8 | 58.8 |
| 120 | 22.2 | 53.6 | 44.9 | 58.9 |

Table 5: Fiber Morphology and Water Contact Angle

| Group | Fiber diameter (nm) | Contact angle |
| --- | --- | --- |
| PC | 198 ± 39.56 | 54 ± 4 |
| PCB | 245 ± 31.72 | 60 ± 8 |
| PCPZ | 247 ± 38.64 | 42 ± 2 |
| PCBPZ | 287 ± 29.12 | 56 ± 3.5 |

Table 6: Zn2+ Release Profile (μg/mL) of PCBPZ group

|  | pH 7.4 | pH 6.5 | pH 5.5 |
| --- | --- | --- | --- |
| Day 1 | 3.93 | 3.86 | 7.37 |
| Day 3 | 3.96 | 4.36 | 8.74 |
| Day 7 | 4.45 | 5.08 | 10.22 |
| Day 11 | 4.93 | 5.54 | 11.45 |
| Day 14 | 5.20 | 5.94 | 11.86 |
| Day 21 | 5.88 | 6.91 | 12.58 |

Table 7: Antibacterial Efficacy

3 min survival (%)

| Group | MSSA | MRSA | E. coli |
| --- | --- | --- | --- |
| NC | 99.0 | 95.0 | 97.3 |
| PC | 76.0 | 94.0 | 71.3 |
| PCB-NIR | 47.7 | 62.3 | 51.7 |
| PCPZ | 67.0 | 82.0 | 58.3 |
| PCBPZ-NIR | 0.33 | 2.33 | 1.0 |

5 min survival (%)

| Group | MSSA | MRSA | E. coli |
| --- | --- | --- | --- |
| NC | 98.8 | 95.2 | 96.6 |
| PC | 75.1 | 88.3 | 69.1 |
| PCB-NIR | 38.2 | 51.7 | 40.5 |
| PCPZ | 55.4 | 72.6 | 47.2 |
| PCBPZ-NIR | 0.28 | 0.67 | 0.86 |

Table 8: Biofilm Damage Rate

| Strian | NC | PC | PCB-NIR | PCPZ-NIR | PCBPZ-NIR |
| --- | --- | --- | --- | --- | --- |
| ATCC25923 | 4.0 | 13.3 | 59.3 | 51.0 | 97.7 |
| ATCC43300 | 3.0 | 10.7 | 48.0 | 45.0 | 96.3 |
| ATCC25922 | 3.3 | 5.3 | 41.0 | 44.3 | 98.3 |