Supporting Information

Self-assembled fluorescent nanosensor for ultrafast and field-deployable monitoring of herbicide fomesafen in multiple matrices

Mei-Hong Ge a, Shuai Tan a, Wei Niu a, Feng Gao a, Shi-Tao Liu a, Lin-Lin Yang a, c, Li-Wei Liu a, A-Ling Tang a, b, *, Xiang Zhou a,* and Song Yang a,*

a State Key Laboratory of Green Pesticides, Key Laboratory of Green Pesticide and Agricultural Bioengineering, Ministry of Education, Center for R&D of Fine Chemicals of Guizhou University, Guiyang, 550025, China.

b School of Biological Sciences, Guizhou Education University, Guiyang, 550018, China

c College of Materials Science and Engineering, Guiyang University, Guiyang 550003, PR China.

* Corresponding author.

E-mail: xiangzhou@gzu.edu.cn or zhoux1534@163.com (X. Zhou);

AL1358703140@163.com (A.-L. Tang);

jhzx.msm@gmail.com or syang@gzu.edu.cn (S. Yang)

Contents

1.	Materials and Instruments	4

2.	Synthesis and characterization of probes	4

3.	1H NMR, 13C NMR, and HRMS spectra of probes	7

4.	Self-Assembly Molecular Dynamics Simulation of RBO	21

5.	Scanning electron microscope images of RT, RO, RBT, RMBO and RNBO	21

6.	Comparison of fluorescence intensity of probes for FSA	22

7.	Investigation of the Optimal Excitation Wavelength	22

8.	The molecular structure of various herbicides	23

9.	Anti-disturbance experiments in the presence of two or more other herbicides	23

10.	Detection limit calculation	24

11.	Reversibility	25

12.	pH-Dependent Fluorescence Response	25

13.	Stability of the RBO under different storage conditions	25

15.	Response of RBO to the FSA analogues	29

16.	Detection of FSA in the soil extract solution	30

17.	Linear calibration curve of test paper fluorescence intensity versus FSA concentration	30

18.	Smartphone platform test parameters	31

19.	The RGB values of the test strips under different concentrations of FSA	31

22.	Linear calibration curve of hydrogel fluorescence intensity versus FSA concentration	34

23.	The RGB values of the hydrogel under different concentrations of FSA	34

24.	Bioluminescence Imaging	35

25.	Comparison of different methods for FSA determination	36

- Materials and Instruments

Rhodamine B, 2-aminobenzoxazole, and other chemical reagents/starting materials were purchased from commercial suppliers. Unless otherwise specified, all chemicals were used directly without further purification. All solvents were of HPLC/ACS grade. NMR spectra were recorded on a Bruker Biospin AG-400 or JEOL ECX 500 spectrometer. Crystal structures were determined using a Bruker D8 Venture instrument. Tetramethylsilane (TMS) served as the internal standard. HRMS was performed on a Thermo Scientific Ultimate 3000 system. Fluorescence measurements were conducted on a Horiba PTI QuantaMasterTM 8000 spectrofluorometer, while absorption spectra were acquired with a Shimadzu UV-1900 spectrophotometer. FT-IR spectra were recorded on a Nicolet iS 50 spectrometer. Fluorescent imaging was performed using a ZEISS LSM 900 confocal microscope and an Olympus FVMPE-RS multiphoton laser scanning microscope. The high-performance liquid chromatography (HPLC) system involved was an Agilent Technologies 1260 Infinity II system equipped with a Kinetex® 5 μm EVO C18 100 Å column.

- Synthesis and characterization of probes

Scheme S1. Synthetic routes of probes.

The synthetic route of probes was depicted in Scheme S1. Probes RT, RO, RBT, RMBO, and RNBO were synthesized according to the reference [1, 2]. Take probe RT and RNBO as examples. The details are as follows:

Synthesis of RT: A mixture of rhodamine B (200 mg, 450.89 μmol), EDCI (103.72 mg, 541.07 μmol), and HOBT (73.11 mg, 541.07 μmol) in anhydrous acetonitrile (8 mL) was magnetically stirred at room temperature for 30 minutes. After the addition of 2-aminothiazole (80.17 mg, 541.07 μmol), the reaction was allowed to proceed with continuous stirring at room temperature for 5 hours. Upon completion, the solvent was removed in vacuo using a rotary evaporator. The resulting crude product was subjected to flash column chromatography (eluent: petroleum ether/ethyl acetate = 2:1, v/v) to afford probe RT (yield: 85%). 1H NMR (500 MHz, CDCl3) δ 8.04 (d, J = 7.5 Hz, 1H), 7.54 (dqd, J = 14.5, 7, 1.0 Hz, 2H), 7.27 (d, J = 1 Hz, 1H), 7.19 (d, J = 7.5 Hz, 1H), 6.81 (d, J = 3.5 Hz, 1H), 6.44 (d, J = 2.5 Hz, 2H), 6.40 (d, J = 9 Hz, 2H), 6.17 (dd, J = 9, 2.5 Hz, 2H), 3.37 – 3.25 (m, 8H), 1.14 (d, J = 7.0 Hz, 12H).13C NMR (126 MHz, CDCl3) δ 166.66, 155.26, 153.95, 153.85, 148.85, 138.67, 134.21, 128.96, 128.61, 128.02, 124.76, 123.43, 112.61, 107.39, 106.56, 97.67, 67.66, 44.36, 12.77. HRMS calc. for C31H33O2N4S: 525.2300, [M + H]+, Found: 525.2300.

Synthesis of RNBO: A solution of rhodamine B (300 mg, 676.34 μmol) in 1,2-dichloroethane (7 mL) was treated with phosphorus oxychloride (0.5 mL) and further refluxed for 4 hours, followed by solvent evaporation under reduced pressure. The resulting crude chloric acid was dissolved in acetonitrile (4 mL) and subsequently added dropwise to a mixture of 5-nitro-2-benzoxazolamide (155.59 mg, 811.60 μmol) and triethylamine (0.5 mL). After the reaction for 5 hours, the solvent was removed, and the crude product was purified via column chromatography using a petroleum ether/ethyl acetate (2:1, v/v) eluent system, affording the target RNBO with a yield of 12%. 1H NMR (500 MHz, DMSO-d6) δ 8.16 (d, J = 1.5 Hz), 8.08 (dd, J = 9, 2 Hz), 8.04 (d, J = 7.5 Hz), 7.72 (dd, J = 17, 9 Hz), 7.64 (t, J = 7.5 Hz), 7.14 (d, J = 7.5 Hz), 6.49 (d, J = 9 Hz), 6.43 (d, J = 2 Hz), 6.25 (dd, J = 9, 2 Hz), 3.27 (dd, J = 6.5, 13.5 Hz), 1.03 (t, J = 7 Hz).13C NMR (126 MHz, DMSO-d6) δ 165.12, 155.80, 153.29, 152.98, 151.38, 148.57, 144.90, 140.40, 135.65, 129.39, 127.83, 127.12, 124.58, 123.84, 119.97, 114.16, 110.74, 107.72, 104.95, 97.00, 43.62, 12.42. HRMS calc. for C36H37O3N4: 604.2542, [M + H]+, Found: 604.2554.

RO: 51% yield. 1H NMR spectrum, 1H NMR (400 MHz, CDCl3) δ 8.03 (d, J = 6.8 Hz, 1H), 7.55 - 7.44 (m, 2H), 7.24 (s, 1H), 7.6 (d, J = 7.3 Hz, 1H), 6.85 (s, 1H), 6.54 (d, J = 8.8 Hz, 2H), 6.38 (d, J = 2.4 Hz, 2H), 6.22 (dd, J = 8.8, 2.4 Hz, 2H), 3.30 (q, J = 7.2 Hz, 8H), 1.14 (t, J = 7.2 Hz, 12H). 13C NMR (101 MHz, CDCl3) δ 166.19, 153.4, 152.52, 148.96, 135.35, 134.28, 128.83, 128.54, 127.06, 124.46, 123.95, 107.80, 106.01, 97.66, 44.39, 12.73. HRMS calc. for C31H33O3N4: 509.2523, [M + H]+, Found: 509.2547.

RBT: 51% yield. 1H NMR (400 MHz, DMSO-d6) δ 8.05 (d, J = 7.6 Hz, 1H), 7.92 (d, J = 7.6 Hz, 1H), 7.69 (dt, J = 25.2, 6.8 Hz, 2H), 7.42 (d, J = 8.0 Hz, 1H), 7.31 (t, J = 7.2 Hz, 1H), 7.26 – 7.16 (m, 2H), 6.43 (d, J = 2.4 Hz, 2H), 6.34 (d, J = 8.8 Hz, 2H), 6.19 (dd, J = 8.8, 2.4 Hz, 2H), 3.27 (dd, J = 6.8, 7.2 Hz, 8H), 1.04 (t, J = 6.8 Hz, 12H).13C NMR (101 MHz, DMSO-d6) δ 166.38, 153.63, 153.58, 153.27, 148.55, 148.40, 135.29, 131.08, 129.28, 127.83, 127.63, 126.05, 124.70, 123.80, 123.46, 121.57, 121.08, 107.29, 105.69, 96.86, 67.50, 43.63, 12.45. HRMS calc. for C35H36O2N4S: 575.2462, [M + H]+, Found: 575.2475.

RMBO: 45% yield. 1H NMR (500 MHz, DMSO-d6) δ 8.00 (d, J = 7.5 Hz), 7.67 (t, J = 8.0 Hz), 7.62 (t, J = 7.4 Hz), 7.38 (d, J = 8.3 Hz), 7.22 (s), 7.10 (d, J = 7.6 Hz), 7.01 (d, J = 8.9 Hz), 6.47 (d, J = 8.9 Hz), 6.39 (d, J = 2.4 Hz), 6.26 (dd, J = 8.9, 2.5 Hz), 3.28 (q, J = 6.9 Hz), 2.29 (s), 1.05 (t, J = 7.0 Hz).13C NMR (126 MHz, DMSO-d6) δ 165.23, 153.42, 152.82, 148.43, 145.92, 140.03, 135.18, 133.99, 129.16, 127.75, 127.45, 124.74, 124.43, 123.59, 118.79, 109.48, 107.65, 105.33, 97.00, 43.62, 20.87, 12.36. HRMS calc. for C36H37O3N4: 573.2800, [M + H]+, Found: 573.2900.

- 1H NMR, 13C NMR, and HRMS spectra of probes

Fig. S1. 1H NMR (500 MHz) spectrum of RT in CDCl3.

Fig. S2. 13C NMR (126 MHz) spectrum of RT in CDCl3.

Fig. S3. HRMS spectrum of RT.

Fig. S4. 1H NMR (400 MHz) spectrum of RO in CDCl3.

Fig. S5. 13C NMR (101 MHz) spectrum of RO in CDCl3.

Fig. S6. HRMS spectrum of RO.

Fig. S7. 1H NMR (400 MHz) spectrum of RBT in DMSO-d6.

Fig. S8. 13C NMR (101 MHz) spectrum of RBT in DMSO-d6.

Fig. S9. HRMS spectrum of RBT.

Fig. S10. 1H NMR (500 MHz) spectrum of RBO in CDCl3.

Fig. S11. 13C NMR (126 MHz) spectrum of RBO in CDCl3.

Fig. S12. HRMS spectrum of RBO.

Fig. S13. 1H NMR (500 MHz) spectrum of RMBO in DMSO-d6.

Fig. S14. 13C NMR (126 MHz) spectrum of RMBO in DMSO-d6.

Fig. S15. HRMS spectrum of RMBO.

Fig. S16. 1H NMR (500 MHz) spectrum of RNBO in DMSO-d6.

Fig. S17. 13C NMR (126 MHz) spectrum of RNBO in DMSO-d6.

Fig. S18. HRMS spectrum of RNBO.

Fig. S19. The crystal structure of RBT and all the hydrogen atoms are omitted for clarity (CCDC: 2403991; grey atoms, C; red atoms, O; blue atoms, N; yellow, S).

Table S1. Crystal data and structural refinement parameters of RBT.

| Compound | Molecule RBT |
| --- | --- |
| Formula | C35H34N4O2S |
| CCDC numbers | 2403991 |
| Fw | 574.72 |
| Crystal system | orthorhombic |
| Space group | Pccn |
| a (Å) | 30.808(2) |
| b (Å) | 27.2936(15) |
| c (Å) | 9.8153(5) |
| α (°) | 90 |
| β (°) | 90 |
| γ (°) | 90 |
| Z | 8 |
| Calculated density (gcm−3) | 0.925 |
| F (000) | 2432.0 |
| Reflections | 20527 / 7299 |
| collected/unique | [R(int) = 0.0790] |
| Goodness-of-fit on F2 | 0.979 |
| Final R indices | R1 = 0.1007 |
| [I >2σ(I)] | wR2 = 0.2633 |
| R indices (all data) | R1 = 0.1458, wR2 = 0.3158 |

Fig. S20. The crystal structure of RBO and all the hydrogen atoms are omitted for clarity (CCDC: 2385138; grey atoms, C; red atoms, O; blue atoms, N).

Table S2. Crystal data and structural refinement parameters of RBO.

| Compound | Molecule RBO |
| --- | --- |
| Formula | C35H34N4O3 |
| CCDC numbers | 2385138 |
| Fw | 558.66 |
| Crystal system | Monoclinic |
| Space group | P2(1)/c |
| a (Å) | 33.506(4) |
| b (Å) | 12.0476(14) |
| c (Å) | 15.2625(18) |
| α (°) | 90 |
| β (°) | 104.219(9) |
| γ (°) | 90 |
| Z | 8 |
| Calculated density (gcm−3) | 1.274 |
| F (000) | 1184 |
| Reflections | 13426 / 5119 |
| collected/unique | [R(int) = 0.0365] |
| Goodness-of-fit on F2 | 1.076 |
| Final R indices | R1 = 0.0643 |
| [I >2σ(I)] | wR2 = 0.1223 |
| R indices (all data) | R1 = 0.1005, wR2 = 0.1371 |

Fig. S21. The crystal structure of RMBO and all the hydrogen atoms are omitted for clarity (CCDC: 2403984; grey atoms, C; red atoms, O; blue atoms, N).

Table S3. Crystal data and structural refinement parameters of RMBO.

| Compound | Molecule RMBO |
| --- | --- |
| Formula | C36H36N4O3 |
| CCDC numbers | 2403984 |
| Fw | 572.69 |
| Crystal system | monoclinic |
| Space group | P21/c |
| a (Å) | 9.8527(2) |
| b (Å) | 26.2592(6) |
| c (Å) | 11.5347(3) |
| α (°) | 90 |
| β (°) | 101.867(2) |
| γ (°) | 90 |
| Z | 2920.52(12) |
| Calculated density (gcm−3) | 1.302 |
| F (000) | 1216.0 |
| Reflections | 11172 / 5759 |
| collected/unique | [R(int) = 0.0402] |
| Goodness-of-fit on F2 | 1.026 |
| Final R indices | R1 = 0.0488 |
| [I >2σ(I)] | wR2 = 0.1270 |
| R indices (all data) | R1 = 0.0561, wR2 = 0.1357 |

- Self-Assembly Molecular Dynamics Simulation of RBO

Fig. S22. Molecular dynamics simulation of the RBO self-assembly process. (a) The root mean square deviation of the RBO system during the simulation process. (b) Solvent accessible surface area (SASA) of RBO system during the simulation time. (c) Time evolution of the radius of gyration for the RBO system during the simulation time.

- Scanning electron microscope images of RT, RO, RBT, RMBO and RNBO

Fig. S23. SEM of RT, RO, RBT, RMBO and RNBO

- Comparison of fluorescence intensity of probes for FSA

Fig. S24. (a) The fluorescence intensity and (b) enhancement folds of the six probes (10 μM) upon the addition of 10 μM FSA. Error bars indicate the SD calculated from three independent measurements (n=3). Experimental conditions: λex = 560 nm; slits, 2/2 nm; and MeOH-H2O, 2:3 (v/v).

- Investigation of the Optimal Excitation Wavelength

Fig. S25. (a) Normalized absorption, excitation, and emission spectra of the RBO-FSA complex in solution. (b) After adding the FSA, the fluorescence intensities were measured at excitation wavelengths of 550, 555, 560, 565, and 570 nm respectively.

- The molecular structure of various herbicides

Fig. S26. The molecular structure of various herbicides

- Anti-disturbance experiments in the presence of two or more other herbicides

Fig. S27. Anti-interference experiments adding 10 μM FSA into the premixed solution incorporating the probe RBO (10 μM) and two or more other herbicides (10 μM): (1) Blank, (2) clodinafop-propargyl + bifenox, (3) clodinafop-propargyl + bifenox + flutolanil, (4) clodinafop-propargyl + bifenox + flutolanil + fenoxaprop-p-ethyl, (5) clodinafop-propargyl + bifenox + flutolanil + fenoxaprop-p-ethyl + metamifop, (6) clodinafop-propargyl + bifenox + flutolanil + fenoxaprop-p-ethyl + metamifop + oxyfluorfen, (7) clodinafop-propargyl + bifenox + flutolanil + fenoxaprop-p-ethyl + metamifop + oxyfluorfen + cyhalofop-butyl, (8) clodinafop-propargyl + bifenox + flutolanil + fenoxaprop-p-ethyl + metamifop + oxyfluorfen + cyhalofop-butyl + tribenuron methyl.

- Detection limit calculation

To determine the detection limit, we processed the spectrofluorometric titration datasets and established a calibration curve between the concentrations of FSA and the fluorescence titration data at 588 nm. Detection limit is calculated as follows:

LOD = 3σ/k

where σ denotes deviation of the blank measurement (ten blank determinations) and k represents the slope between the fluorescence intensity versus analyte concentration.

- Reversibility

Fig. S28. Fluorescence intensity of RBO recorded after adding FSA and TEA for six continuous cycles (Experimental conditions: λex = 561 nm; slits, 2/2 nm; and MeOH/H2O = 2:3, v/v)

- pH-Dependent Fluorescence Response

Fig. S29. (a) Fluorescence emission spectra of the RBO at different pH values.

- Stability of the RBO under different storage conditions

Fig. 30. (a) Fluorescence response of the RBO to FSA after one-week storage at different temperatures (4℃, 25℃, and 37℃). (b) Fluorescence response of the RBO to FSA after two -week storage at different temperatures (4℃, 25℃, and 37℃). (c) Fluorescence intensities of RBO stored at the same temperature (4 ℃) for 1 day, 7 days and 14 days, respectively. Data are presented as mean ± SD (n = 3).

- Chemical shifts of FSA and RBO after complex formation

Table S4. The chemical shift of FSA after the formation of the complex RBO-FSA with different molar ratios.

| Chemical shift (ppm) | proton |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | 1' | 2' | 3' | 4' | 5' | 6' |
| FSA | 8.18 | 7.78 | 7.61 | 7.26 | 7.08 | 6.98 |
| FSA: RBO = 0.5:1 | 8.19 | 7.79 | 7.59 | 7.22 | 7.1 | 6.99 |
| FSA: RBO = 1:1 | 8.19 | 7.78 | 7.60 | 7.25 | 7.09 | 6.98 |
| FSA: RBO = 1.5:1 | 8.18 | 7.78 | 7.60 | 7.24 | 7.08 | 6.98 |
| FSA: RBO = 2:1 | 8.18 | 7.77 | 7.59 | 7.24 | 7.07 | 6.98 |
| FSA: RBO = 3:1 | 8.18 | 7.77 | 7.59 | 7.24 | 7.07 | 6.97 |
| Shift FSA: RBO = 0.5:1 | 0.01 | 0.01 | -0.02 | -0.04 | 0.02 | -0.01 |
| Shift FSA: RBO = 1:1 | 0.01 | 0 | -0.01 | -0.01 | 0.01 | 0 |
| Shift FSA: RBO = 1.5:1 | 0 | 0 | -0.01 | -0.02 | 0 | 0.01 |
| Shift FSA: RBO = 2:1 | 0 | -0.01 | -0.02 | -0.02 | -0.01 | -0.01 |
| Shift FSA: RBO = 3:1 | 0 | -0.01 | -0.02 | -0.02 | -0.01 | -0.02 |

Table S5. The chemical shift of RBO after the formation of the complex RBO-FSA with different molar ratios.

| Chemical shift (ppm) | proton |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 1 | 2-4 | 5 | 6,7 | 8 | 9,10 | 11,12 | 13,14 |
| RBO | 8.09 | 7.51 | 7.30 | 7.17 | 7.11 | 6.54 | 6.43 | 6.20 |
| FSA: RBO = 0.5:1 | 8.06 | 7.5 | 7.27 | 7.15 | 7.1 | 6.50 | 6.40 | 6.19 |
| FSA: RBO = 1:1 | 8.04 | 7.48 | 7.25 | 7.15 | 7.09 | 6.49 | 6.39 | 6.18 |
| FSA: RBO = 1.5:1 | 8.03 | 7.47 | 7.24 | 7.14 | 7.08 | 6.48 | 6.39 | 6.17 |
| FSA: RBO = 2:1 | 8.02 | 7.46 | 7.24 | 7.13 | 7.07 | 6.47 | 6.38 | 6.16 |
| FSA: RBO = 3:1 | 8.02 | 7.45 | 7.24 | 7.13 | 7.07 | 6.47 | 6.38 | 6.16 |
| Shift FSA: RBO = 0.5:1 | -0.03 | -0.01 | -0.03 | -0.02 | -0.01 | -0.04 | -0.03 | -0.01 |
| Shift FSA: RBO = 1:1 | -0.05 | -0.03 | -0.05 | -0.02 | -0.02 | -0.05 | -0.04 | -0.02 |
| Shift FSA: RBO = 1.5:1 | -0.06 | -0.04 | -0.06 | -0.03 | -0.03 | -0.06 | -0.04 | -0.03 |
| Shift FSA: RBO = 2:1 | -0.04 | -0.05 | -0.06 | -0.04 | -0.04 | -0.07 | -0.05 | -0.04 |
| Shift FSA: RBO = 3:1 | -0.04 | -0.06 | -0.06 | -0.04 | -0.04 | -0.07 | -0.05 | -0.04 |

- Response of RBO to the FSA analogues

Fig. S31. Fluorescence spectra of RBO after adding 10 μM contrast. Data are presented as mean ± SD (n = 3). (Experimental conditions: MeOH/H2O = 2/3, v/v, λex = 560 nm, slits: 2 nm/2 nm).

- Detection of FSA in the soil extract solution

Fig. S32. The fluorescence intensity of the soil filtrate containing different concentrations of FSA after the addition of RBO. Data are presented as mean ± SD (n = 3).

- Linear calibration curve of test paper fluorescence intensity versus FSA concentration

Fig. S33. Linear calibration curve of test strips fluorescence intensity versus FSA concentration.

- Smartphone platform test parameters

Table S6. Smartphone platform test parameters.

| Projects | Test condition |
| --- | --- |
| Phone model Camera settings | iphone XR No special settings |
| Shooting environment（Fluorescence） | Camera obscura-type UV analyzer |
| Smartphone software | “Color recognizer” and “Curve fitting” app |

- The RGB values of the test strips under different concentrations of FSA

Table S7. The RGB values of the test strips under different concentrations of FSA.

| CFSA (μm) | R/B |  |  | Mean | SD |
| --- | --- | --- | --- | --- | --- |
| 0 | 122/212 | 124/221 | 130/224 | 0.5723 | 0.01002 |
| 100 | 149/233 | 155/235 | 155/238 | 0.65011 | 0.01009 |
| 200 | 139/205 | 140/207 | 140/203 | 0.68134 | 0.00725 |
| 300 | 157/213 | 160/216 | 157/216 | 0.73489 | 0.0072 |
| 400 | 147/180 | 143/178 | 143/180 | 0.80483 | 0.01118 |
| 500 | 175/194 | 175/196 | 175/194 | 0.88976 | 0.0141 |
| 600 | 176/188 | 177/190 | 177/189 | 0.93475 | 0.00275 |

- The rate of recovery of FSA in real samples

Table S8. The rate of recovery of FSA in real samples (n = 3).

| Sample | added (μM) | FSA found (μM) | RSD of RBO (％) | Recovery of RBO (％) | HPLC (μM) |
| --- | --- | --- | --- | --- | --- |
| Potatoes | 0 | Not detected |  |  |  |
|  | 7 | 7.45 | 1.03 | 106.3 | 7.26 |
|  | 10 | 10.58 | 2.67 | 105.8 | 11.7 |
| Sweet potato | 0 | Not detected |  |  |  |
|  | 7 | 7.07 | 0.32 | 100.9 | 6.87 |
|  | 10 | 9.70 | 0.47 | 97 | 11.1 |

- HPLC method for determining FSA content

HPLC analysis was performed on an Agilent Technologies 1260 Infinity II system equipped with a Kinetex® 5 μm EVO C18 100 Å column. The mobile phase was composed of 90% acetonitrile (v/v) and 10% water, delivered at a flow rate of 0.50 mL/min. Detection was performed at 290 nm.

Fig. S34. HPLC calibration curve for FSA quantification.

Fig. S35. Representative HPLC chromatograms of potato samples spiked with FSA at concentrations of 7 μM and 10 μM.

Fig. S36. Representative HPLC chromatograms of sweet potato samples spiked with FSA at concentrations of 7 μM and 10 μM.

- Linear calibration curve of hydrogel fluorescence intensity versus FSA concentration

Fig. S37. Linear calibration curve of hydrogel fluorescence intensity versus FSA concentration.

- The RGB values of the hydrogel under different concentrations of FSA

Table S9. The RGB values of the hydrogel under different concentrations of FSA.

| CFSA (μm) | R/B |  |  | Mean | SD |
| --- | --- | --- | --- | --- | --- |
| 0 | 98/212 | 93/203 | 93/191 | 0.4691 | 0.01556 |
| 50 | 122/224 | 120/217 | 123/227 | 0.5465 | 0.0058 |
| 100 | 109/173 | 124/197 | 122/196 | 0.62732 | 0.00423 |
| 200 | 153/210 | 149/192 | 143/194 | 0.74724 | 0.0253 |
| 300 | 236/219 | 239/215 | 242/222 | 1.09311 | 0.0172 |
| 400 | 247/200 | 246/201 | 243/202 | 1.22062 | 0.01626 |
| 500 | 251/166 | 253/164 | 251/166 | 1.52226 | 0.01769 |

- Bioluminescence Imaging

Fig. S38. (a) and (b) Blank group of fluorescence imaging. (c) The relative fluorescence intensity of the Arabidopsis root. (d) The relative fluorescence intensity of zebrafish. Data are presented as mean ± SD (n = 3).

- Comparison of different methods for FSA determination

Table S10. Comparison of different methods for FSA determination.

| Methods | LOD | LOQ | Linear range | QY | Application | Portable detection | Fluorescent imaging | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| HPLC-DAD-MS/MS | 0.00935-0.0825 μM | No data | No data | No data | Water | No | No | [3] |
| MIPs | No data | No data | No data | No data | No | No | No | [4] |
| SLE/LTP-HPLC/DAD | 0.0166 μM | 0.05039 μM | 0.0570-0.615 μM | No data | Soil | No | No | [5] |
| LC-MS/MS | 4.10×10−5-2.85×10−4 μM | 0.023-0.046 μM | No data | No data | Agricultural products | No | No | [6] |
| Nanozyme sensor arrays | No data | No data | No data | No data | Soil | No | No | [7] |
| Colorimetric nanozyme array | 0.071 μM | No data | No data | No data | Water | No | No | [8] |
| Immunoassay | No data | No data | 4.38×10−3 - 1.78 μM | - | Soil | No | No | [9] |
| Immune sensor | 0.5 fM | No data | 0.5 fM - 500 pM | - | No | No | No | [10] |
| This work | 0.39 μM |  | 0 – 10 μM | 0.2564 | Soil, agricultural products | Yes | Yes |  |

References:

1. Laganà A, Fago G, Fasciani L, Marino A, Mosso M. Determination of diphenyl-ether herbicides and metabolites in natural waters using high-performance liquid chromatography with diode array tandem mass spectrometric detection. Anal Chim Acta. 2000;414(1):79-94.

2. Jin XY, Wang Y, Bai WY, Zhao D, Song XL, Xu XW. Synthesis and Characterization of Fomesafen Imprinted Polymers. Journal of Macromolecular Science. Part a, Pure Appl Chem. 2015;52(12):316-321.

3. Costa AIG, Queiroz MELR, Neves AA, de Assis RC, Soares CESD, Silva AAD, et al. Mobility and persistence of the herbicide fomesafen in soils cultivated with bean plants using SLE/LTP and HPLC/DAD. Environ Sci Pollut R. 2015;22(5):3457-3466.

4. Pang K, Hu JY. Simultaneous Analysis and Dietary Exposure Risk Assessment of Fomesafen,  Clomazone, Clethodim and Its Two Metabolites in Soybean Ecosystem. Int J Env Res Pub He. 2020;17(6):1951.

5. Zhu YY, Wu JJX, Han LJ, Wang XY, Li W, Guo HC, et al. Nanozyme Sensor Arrays Based on Heteroatom-Doped Graphene for Detecting Pesticides. Anal Chem. 2020;92(11):7444-7452.

6. Tai SM, Wang J, Sun FX, Pan QL, Peng CF, Wang ZP. A colorimetric sensor array based on nanoceria crosslinked and heteroatom-doped graphene oxide nanoribbons for the detection and discrimination of multiple pesticides. Anal Chim Acta. 2023;1283:341929.

7. Gao QQ, Chen L, An ZX, Wang YS, Yang DC, Wang ZZ, et al. Development of an immunoassay based on a specific antibody for the detection of diphenyl ether herbicide fomesafen. Sci Total Environ. 2024;914:169858.

8. Xu P, Zhao E. Fomesafen accurate detection by poly (3-hexylthiophene) transistor-based sensor. Journal of Materials Science: Materials in Electronics. 2023;34(36):2279.

9. Wang F, Nam S, Guo Z, Park S, Yoon J. A new rhodamine derivative bearing benzothiazole and thiocarbonyl moieties as a highly selective fluorescent and colorimetric chemodosimeter for Hg2+. Sensors and Actuators B: Chemical. 2012;161(1):948-953.

10. Zhang Y, Chen X, Shao J, Zhang J, Yuan Q, Miao J, et al. A Ratiometric Fluorescent Probe for Sensing HOCl Based on Coumarin-rhodamine Dyad. Chem Commun. 2014;50(91): 14241-14244.