<Supporting Information>

Improving Wound Healing Function and Storage Stability of Stem Cell-Derived Extracellular Vesicles via Lyophilized Hyaluronic Acid Formulation

Van Dat Bui 1,2†, Van Hieu Duong 1†, Dong Gil You 3†, Won Ho Jang 1, Jungmi Lee 1, Jae Yoon An 1, Seunglee Kwon 1,*, Jae Hyung Park 1,4,5,*

1 School of Chemical Engineering, College of Engineering, Sungkyunkwan University (SKKU), Suwon 16419, Republic of Korea

2 Vinmec Research Institute of Stem Cell and Gene Technology, College of Health Sciences, VinUniversity, Vinhomes Ocean Park, Gia Lam, Hanoi 1310, Vietnam

3 Department of Chemical Engineering and Biotechnology, Tech University of Korea, Siheung 15073, Republic of Korea

4 Department of Health Sciences and Technology, SAIHST, Sungkyunkwan University, Suwon 16419, Republic of Korea

5 Biomedical Institute for Convergence at SKKU (BICS), Sungkyunkwan University, Suwon 16419, Republic of Korea

†Van Dat Bui, Hieu Duong Van, and Dong Gil You contributed equally to this study.

* Corresponding author.

CONTACT: Prof. Jae Hyung Park (jhpark1@skku.edu), School of Chemical Engineering, College of Engineering, Sungkyunkwan University (SKKU), Suwon 16419, Republic of Korea

Western Blotting

To evaluate the expression of CD9 and CD44 in ADSC-EV, EV samples were concentrated using a 100 kDa Amicon Ultra-0.5 centrifugal filter unit (Merck, Rahway, NJ, USA), followed by lysis in RIPA buffer. Total protein concentration was quantified using a BCA assay. EV samples were separated by electrophoresis on 6% or 12% SDS-PAGE gels. CD44 (1:1000), CD9, and β-actin (1:1000, Cell Signalling Technology, Danvers, MA, USA) were used as primary antibodies, and HRP-conjugated anti-rabbit IgG and anti-mouse IgG (1:1000) were used as secondary antibodies. The membranes were investigated using ChemiDocTM imaging system (BIORAD Laboratories, CA, USA). The protein’s molecular weights were distinguished using a protein ladder (Precision Plus Protein Dual Color Standards; BIORAD Laboratories, CA, USA).

Cryo-EM

HA-EV and bare EV samples were applied onto freshly glow-discharged holey carbon electron microscopy grids (Lacey Carbon, 200 mesh, copper; Electron Microscopy Sciences, Hatfield, PA, USA). The grids were plunge-frozen using a Vitrobot Mark IV (Thermo Fisher Scientific, Waltham, MA, USA) operated at 4 °C and >95% relative humidity, with a blot force of 3 and a blot time of 4 s. Vitrified samples were subsequently imaged using a Krios Cryo-EM system (Thermo Fisher Scientific).

Single EV imaging

To verify HA deposition onto ADSC-derived EVs, the co-localization of HA and EVs was visualized using confocal laser scanning microscopy. To prepare fluorescently labeled HA, 10 mg of HA was dissolved in 5 mL of DIW with stirring for 30 min. Subsequently, 20 μL of Flamma® 675 dichlorotriazine (5 mg/mL in DMSO; BioAct, Incheon, South Korea) was added, and the reaction mixture was stirred at room temperature for 24 h in the dark. The resulting Flamma® 675-labeled HA was purified by dialysis against DIW using a 3.5 kDa molecular weight cutoff membrane for 3 days, followed by lyophilization. For single-EV co-localization analysis, 1 mL of DiO-labeled EVs (4 × 10⁹ particles/mL) was mixed with 1 mL of Flamma® 675-labeled HA (1 mg/mL) and incubated for 30 min at 25 °C. To evaluate CD44 specificity, EVs were pre-incubated with either an anti-CD44 antibody (3578, 1:1000 dilution, Cell Signaling Technology, Danvers, MA, USA) or an anti-CD9 antibody (13174, 1:1000 dilution, non-CD44 control, Cell Signaling Technology) for 12 h at 4 °C prior to incubation with Flamma® 675-labeled HA. Following incubation, 10 μL of each sample was placed onto a glass slide (Paul Marienfeld GmbH & Co. KG, Lauda-Königshofen, Germany), covered with a coverslip (Electron Microscopy Sciences, Hatfield, PA, USA), and sealed using nail polish. EVs were imaged using a confocal laser scanning microscope (TCS SP8 HyVolution, Leica Microsystems CMS GmbH, Germany).

Confocal Microscopy Imaging

To evaluate the lysosomal escape capability of HA-coated EVs, M1 macrophages or senescent dermal fibroblasts were seeded onto confocal dishes at a density of 1 × 10⁵ cells per dish. Cells were then co-incubated with Flamma® 675–labeled HA-EVs for 6 h. After incubation, cells were washed twice with DPBS and subsequently incubated with 0.1 μM LysoTracker™ Green DND-26 (Thermo Fisher Scientific, Waltham, MA, USA) for 1 h. Cells were then washed twice with DPBS, and nuclei were counterstained with Hoechst. Finally, cells were imaged using a confocal laser scanning microscope (TCS SP8 HyVolution, Leica Microsystems CMS GmbH, Germany).

Fig. S1 Characterization of fresh EV. A Size distribution and B TEM image of EVs. The scale bar represents 200 nm. C Western blotting of ADSCs and ADSC-derived EVs.

Fig S2 Cryo-EM images of bare EV and HA-EV.

Fig S3 Single–EV–level confocal microscopy analysis of HA binding to EVs.

Fig. S4 A Schematics for analyzing CD44-expressing cells. B Flow cytometry of CD44 expression on young HDF (yHDF), M1 macrophage, and senescent HDF (sHDF). C Quantification of CD44 expression from panel B.

Fig S5 Immunofluorescent staining of CD44 expression in the skin wound.

Fig S6 Distribution of CD44 (FITC, green) and EVs (Flamma® 675, red) in the skin of the wound healing mouse models. Cell nuclei were counterstained with DAPI (blue).

Fig. S7 Confocal microscopy images showing the intracellular localization of Flamma® 675–labeled HA-EVs in M1 macrophages and senescent dermal fibroblasts, co-stained with LysoTracker to visualize lysosomal compartments.

Fig. S8 Confocal microscope images of the wound sites. A For immunohistochemical analysis, the tissue sections were immuno-stained with F4/80 (red) and CD86 (green). B The wound tissues were immuno-stained p16INK4A (red) and ER-TR (green). DAPI (blue) was used as a nuclear counterstain.

Fig. S9 Immunohistochemical staining of wound sections on day 9 after treatments. A The tissue sections were immuno-stained with CD31 (red) and α-SMA (green). B The wound tissues were immuno-stained with CK19 (red) and ER-TR7 (green). DAPI (blue) was used as a nuclear counterstain.