pH-Responsive Chitosan–Mesoporous Organosilica Nanoplatform: Enhancement of Biocompatibility and Tumor Eradication for Precision Colorectal Cancer Chemotherapy

Juan Shao 1, 2, 3,†, Wenjing Li 4,†, Chuxin Zhang 2, 3,†, Jiaxing An 2, 3, Huimei Yu 5, Yitao Yan 6, Xu Li 2, 3, Wenbo Zhang 7, Yingying Wei 7, Weiwei Kang 4, Keming Yun 2, 3, Ruiping Zhang 1,*, Jie Zheng 2, 4, 5, 8,*, Zhongyuan Guo 2, 3, 4,*

1 The Fifth Clinical Medical College of Shanxi Medical University/Shanxi Provincial People's Hospital Affiliated to Shanxi Medical University, Taiyuan 030001, PR China.

2 School of Forensic Medicine, Shanxi Medical University, Jinzhong, 030600, PR China.

3 Shanxi Key Laboratory of Forensic Medicine, Jinzhong 030600, PR China.

4 Academy of Medical Sciences, Shanxi Medical University, Jinzhong, 030600, PR China.

5 School of Industry, Shanxi Medical University, Jinzhong, 030600, PR China.

6 The First Clinical Medical School, Shanxi Medical University, Taiyuan, 030001, PR China.

7 Shanxi Province Cancer Hospital/Shanxi Hospital Affiliated to Cancer Hospital, Chinese Academy of Medical Sciences/Cancer Hospital Affiliated to Shanxi Medical University, Taiyuan, 030001, PR China.

8 School of Nursing, Shanxi Medical University, Taiyuan, 030001, PR China.

† These authors contribute equally.

∗ Corresponding author.

Zhongyuan Guo, E-mail: guozhongyuan@sxmu.edu.cn

Address: 98 Daxue Street, School of Forensic Medicine, Shanxi Medical University, Jinzhong, Shanxi Province, People’s Republic of China

Jie Zheng, E-mail: zhengjie@sxmu.edu.cn

Ruiping Zhang, E-mail: zrp_7142@sxmu.edu.cn

Figure S1. Zeta potential of MOMs, CS-MOMs, DOX@MOMs, DOX@CS-MOMs and DOX. Data are presented as mean ± SD (n ≥ 3).

Figure S2. Biocompatibility evaluation of empty carriers. (a) Cell viability determined by CCK-8 assay and (b) LDH release levels after 24 h of treatment with MOMs and CS-MOMs. Data are presented as mean ± SD (n ≥ 3). Statistical significance relative to the Control group is indicated by ***p < 0.001 and ****p < 0.0001.

Figure S3. Quantitative analysis of intracellular superoxide fluorescence intensity visualized by DHE staining. Data are presented as mean ± SD (n ≥ 3). Statistical significance relative to the Control group is indicated by ***p < 0.001 and ****p < 0.0001.

Figure S4. Histological safety evaluation using special staining techniques. AB/PAS staining of liver and kidney tissues to assess mucin/glycogen integrity. Masson’s trichrome staining of kidney and spleen tissues to monitor collagen fiber changes. Oil Red O staining of liver tissues to visualize lipid accumulation. Nissl staining of brain tissues to examine neuronal structure and integrity. Scale bar = 100 μm.

Figure S5. Quantitative analysis results of organ function markers: liver function markers (ALT, DBIL, γ-GT), cardiac function markers (cTnT, cTnl), kidney function markers (BUN), pro-inflammatory cytokines (TNF-α), ALB, TC, LDH. Data are presented as mean ± SD (n ≥ 3). Statistical significance relative to the Control group is indicated by *p < 0.05, **p < 0.01, ***p < 0.001, and ****p < 0.0001.

Table S1. Textural parameters of MOMs and CS-MOMs

| Thermophysical | BET Surface Area | t-Plot Micropore Area | t-Plot External Surface Area | t-Plot micropore volume | Adsorption average pore width (4V/A by BET) |
| --- | --- | --- | --- | --- | --- |
| MOMs | 905.48 m2/g | 696.77 m2/g | 208.72 m2/g | 0.48 cm3/g | 2.98 nm |
| CS-MOMs | 855.38 m2/g | 733.50 m2/g | 121.89 m2/g | 0.46 cm3/g | 2.87 nm |

Table S2: Primer Sequences for RT-qPCR

| Species | Gene | Primer (5’-3’) |
| --- | --- | --- |
| Human | Occludin | Forward: AGAGTTGACAGTCCCATGGC Reverse: AGTCATCCACAGGCGAAGTT |
| Human | ZO-1 | Forward: TAGAAGATAGCCCTGCAGCC Reverse: GTCAAGCAGGAAAAGGACGG |
| Human | Bax | Forward: AGATCATGAAGACAGGGGCC Reverse: AGACACTCGCTCAGCTTCTT |
| Human | Bcl-2 | Forward: CGTGGAAAGCGTAGACAAGG Reverse: TGCTGCATTGTTCCCATAGAG |