Supplementary material

Figures

Figure S1. Levels of pro-inflammatory mediators in cell supernatants in vitro (adapted from [13]).

Figure S2. Levels of proteins, LDH (cytotoxicity) and intracellular ROS (oxidative stress) in BALF.

Figure S3. Examples of critical effect doses (CED) and dose intervals (CEDL/BMDL and CEDU/BMDU) determined using benchmark dose response modeling.

Figure S4. Size distribution of the NMs in water suspensions used to expose rats.

Figure S5. Initial lung burden in vivo assessed by ICP-MS 3h after instillation (n=2).

Tables

Table S1. Doses deposited in vitro in submerged conditions in function of nominal concentrations in suspensions (First published in [13] ).

Table S2. LOAELs (in µg/cm²) determined in vitro with the pro-inflammatory effects for each exposure method used (First published in [13]).

Table S3. Dose intervals (in µg/106 macrophages) determined for each NM and each methodology.

Table S4. Dose intervals normalized by primary surface areas (in cm²/106 macrophages) for each NM and each methodology.

Table S5. Dose intervals normalized by agglomerate surface areas (in cm²/106 macrophages) for each NM and methodology.

Table S6. Characterization of mass deposited in vitro on cells after 3h exposure at the ALI to aerosols of NMs (Adapted from [13]).

Tables of results

Table S7. Total number of cells in bronchoalveolar lavage fluids in vivo.

Table S8. Number of macrophages in bronchoalveolar lavage fluids in vivo.

Table S9. Number of neutrophils in bronchoalveolar lavage fluids in vivo.

Table S10. IL-1β secretion in bronchoalveolar lavage fluids in vivo.

Table S11. IL-6 secretion in bronchoalveolar lavage fluids in vivo.

Table S12. KC-GRO secretion in bronchoalveolar lavage fluids in vivo.

Table S13. TNF-α secretion in bronchoalveolar lavage fluids in vivo.

References

Figures

Figure S1. Levels of pro-inflammatory mediators in cell supernatants in vitro (adapted from [13]).

Figure S2. Levels of proteins, LDH (cytotoxicity) and intracellular ROS (oxidative stress) in BALF.

Figure S3. Examples of critical effect doses (CED) and dose intervals (CEDL and CEDU) determined using benchmark dose response modeling.

Figure S4. Size distribution of the NMs in water suspensions used to expose rats.

Figure S5. Initial lung burden in vivo assessed by ICP-MS 3h after instillation (n=2).

Tables

Table S1. Doses deposited in vitro in submerged conditions in function of nominal concentrations in suspensions (First published in [13]).

|  |  | 24h deposition in plates |  |  |  | 3h deposition in inserts |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| TiO2 NM105 | Nominal dose (µg/mL) | 10 | 50 | 100 | 200 | 54.5 | 163.5 | 544.9 |
|  | Nominal dose (µg/cm²) | 2.5 | 12.5 | 25 | 50 | 11.7 | 35.0 | 116.7 |
|  | Estimated dose using the ISDD model (µg/cm²) | 0.7 | 3.6 | 7.1 | 14.3 | 1 | 3 | 10 |
| TiO2 NM101 | Nominal dose (µg/mL) | 4 | 10 | 50 | 100 | 23.4 | 70.1 | 233.5 |
|  | Nominal dose (µg/cm²) | 1 | 2.5 | 12.5 | 25 | 5.0 | 15.0 | 50.0 |
|  | Estimated dose using the ISDD model (µg/cm²) | 1.0 | 2.5 | 12.5 | 25.0 | 1 | 3 | 10 |
| TiO2 NM100 | Nominal dose (µg/mL) | 4 | 10 | 50 | 100 | 34.3 | 102.9 | 343.1 |
|  | Nominal dose (µg/cm²) | 1 | 2.5 | 12.5 | 25 | 7.3 | 22.0 | 73.5 |
|  | Estimated dose using the ISDD model (µg/cm²) | 0.7 | 1.8 | 8.8 | 17.5 | 1 | 3 | 10 |
| CeO2 NM212 | Nominal dose (µg/mL) | 10 | 50 | 100 | 200 | 42.5 | 127.4 | 424.5 |
|  | Nominal dose (µg/cm²) | 2.5 | 12.5 | 25 | 50 | 9.1 | 27.3 | 90.9 |
|  | Estimated dose using the ISDD model (µg/cm²) | 0.9 | 4.7 | 9.5 | 18.9 | 1 | 3 | 10 |
| Tested doses about (µg/cm²) |  | 1 | 3 | 10 | 20 | 1 | 3 | 10 |

Table S2. LOAELs (in µg/cm²) determined in vitro with the pro-inflammatory effects for each exposure method used (First published in [13]).

|  | IL-1β |  |  | IL-6 |  |  | IL-8 |  |  | TNF-α |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | ALIa | Subm insertb | Subm platec | ALIa | Subm insertb | Subm platec | ALIa | Subm insertb | Subm platec | ALIa | Subm insertb | Subm platec |
| NM105 | 1 | 3 | 10 | 1 | 1 | 3 | 10 | 1 | 1 | 3 | 10 | 1 |
| NM101 | 1 | 10 | 10 | 1 | 1 | 10 | 10 | 1 | 1 | 10 | 10 | 1 |
| NM100 | Ø | Ø | Ø | 3 | Ø | Ø | Ø | 3 | Ø | Ø | Ø | 3 |
| NM212 | 3 | Ø | Ø | 3 | 3 | Ø | Ø | 3 | 3 | Ø | Ø | 3 |

aExposure at the air-liquid interface (ALI) in insert for 24h. Final deposited within 3h.

bExposure in submerged conditions in inserts for 24h. Final dose deposited within 3h.

cExposure in submerged conditions in plates. Final dose deposited within 24h.

Ø No effects measured at the tested doses

Table S3. Dose intervals (in µg/106 macrophages) determined for each NM and each methodology.

|  | Cytokines | NM105 |  |  | NM101 |  |  | NM100 |  |  | NM212 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Dose interval |  |  | Dose interval |  |  | Dose interval |  |  | Dose interval |  |  |
|  |  | BMDL | BMDU | Median | BMDL | BMDU | Median | BMDL | BMDU | Median | BMDL | BMDU | Median |
| In vitro, suspension (24h) | IL-1β | 3.83 | 475.94 | 185.23 - 447.98 | 21.19 | 114.01 | 112.93 - 254.43 | 427.32 | 1303.4 | 438.55 - 1047.6 | 2.5197 | 410.28 | 17.21 - 566.71 |
|  | IL-6 | 180.05 | 444.26 |  | 194.47 | 418.63 |  | ND | ND |  | ND | ND |  |
|  | IL-8 | ND | ND |  | ND | ND |  | ND | ND |  | ND | ND |  |
|  | TNF- α | 190.4 | 448.0 |  | 112.9 | 254.4 |  | 449.8 | 791.8 |  | 31.9 | 723.13 |  |
| In vitro, suspension (3h + 21h) | IL-1β | 7.22 | 37.63 | 4.30 - 25.20 | 10.085 | 110.38 | 13.37 - 103.42 | 57.994 | 888.95 | 57.99 - 929.20 | 57.99 | 915.3 | 56.21 - 876.70 |
|  | IL-6 | 3.38 | 22.65 |  | 21.43 | 136.47 |  | ND | ND |  | 38.48 | 839.14 |  |
|  | IL-8 | 1.86 | 18.58 |  | 14.041 | 62.361 |  | 55.996 | 969.44 |  | 57.181 | 161.06 |  |
|  | TNF- α | 5.2 | 27.8 |  | 12.7 | 96.5 |  | 63.9 | 883.0 |  | 55.23 | 914.25 |  |
| ALI (3h + 21h) | IL-1β | 0.85 | 13.36 | 1.01 - 13.64 | 1.02 | 12.41 | 1.64 - 13.43 | 0.092 | 15.14 | 0.75 - 15.05 | 10.47 | 43.57 | 14.69 - 45.28 |
|  | IL-6 | 0.61 | 13.53 |  | 1.48 | 12.86 |  | 0.195 | 14.647 |  | 14.69 | 45.28 |  |
|  | IL-8 | 1.31 | 13.78 |  | 18.89 | 198.27 |  | 1.30 | 14.96 |  | ND | ND |  |
|  | TNF- α | 1.17 | 13.75 |  | 1.81 | 14.00 |  | 3.96 | 16.12 |  | ND | ND |  |
| In vivo | IL-1β | 0.18 | 10.71 | 0.11 - 12.06 | ND | ND | 0.35 - 13.45 | ND | ND | ND | ND | ND | 0.00 - 11.85 |
|  | IL-6 | 0.11 | 22.26 |  | 0.71 | 13.77 |  | ND | ND |  | 0.00 | 3.10 |  |
|  | IL-8 | 0.03 | 13.40 |  | ND | ND |  | ND | ND |  | 0.52 | 13.07 |  |
|  | TNF- α | 0.12 | 1.46 |  | 0.00 | 13.14 |  | ND | ND |  | 0.00 | 11.85 |  |

BMDL: Benchmark Dose Lower confidence limit

BMDU: Benchmark Dose Upper confidence limit

Median: Median BMDL and BMDU values calculated by pooling the four cytokines, to have a dose-interval for a general pro-inflammatory response

Table S4. Dose intervals normalized by primary surface areas (in cm²/106 macrophages) for each NM and methodology.

|  | Cytokines | NM105 |  |  | NM101 |  |  | NM100 |  |  | NM212 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Dose interval |  |  | Dose interval |  |  | Dose interval |  |  | Dose interval |  |  |
|  |  | BMDL | BMDU | Median | BMDL | BMDU | Median | BMDL | BMDU | Median | BMDL | BMDU | Median |
| In vitro, suspension (24h) | IL-1β | 1.77 | 219.41 | 85.39 - 206.52 | 66.96 | 360.27 | 356.86 - 804.00 | 42.73 | 130.34 | 43.86 - 104.76 | 0.68 | 110.78 | 4.65 - 153.01 |
|  | IL-6 | 83.00 | 204.80 |  | 614.53 | 1322.87 |  | ND | ND |  | ND | ND |  |
|  | IL-8 | ND | ND |  | ND | ND |  | ND | ND |  | ND | ND |  |
|  | TNF- α | 87.77 | 206.53 |  | 356.76 | 803.90 |  | 44.98 | 79.18 |  | 8.61 | 195.25 |  |
| In vitro, suspension (3h + 21h) | IL-1β | 3.33 | 17.35 | 1.98 - 11.62 | 31.87 | 348.80 | 42.26 - 326.82 | 5.80 | 88.90 | 5.80 - 92.92 | 15.66 | 247.13 | 15.18 - 236.71 |
|  | IL-6 | 1.56 | 10.44 |  | 67.72 | 431.25 |  | ND | ND |  | 10.39 | 226.57 |  |
|  | IL-8 | 0.86 | 8.57 |  | 44.37 | 197.06 |  | 5.60 | 96.94 |  | 15.44 | 43.49 |  |
|  | TNF- α | 2.40 | 12.82 |  | 40.13 | 304.94 |  | 6.39 | 88.30 |  | 14.91 | 246.85 |  |
| ALI (3h + 21h) | IL-1β | 0.39 | 6.16 | 0.47 - 6.29 | 3.22 | 39.22 | 5.20 - 42.44 | 0.01 | 1.51 | 0.07 - 1.51 | 2.83 | 11.76 | 3.97 - 12.23 |
|  | IL-6 | 0.28 | 6.24 |  | 4.68 | 40.64 |  | 0.02 | 1.46 |  | 3.97 | 12.23 |  |
|  | IL-8 | 0.60 | 6.35 |  | 59.69 | 626.53 |  | 0.13 | 1.50 |  | ND | ND |  |
|  | TNF- α | 0.54 | 6.34 |  | 5.72 | 44.24 |  | 0.40 | 1.61 |  | ND | ND |  |
| In vivo | IL-1β | 0.08 | 4.94 | 0.05 - 5.56 | ND | ND | 1.12 - 42.51 | ND | ND | ND | ND | ND | 0.00 - 3.20 |
|  | IL-6 | 0.05 | 10.26 |  | 2.24 | 43.51 |  | ND | ND |  | 0.00 | 0.84 |  |
|  | IL-8 | 0.01 | 6.18 |  | ND | ND |  | ND | ND |  | 0.14 | 3.53 |  |
|  | TNF- α | 0.06 | 0.67 |  | 0.00 | 41.52 |  | ND | ND |  | 0.00 | 3.20 |  |

BMDL: Benchmark Dose Lower confidence limit

BMDU: Benchmark Dose Upper confidence limit

Median: Median BMDL and BMDU values calculated by pooling the four cytokines, to have a dose-interval for a general pro-inflammatory response

Table S5. Dose intervals normalized by agglomerate surface areas (in cm²/106 macrophages) for each NM and methodology.

|  | Cytokines | NM105 |  |  | NM101 |  |  | NM100 |  |  | NM212 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Dose interval |  |  | Dose interval |  |  | Dose interval |  |  | Dose interval |  |  |
|  |  | BMDL | BMDU | Median | BMDL | BMDU | Median | BMDL | BMDU | Median | BMDL | BMDU | Median |
| In vitro, suspension (24h) | IL-1β | 0.52 | 64.44 | 25.08 - 60.65 | 1.43 | 7.69 | 7.62 - 17.16 | 50.36 | 153.62 | 51.69 - 123.47 | 0.32 | 51.40 | 2.16 - 70.99 |
|  | IL-6 | 24.38 | 60.15 |  | 13.12 | 28.23 |  | ND | ND |  | ND | ND |  |
|  | IL-8 | ND | ND |  | ND | ND |  | ND | ND |  | ND | ND |  |
|  | TNF- α | 25.78 | 60.65 |  | 7.61 | 17.16 |  | 53.01 | 93.32 |  | 4.00 | 90.59 |  |
| In vitro, suspension (3h + 21h) | IL-1β | 0.98 | 5.09 | 0.58 - 3.41 | 0.68 | 7.44 | 0.90 - 6.97 | 6.84 | 104.77 | 6.84 - 109.51 | 7.26 | 114.66 | 7.04 - 109.82 |
|  | IL-6 | 0.46 | 3.07 |  | 1.45 | 9.20 |  | ND | ND |  | 4.82 | 105.12 |  |
|  | IL-8 | 0.25 | 2.52 |  | 0.95 | 4.21 |  | 6.60 | 114.26 |  | 7.16 | 20.18 |  |
|  | TNF- α | 0.70 | 3.76 |  | 0.86 | 6.51 |  | 7.53 | 104.07 |  | 6.92 | 114.53 |  |
| ALI (3h + 21h) | IL-1β | 0.30 | 4.77 | 0.36 - 4.87 | 0.85 | 10.34 | 1.37 - 11.19 | 0.03 | 4.73 | 0.23 - 4.70 | 2.86 | 11.88 | 4.01 - 12.35 |
|  | IL-6 | 0.22 | 4.83 |  | 1.23 | 10.72 |  | 0.06 | 4.58 |  | 4.01 | 12.35 |  |
|  | IL-8 | 0.47 | 4.92 |  | 15.74 | 165.23 |  | 0.41 | 4.68 |  | ND | ND |  |
|  | TNF- α | 0.42 | 4.91 |  | 1.51 | 11.67 |  | 1.24 | 5.04 |  | ND | ND |  |
| In vivo | IL-1β | 0.02 | 1.45 | 0.02 - 1.63 | ND | ND | 0.02 - 0.91 | ND | ND | ND | ND | ND | 0.00 - 1.48 |
|  | IL-6 | 0.01 | 3.01 |  | 0.05 | 0.93 |  | ND | ND |  | 0.00 | 0.39 |  |
|  | IL-8 | 0.00 | 1.81 |  | ND | ND |  | ND | ND |  | 0.07 | 1.64 |  |
|  | TNF- α | 0.02 | 0.20 |  | 0.00 | 0.89 |  | ND | ND |  | 0.00 | 1.48 |  |

Table S6. Characterization of mass deposited in vitro on cells after 3h exposure at the ALI to aerosols of NMs (Adapted from [13]).

| # Nebulizer (PALAS, AGK 2000) | ##### TiO2 NM105 |  |  | TiO2 NM101 |  |  |  | TiO2 NM100 |  |  | CeO2 NM212 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Suspension concentration (g/L) | 1 | 5 | 10 |  | 1 | 5 | 10 | 1 | 5 | 10 | 1 | 5 | 10 |  |
| Deposited massd(µg/cm2 in 3h) (n=4-7) (ICP-MS) | 0.06± 0.01 | 0.66± 0.12 | 2.68 ± 0.6 |  | 0.22 ± 0.03 | 1.51 ± 0.11 | 3.15 ± 0.44 | 0.11 ± 0.01 | 0.50 ± 0.12 | 2.85 ± 0.30 | 0.22 ± 0.02 | 1.54 ± 0.08 | 3.26 ± 0.68 |  |

Tables of results

Table S7. Total number of cells in bronchoalveolar lavage fluids in vivo.

| Total cells (x 106) | NM105 |  |  | NM101 |  |  | NM100 |  |  | NM212 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Dose (µg) | Mean | SD | n | Mean | SD | n | Mean | SD | n | Mean | SD | n |
| 0 | 8,116667 | 2,469143 | 6 | 8,320 | 1,104681 | 6 | 8,320 | 1,104681 | 6 | 6,758333 | 0,8873649 | 6 |
| 5 | 11,94167 | 7,829394 | 6 | 7,606667 | 1,515449 | 6 | 7,041667 | 1,81863 | 6 | 7,378333 | 2,405497 | 6 |
| 50 | 10,125 | 3,014424 | 6 | 8,580 | 2,256333 | 6 | 9,500 | 3,018609 | 6 | 7,758334 | 1,546744 | 6 |
| 500 | 13,40833 | 7,89116 | 6 | 6,480 | 1,718232 | 6 | 8,866667 | 2,73636 | 6 | 6,595 | 1,546205 | 6 |

Table S8. Number of macrophages in bronchoalveolar lavage fluids in vivo.

| Macrophages (x 106) | NM105 |  |  | NM101 |  |  | NM100 |  |  | NM212 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Dose (µg) | Mean | SD | n | Mean | SD | n | Mean | SD | n | Mean | SD | n |
| 0 | 7,906667 | 2,405815 | 6 | 8,088333 | 1,261942 | 6 | 8,088333 | 1,261942 | 6 | 6,400 | 0,7920605 | 6 |
| 5 | 11,80167 | 7,818852 | 6 | 6,755 | 1,747624 | 6 | 7,083333 | 1,690535 | 6 | 7,245 | 2,231123 | 6 |
| 50 | 9,778334 | 2,919284 | 6 | 9,286667 | 3,087139 | 6 | 8,116667 | 2,073438 | 6 | 7,330 | 1,470687 | 6 |
| 500 | 12,45333 | 7,389264 | 6 | 8,585 | 2,852155 | 6 | 5,630 | 1,935407 | 6 | 5,946667 | 1,534675 | 6 |

Table S9. Number of neutrophils in bronchoalveolar lavage fluids in vivo.

| Neutrophils (x 106) | NM105 |  |  | NM101 |  |  | NM100 |  |  | NM212 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Dose (µg) | Mean | SD | n | Mean | SD | n | Mean | SD | n | Mean | SD | n |
| 0 | 2,533333 | 1,834848 | 6 | 0,650 | 0,5504543 | 6 | 0,650 | 0,5504543 | 6 | 5,000 | 6,131884 | 6 |
| 5 | 1,383333 | 1,937438 | 6 | 6,950 | 7,524294 | 6 | 3,550 | 3,894997 | 6 | 1,333333 | 2,160247 | 6 |
| 50 | 3,100 | 2,565151 | 6 | 4,850 | 3,924666 | 6 | 2,250 | 3,318283 | 6 | 5,166667 | 2,316607 | 6 |
| 500 | 6,766666 | 3,631896 | 6 | 13,33333 | 12,72143 | 6 | 3,633333 | 2,063654 | 6 | 9,833333 | 4,833908 | 6 |

Table S10. IL-1β secretion in bronchoalveolar lavage fluids in vivo.

| IL-1β (pg/mL) | NM105 |  |  | NM101 |  |  | NM100 |  |  | NM212 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Dose (µg) | Mean | SD | n | Mean | SD | n | Mean | SD | n | Mean | SD | n |
| 0 | 8,884489 | 1,849256 | 6 | 9,138938 | 4,634266 | 6 | 9,138938 | 4,634266 | 6 | 5,91275 | 2,010868 | 6 |
| 5 | 8,277813 | 2,307245 | 6 | 11,53626 | 5,389348 | 6 | 10,98688 | 6,011103 | 6 | 9,572947 | 4,58724 | 6 |
| 50 | 10,45812 | 2,844312 | 6 | 9,932984 | 3,694911 | 6 | 6,774626 | 2,236386 | 6 | 6,11853 | 0,7779508 | 6 |
| 500 | 11,85874 | 2,137961 | 6 | 13,254 | 11,96707 | 6 | 6,882884 | 2,226868 | 6 | 9,275265 | 2,540267 | 6 |

Table S11. IL-6 secretion in bronchoalveolar lavage fluids in vivo.

| IL-6 (pg/mL) | NM105 |  |  | NM101 |  |  | NM100 |  |  | NM212 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Dose (µg) | Mean | SD | n | Mean | SD | n | Mean | SD | n | Mean | SD | n |
| 0 | 641,9868 | 1090,115 | 6 | 201,9327 | 409,2815 | 6 | 201,9327 | 409,2815 | 6 | 247,1255 | 251,5747 | 6 |
| 5 | 83,94656 | 123,9007 | 6 | 1561,140 | 2454,902 | 6 | 1728,992 | 2213,854 | 6 | 646,437 | 1215,112 | 6 |
| 50 | 299,6054 | 373,0139 | 6 | 102,3409 | 130,1647 | 6 | 247,705 | 340,396 | 6 | 575,3152 | 452,0587 | 6 |
| 500 | 494,0656 | 372,196 | 6 | 2547,297 | 5762,785 | 6 | 124,1872 | 177,432 | 6 | 2057,351 | 1911,255 | 6 |

Table S12. KC-GRO secretion in bronchoalveolar lavage fluids in vivo.

| KC-GRO (pg/mL) | NM105 |  |  | NM101 |  |  | NM100 |  |  | NM212 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Dose (µg) | Mean | SD | n | Mean | SD | n | Mean | SD | n | Mean | SD | n |
| 0 | 154,921 | 130,2589 | 6 | 436,0563 | 849,0498 | 6 | 436,0563 | 849,0498 | 6 | 612,267 | 769,132 | 6 |
| 5 | 117,6946 | 33,43017 | 6 | 505,3957 | 611,5626 | 6 | 525,504 | 449,3068 | 6 | 245,1932 | 185,7892 | 6 |
| 50 | 357,3673 | 484,7474 | 6 | 101,2313 | 68,70238 | 6 | 238,2058 | 235,6528 | 6 | 255,8444 | 96,38566 | 6 |
| 500 | 514,3612 | 597,0824 | 6 | 584,2678 | 709,4099 | 6 | 259,6591 | 309,2401 | 6 | 1358,297 | 933,4235 | 6 |

Table S13. TNF-α secretion in bronchoalveolar lavage fluids in vivo.

| TNF-α (pg/mL) | NM105 |  |  | NM101 |  |  | NM100 |  |  | NM212 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Dose (µg) | Mean | SD | n | Mean | SD | n | Mean | SD | n | Mean | SD | n |
| 0 | 1,704346 | 0,8449346 | 6 | 1,903974 | 2,234239 | 6 | 1,903974 | 2,234239 | 6 | 2,425805 | 1,646873 | 6 |
| 5 | 1,420876 | 0,4093659 | 6 | 2,528478 | 2,363132 | 6 | 2,463016 | 1,448268 | 6 | 3,038258 | 2,296852 | 6 |
| 50 | 2,914879 | 0,9622893 | 6 | 2,734777 | 2,081956 | 6 | 1,390201 | 0,7100273 | 6 | 5,076797 | 5,844111 | 6 |
| 500 | 6,758596 | 2,074849 | 6 | 6,386044 | 4,192086 | 6 | 1,478584 | 0,8414167 | 6 | 8,041635 | 3,607172 | 6 |

Reference

13.	Loret T, Peyret E, Dubreuil M, Aguerre-Chariol O, Bressot C, le Bihan O, et al. Air-liquid interface exposure to aerosols of poorly soluble nanomaterials induces different biological activation levels compared to exposure to suspensions. Part Fibre Toxicol. 2016;13(1):58.