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Table S1. Overview table of results from TEM analysis.
	Sample
	Images Analyzed, #
	Area Analyzed, µm2
	Particles Analyzed, #
	Mean agglomerate size, nm
	Primary particle size, nm a
	Lattice spacing, Å

	Al2O3
	4
	71.8
	7920
	15 ± 9
	5.5 ± 5.5
	-

	CuO
	6
	2932
	8239
	42 ± 25
	7.8 ± 6.8
	2.7 ± 0.1

	SnO2
	6
	57
	3438
	13 ± 9
	4.5 ± 2.3
	3.4 ± 0.1

	TiO2
	3
	10
	46
	21 ± 16
	6.6 ± 4.1
	3.5 ± 0.1

	ZnO
	5
	58
	697
	27 ± 15
	5.7 ± 3.8
	3.4 ± 0.1


[bookmark: _GoBack]Note: aPrimary particle size was measured for at least 15 different primary particles. Uncertainties are shown as the standard deviation of the measured quantities.
