Additional information 3

Table S1. Overview table of results from TEM analysis.

| Sample | Images Analyzed, # | Area Analyzed, µm2 | Particles Analyzed, # | Mean agglomerate size, nm | Primary particle size, nm a | Lattice spacing, Å |
| --- | --- | --- | --- | --- | --- | --- |
| Al2O3 | 4 | 71.8 | 7920 | 15 ± 9 | 5.5 ± 5.5 | - |
| CuO | 6 | 2932 | 8239 | 42 ± 25 | 7.8 ± 6.8 | 2.7 ± 0.1 |
| SnO2 | 6 | 57 | 3438 | 13 ± 9 | 4.5 ± 2.3 | 3.4 ± 0.1 |
| TiO2 | 3 | 10 | 46 | 21 ± 16 | 6.6 ± 4.1 | 3.5 ± 0.1 |
| ZnO | 5 | 58 | 697 | 27 ± 15 | 5.7 ± 3.8 | 3.4 ± 0.1 |

Note: aPrimary particle size was measured for at least 15 different primary particles. Uncertainties are shown as the standard deviation of the measured quantities.