Supplementary table 1 Particle size distribution of the test materials in the final preliminary test batch

|  |  | Material class 1 | Material class 2 | Material class 3 | Material class 4 | Material class 5 | Positive control |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | SWCNT | MWCNT | MWCNT | MWCNT | Carbon fiber fragment | Asbestos |
|  |  | OCSiAl Tuball | Nanocyl NC-7000 | IFW CNT1_1 | USRN 20-30 nm | Mitsubishi Dialed K13D2U | Long Amosite |
| Dispersion | Ultrasound duration [min] | 2 x 5 | 1 | 1 | 2 | 18 h magnetic stirrer, US bath 15 min, 2 min US tip (100 %) | 2 x 5 |
|  | Ultrasound amplitude [%] | 100 | 100 | 30 (short 100) | 30 (short 100) |  | 100 |
| Concentration | Number FWHO/mg material | 107.9 x 109 | 14.4 x 109 | 3.1 x 109 | 1.5 x 109 | 0.032 x 109* | 0.155 x 109 |
| Relative percentage | FWHO | 6.3% | 3.6% | 3.92% | 1.7% | 26.7%* | 59.5% |
|  | 3.5 ≤ L ≤ 5 µm | 6.8% | 0.8% | 3.61% | 0.0% | 17.8% | 11.3% |
|  | < 3.5 µm | 86.9% | 93.6% | 88.20% | 97.1% | 17.5% | 28.1% |
|  | L/D < 3 (Agglom./Part.) | 0.0% | 1.2% | 4.27% | 1.2% | 36.1% | 1.0% |
| PSD FWHO | GML (µm) | 6.72 | 6.41 | 7.35 | 6.85 | 7.26 | 12.63 |
|  | SD | 1.26 | 1.22 | 1.38 | 1.30 | 1.30 | 1.98 |
|  | GMD (µm) | 0.007 | 0.011 | 0.020 | 0.030 | 1.20 | 0.37 |
|  | SD | 1.594 | 1.566 | 1.489 | 1.57 | 1.547 | 1.71 |
| PSD Fibers 3.5 < L < 5 µm | GML (µm) | 3.99 | 4.40 | 4.04 | 0 | 4.32 | 4.16 |
|  | SD | 1.06 | 1.00 | 1.11 | 0 | 1.12 | 1.11 |
|  | GMD (µm) | 0.013 | 0.020 | 0.024 | 0 | 0.834 | 0.27 |
|  | SD | 1.386 | 1.000 | 1.185 | 0 | 1.358 | 1.71 |
| PSD L/D > 3 (all fibers) | GML (µm) | 1.70 | 0.94 | 1.46 | 1.14 | 4.81 | 6.72 |
|  | SD | 1.92 | 2.22 | 1.90 | 1.72 | 1.66 | 2.64 |
|  | GMD (µm) | 0.007 | 0.010 | 0.020 | 0.022 | 0.864 | 0.31 |
|  | Std | 1.696 | 1.574 | 1.469 | 1.450 | 1.824 | 1.79 |

* Note: Material contains also fibers longer than 5 µm and with a diameter ≥3 µm to a minor extent. The value of 0.035 x 109 fibers was initially used to calculate weight in the suspensions prepared for the study. The values in this table (e.g. 0.032 x 109 WHO fibers or a percentage of 26.7%) are the corrected values.

FWHO refers to WHO-analog nanofibers in the case of CNTs and to WHO fibers in the case of carbon fibers and the positive control.

Short means few sections.
US: ultrasound; Agglom: agglomerates; Part.: particles; L: length, D: diameter; PSD: particle size distribution; GML: geometric length; GMD: geometric diameter; SD: standard deviation.