# SUPPLEMENTARY INFORMATION

# Novel diaminoguanidine functionalized cellulose: synthesis, characterization, adsorption characteristics and application for ICP-AES determination of copper(II), mercury(II), lead(II) and cadmium(II) from aqueous solutions

Magda A Akl1*, Mohammed A Hashem1, Mohammed A Ismail1 and Dina A Abdelgalil1

1Department 	of Chemistry, Faculty of Science, Mansoura University, Mansoura 35516, Egypt

*To whom all correspondence should be addressed: Prof Magda Akl

e. mail: magdaakl@yahoo.com

(a)Native cellulose

(b)DAC

(c) DiGu.MC

(d) DiGu.MC-Cu(II)

Fig. S1. FTIR of (a)Native cellulose, (b)DAC, (c) DiGu.MC     (d) DiGu.MC-Cu(II)

Fig. S2 TGA curves of (a) DiGu-MC, (b) Cu-DiGu-MC, (c) Hg-DiGu-MC, (d) Pb-DiGu-MC

(e) Cd-DiGu-MC.

Fig. S3. Effect of initial concentration on adsorption of heavy metals by DiGu-MC

Table S1: Specific Surface areas of native cellulose and DiGu-MC fibers.

| Samples | BET surface area (m2 g−1) |
| --- | --- |
| Native ellulose | 10.400 |
| DiGu.MC | 3.4028 |