Supplementary material

A novel hybrid approach for predicting and optimizing the adsorption of methyl orange and Cr(VI) removal from aqueous solutions using fungal-cross linked chitosan integrated into graphene oxide as a cost-effective adsorbent

Mohammed T.M. H.Hamad

Central Laboratory for Environmental Quality Monitoring, National Water Research Center, Egypt

Corresponding author:

Mohammed T.M.H.Hamad

e-mail: mohamed_taha@nwrc.gov.eg

Contents

Fig. S1 Phylogenetic tree of the fungal isolate Trichoderma sp

Fig.S2.  FTIR spectra of (a)Cs; (b) GO @Cs-GLA-TiO2 composite; (c) TiO2; (d) GO @Cs-GLA-TiO2 composite after dye (e ) MO and(f) Cr(VI).

Fig. S3. (a-b-c-d) the XRD images of GO, TiO2,CS, and GO @Cs-GLA-TiO2 composite

Fig.S4 (a)The actual vs predicted removal percentage, (b) The normal probability vs the plot of the studentized residuals, (c),(d) The cook’s distance for each of the experimental runs, Box–Cox plot (e,f) each of the variables for the removal of MO and Cr(VI) adsorption on GO@Cs-GLA-TiO2.

Fig.S5 (a)The actual vs predicted removal percentage, (b) The normal probability vs the plot of the studentized residuals, (c),(d) The cook’s distance for each of the experimental runs, each of the variables for the removal of MO adsorption on fungal@Cs-GLA-GO.

Fig. S6 Response surface graph for the removal of MO (%) by biosorbent with interactions between(a) temperature and dosage, (b) pH and dosage, and (c) initial concentration of MO (d) pH and temperature, and(e) initial concentration of MO  and temperature, and (fl) pH and initial concentration of MO, and (m) desirability ramps for numerical optimization of four independent variable.

Fig. S7. RSM-ANN model: (a) Linear regression for the ANN-MO model training, verification, testing, and combined input data sets, (b) error histogram, and (c) MSE plot for training, validation, testing, and all data and(d) The percentage of the prediction error of the MO-ANN model.

Fig. S8  Time of  the  lag     phase (t0)  versus  the  initial  MO  concentration  (a), and (b) (S0) maximum specific growth rate μm versus the time of the lag phase t0 for S0 below

Fig. S9 Experimental and predicted  speciﬁc  substrate  consumption  rates  at  diﬀerent  MO concentrations  due to  diﬀerent  models.

Table S1(a) Coded levels and design range of variables.

Table S2. Characterization methods and analyzed properties

Table S3  Kinetic models and their linearized expressions in the adsorption of MO/Cr(VI)by GO@Cs-GLA-TiO2.

Table S4   Isotherm models and their linearized expressions in the adsorption of MO and Cr(VI) onto GO@Cs-GLA-TiO2 adsorbent.

Table S5(a) Coded levels and design range of variables.

Table S5 (b)The ANOVA results for the response surface model for the removal of MO dye.

Table S5c Box–Behnken design-based experimental conditions and results for MO adsorption activity of composites fungal @fungal@Cs-GLA-GO.

Table S6 Various kinetic models for effect of substrate on growth rate.

Table S7 Comparative study for different biomass based adsorbents applied for methyl orange adsorption.

Table S8 Cost analysis of materials used for adsorption using GO @Cs-GLA-TiO2.

Fig. S1 Phylogenetic tree of the fungal isolate Trichoderma sp

a

a

b

b

c

c

d

d

e

e

f

f

Fig.S2.  FTIR spectra of (a)Cs; (b) GO @Cs-GLA-TiO2 composite; (c) TiO2; (d) GO @Cs-GLA-TiO2 composite after dye (e ) MO and(f) Cr(VI).

a

a

Intensity(a.u.)

Intensity(a.u.)

2θ (degree)

2θ (degree)

Intensity(a.u.)

Intensity(a.u.)

b

b

2θ (degree)

2θ (degree)

Intensity(a.u.)

Intensity(a.u.)

c

c

2θ (degree)

2θ (degree)

d

d

Intensity(a.u.)

Intensity(a.u.)

2θ (degree)

2θ (degree)

Fig. S3. (a-b-c-d) the XRD images of GO, TiO2,CS, and GO @Cs-GLA-TiO2 composite.

b

b

a

a

d

d

c

c

c

c

e

e

f

f

Fig.S4(a)The actual vs predicted removal percentage, (b) The normal probability vs the plot of the studentized residuals, (c),(d) The cook’s distance for each of the experimental runs, Box–Cox plot (e,f) each of the variables for the removal of MO and Cr(VI) adsorption on GO@Cs--GLA-TiO2.

b

b

a

a

c

c

Fig.S5 (a)The actual vs predicted removal percentage, (b) The normal probability vs the plot of the studentized residuals, (c),(d) The cook’s distance for each of the experimental runs, each of the variables for the removal of MO adsorption on fungal@Cs-GLA-GO.

Removal %

Removal %

Removal %

Removal %

b

b

a

a

Contact Time

Contact Time

Temperature

Temperature

pH

pH

Contact Time

Contact Time

Removal %

Removal %

Removal %

Removal %

d

d

c

c

Temperature

Temperature

Initial concentration

Initial concentration

pH

pH

Contact Time

Contact Time

Removal %

Removal %

Removal %

Removal %

f

f

Temperature

Temperature

e

e

Initial concentration

Initial concentration

Initial concentration

Initial concentration

pH

pH

Fig. S6 Response surface graph for the removal of MO (%) by biosorbent with interactions between(a) temperature and dosage, (b) pH and dosage, and (c) initial concentration of MO (d) pH and temperature, and(e) initial concentration of MO  and temperature, and (fl) pH and initial concentration of MO, and (m) desirability ramps for numerical optimization of four independent variable.

a

a

b

b

c

c

d

d

Fig. S7. RSM-ANN model: (a) Linear regression for the ANN-MO model training, verification, testing and combined input data sets, (b) error histogram, and (c) MSE plot for training, validation, testing, and all data and(d) The percentage of the prediction error of the MO-ANN model.

a

a

b

b

Fig. S8  Time of  the  lag     phase (t0)  versus  the  initial  MO  concentration  (a), and (b) (S0) maximum specific growth rate μm versus the time of the lag phase t0 for S0 below

a

a

b

b

c

c

d

d

e

e

Fig. S9 Experimental  and  predicted  speciﬁc  substrate  consumption  rates  at  diﬀerent  MO concentrations  due to  diﬀerent  models.

Table S1 Coded levels and design range of variables.

| Factor | Code | -1 | 0 | 1 |
| --- | --- | --- | --- | --- |
| Adsorbent dose(g) | A | 0.4 | 0.6 | 0.8 |
| Contact time(min) | B | 40 | 60 | 80 |
| pH | C | 2 | 3 | 4 |
| Initial concentration (MO/Cr(VI)) (mgL-1) | D | 10 | 15 | 20 |

Table S2. Characterization methods and analyzed properties

| Method | Properties to be Analyzed |
| --- | --- |
| SEM Particle shape, size and morphology. EDX | Energy-dispersive X-ray spectroscopy (EDX) was performed for the semi-quantitative test of the prepared catalysts using scanning electron microscope coupled with EDX unit (Quanta FEG250, FEI Company |
| XRD Extent of Crystallization of the sample. | X-ray diffraction (XRD) analysis was performed on X-ray diffractometer (PANalytical X’Pert Pro, United Kingdom. |
| FT-IR | The Fourier- transformed infrared (FTIR) spectra of the synthesized catalysts were obtained using Bruker-VERTEX 80V to identify the surface functional groups at ambient conditions within the wavelength range from 400 to 4000 cm−1. |

| Kinetic models | Linear expression | Plot | Parameters |
| --- | --- | --- | --- |
| Pseudo-first order | ln(qe − qt) =lnqe − k1pt eq.4 | ln(qe − qt) vs.t | qe = exp(intercept), k1p = −(slope) |
| Pseudo-second Order | t/qt = 1/k2pqe2 + t/qe eq.5 | t/qt vs. t | qe= slope−1, k2p = (slope2)/intercept |
| Intraparticle diffusion | qt = Kpt1∕2 eq.6 | qt vs t1/2 | kiP = slop C =intercept |
| Elovich | qt=1βln(αβ) +1βln(t)eq.(7) | qt vs t |  |

Table S3  Kinetic models and their linearized expressions in the adsorption of MO/Cr(VI)by GO@Cs-GLA-TiO2.

Table S4   Isotherm models and their linearized expressions in the adsorption of MO and Cr(VI) onto GO@Cs-GLA-TiO2 adsorbent.

| Isotherms | Equations | Linear expression | Description | Plot | Parameters |
| --- | --- | --- | --- | --- | --- |
| Langmuir | qe=(qmKLCe)/(1 +KLCe) eq.3 RL=11+KLC° eq.(8) | Ce/qe = (1/KLqm) + (Ce/qm) | qmax (mg/ g) = maximum adsorption capacity. KL (L/mg) = constant of Langmuir (free energy of adsorption) | (Ce/qe) vs. Ce | qm= (slope)−1 KL= slope/intercept |
| Freundlich | qe=KF(Ce)1/n eq.9 | lnqe=lnKF+1nlnCe | KF (mL/g) = constants of Freundlich (the adsorption volume of the adsorbent) 1/n = constants (intensity of the analytes’ sorption) | ln qe vs. ln Ce | KF= exp(intercept), n = (slope)−1 |
| Temkin | qe=qm ln(KTCe) eq. 10 | qe=qm ln KT + qm ln Ce | ΔQ = variation of adsorption energy (ΔH) K0 = constant of Temkin. T = temperature (K) R (8.314 J/mol) K = universal gas constant. | qe vs. ln Ce | qm= slope KT= exp(intercept/slope |
|  | qe =KRp Ce/ 1+αRP (Ce β ) | ln KRP/ qe −1 = βln (Ce)+ln( α RP) |  |  |  |

| Factor | Code | -1 | 0 | 1 |
| --- | --- | --- | --- | --- |
| pH | A | 5 | 7 | 9 |
| Temperature(OC) | B | 20 | 30 | 40 |
| Contact time(day) | C | 3 | 6 | 9 |
| Initial concentration (mgL-1) | D | 10 | 30 | 50 |

Table S5(a) Coded levels and design range of variables.

Table S5 (b)The ANOVA results for the response surface model for the removal of MO dye.

| Source | Sum of Squares | df | Mean Square | F-value | p-value |  |
| --- | --- | --- | --- | --- | --- | --- |
| Model | 3701.07 | 14 | 264.36 | 169.60 | < 0.0001 | significant |
| A-A | 418.90 | 1 | 418.90 | 268.74 | < 0.0001 |  |
| B-B | 7.10 | 1 | 7.10 | 4.55 | 0.0510 |  |
| C-C | 3.63 | 1 | 3.63 | 2.33 | 0.1493 |  |
| D-D | 296.71 | 1 | 296.71 | 190.35 | < 0.0001 |  |
| AB | 101.00 | 1 | 101.00 | 64.80 | < 0.0001 |  |
| AC | 44.89 | 1 | 44.89 | 28.80 | < 0.0001 |  |
| AD | 51.84 | 1 | 51.84 | 33.26 | < 0.0001 |  |
| BC | 19.36 | 1 | 19.36 | 12.42 | 0.0034 |  |
| BD | 4.69 | 1 | 4.69 | 3.01 | 0.1049 |  |
| CD | 9.00 | 1 | 9.00 | 5.77 | 0.0307 |  |
| A² | 164.52 | 1 | 164.52 | 105.55 | < 0.0001 |  |
| B² | 598.11 | 1 | 598.11 | 383.70 | < 0.0001 |  |
| C² | 2497.89 | 1 | 2497.89 | 1602.46 | < 0.0001 |  |
| D² | 232.74 | 1 | 232.74 | 149.31 | < 0.0001 |  |
| Residual | 21.82 | 14 | 1.56 |  |  |  |
| Lack of Fit | 17.00 | 10 | 1.70 | 1.41 | 0.3958 | not significant |
| Pure Error | 4.82 | 4 | 1.21 |  |  |  |
| Cor Total | 3722.90 | 28 |  |  |  |  |

Table S5c Box–Behnken design-based experimental conditions and results for MO adsorption activity of composites fungal@Cs-GLA-GO.

|  | Factor 1 | Factor 2 | Factor 3 | Factor 4 | Response 1 |
| --- | --- | --- | --- | --- | --- |
| Run | A:A | B:B | C:C | D:D | R1 |
| 1 | 0 | 0 | 1 | 1 | 64 |
| 2 | 0 | -1 | 1 | 0 | 64.1 |
| 3 | 0 | 0 | -1 | 1 | 65 |
| 4 | 0 | 1 | -1 | 0 | 62 |
| 5 | -1 | 0 | -1 | 0 | 60 |
| 6 | 0 | -1 | -1 | 0 | 66.9 |
| 7 | -1 | 0 | 1 | 0 | 66.4 |
| 8 | 0 | 1 | 1 | 0 | 68 |
| 9 | 1 | 0 | 1 | 0 | 72 |
| 10 | -1 | 1 | 0 | 0 | 70 |
| 11 | 0 | 0 | -1 | -1 | 70 |
| 12 | 0 | -1 | 0 | 1 | 73 |
| 13 | 0 | 1 | 0 | 1 | 72.9 |
| 14 | 0 | 0 | 1 | -1 | 75 |
| 15 | -1 | 0 | 0 | -1 | 79.7 |
| 16 | 1 | 0 | -1 | 0 | 79 |
| 17 | -1 | -1 | 0 | 0 | 77 |
| 18 | -1 | 0 | 0 | 1 | 76 |
| 19 | 1 | -1 | 0 | 0 | 78.9 |
| 20 | 1 | 0 | 0 | 1 | 80 |
| 21 | 0 | -1 | 0 | -1 | 81.77 |
| 22 | 0 | 1 | 0 | -1 | 86 |
| 23 | 1 | 1 | 0 | 0 | 92 |
| 24 | 0 | 0 | 0 | 0 | 93.9 |
| 25 | 0 | 0 | 0 | 0 | 93 |
| 26 | 0 | 0 | 0 | 0 | 96 |
| 27 | 0 | 0 | 0 | 0 | 94.1 |
| 28 | 0 | 0 | 0 | 0 | 94 |
| 29 | 1 | 0 | 0 | -1 | 98.1 |

Table S6: Various kinetic models for the effect of substrate on growth rate

| Models | Equation | μmax (hr–1) | Ks (mg/L) | Ki | RMSE | AICc | R2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Haldane | μ =μmaxS(S+KS+S^2Ki) eq.(16) | 0.5 | 30 | 100 | 0.009 | -30.9 | 0.95 |
| Han and Levenspiel | μ =μmaxS1-SSmnS+KS-1-SSmm eq.(17) | 1 | 30 |  | 0.022 | -29.02 | 0.91 |
| Luong | μ =μmaxS1-SSmn(S+KS) eq.(18) | 0.7 | 15 |  | 0.05 | -26.4 | 0.90 |
| Aiba | μ=μmaxS exp(- S/Ki) (S + KS) eq.(19) | 1.3 | 10 | 40 | 0.04 | -20.7 | 0.85 |
| Monod | μmax=SKS eq.(20) | 0.9 | 5 |  | 0.23 | -14.2 | 0.53 |

Qmax: Maximal Reduction Rate (h-1)

ks :Half saturation constant for maximal reduction (mg/dm3)

RMS: Residual mean square

Table S7 Comparative study for different biomass-based adsorbents applied for methyl orange adsorption.

| Adsorbents | Removal efficiency/adsorption capacity MO/Cr(VI) | References |
| --- | --- | --- |
| Powdered Rumex abyssinicus | 98.5 % (3.7mg/g) (MO) | (Abewaa et al., 2023) |
| CO3O4 nanoparticles | 15% (46.08 mg/g) MO | (Baig et al., 2020) |
| CuO-ZnO composite | 78% 63.25 mg/g MO | (Najafidoust et al., 2024) |
| Graphene oxide/ZnO | 95% (Cr(VI) (125mg/g) | (Asl et al., 2013) |
| zero-valent iron (S-nZVI) supported on hydrogel | 87.7%(Cr(VI) | (Zhang et al., 2019) |
| PANI@WH composites | 98.5% (31 mg/g)(Cr(VI) | (Kumari et al., 2022) |
| Nnano-magnetic Enteromorpha prolifera hydrogel | 73% (231 mg/g) of MO/ Cr(VI) 54.2 mg/g. 25% | (Yang et al., 2023) |
| GO/ZnO nanocomposites | MO (88%) | (Moradi et al., 2022) |
| Biopolymer chitosan | 78.12 mg g-1 (80%)MO | (Khalil et al., 2021) |
| Jackfruit leaves powder | (78%)MO | (Dutta et al., 2022) |
| GO @Cs-GLA-TiO2 | 277.7 mg/g) of MO/ Cr(VI) 33.89 mg/g | This study |

Table S8 Cost analysis of materials used for adsorption using GO @Cs-GLA-TiO2

| Cost of preparing GO @Cs-GLA-TiO2 for one adsorption | The raw materials used for preparing | Unit price (EGP/kg) | ($/kg) | Amount of raw material required for one adsorption(Kg) |
| --- | --- | --- | --- | --- |
|  | NaOH (99.3%) | 500 | 10 | 100X10-3 |
|  | GO | 1500 |  |  |
|  | Distilled water for washing | 1.08 | 0.0216 | 100X10-3 |
|  | GLA | 2500 | 0.8 |  |
|  | Cs | 600 | 12 |  |
|  | TiO2 | 5000 | 100 |  |
| Cost of electrical energy consumption during drying at 80Oc for 4h($) |  | 3.58 | 0.286 |  |
| The estimated total cost for GO @Cs-GLA-TiO2 ($)+ raw materials cost($) + cost of electrical energy($) |  |  | 0.123 |  |