Table S1: Results of parameters for proximate analysis

| S/N | Sample | Moisture content (%) | Volatile matter (%) | Ash content (%) | Fixed carbon (%) |
| --- | --- | --- | --- | --- | --- |
| 1. | CP | 10.940 ± 0.010ᵃ | 55.000 ± 0.200ᵃ | 5.400 ± 0.020ᶜ | 39.600 ± 0.020ᶜ |
| 2. | SDB | 1.650 ± 0.010ᵇ | 34.000 ± 0.180ᵇ | 7.800 ± 0.020ᵇ | 68.500 ± 0.010ᵃ |
| 3. | CDB | 1.180 ± 0.010ᶜ | 24.000 ± 0.150ᶜ | 9.200 ± 0.010ᵃ | 67.600 ± 0.020ᵇ |
|  | F-value | 302971.000 | 7913.593 | 12311.111 | 900011.111 |
|  | P-value | <0.0001 | <0.0001 | <0.0001 | <0.0001 |

Values are mean ± SE. Means with different superscript letters differ significantly by Tukey HSD at α = 0.05.

CP=Compost, SDB=Sawdust biochar, CDB=Cow Dung biochar

Table S1 shows clear treatment effects on proximate composition. Compost (CP) had the highest moisture content and volatile matter, whereas cow-dung biochar (CDB) had the lowest values for both parameters. CDB had the highest ash content, while CP had the lowest ash content. Sawdust biochar (SDB) had the highest fixed-carbon content, followed by CDB and CP. The very large F-values and p-values below 0.0001 for all four parameters, together with different superscript letters, indicate significant differences among all three materials.

Table S2: Results of heavy metals (mg/kg) concentration in biochar and compost biomass

| S/N | Sample | Zn | Pb | Cd | Cr |
| --- | --- | --- | --- | --- | --- |
| 1. | CP | 0.040 ± 0.010ᵃ | 0.010 ± 0.000ᵃ | 0.001 ± 0.000ᵃ | 0.020 ± 0.010ᵃ |
| 2. | SDB | 0.020 ± 0.010ᵃ | ND | 0.001 ± 0.000ᵃ | 0.020 ± 0.010ᵃ |
| 3. | CDB | 0.020 ± 0.010ᵃ | 0.010 ± 0.000ᵃ | 0.001 ± 0.000ᵃ | 0.010 ± 0.000ᵃ |
|  | F-value | 1.333 | Not estimable | Not estimable | 0.500 |
|  | P-value | 0.3318 | Not estimable | Not estimable | 0.6297 |

Values are mean ± SE. Means with different superscript letters differ significantly by Tukey HSD at α = 0.05.

CP=Compost, SDB=Sawdust biochar, CDB=Cow Dung biochar, ND=No Detection

Table S2 indicates that zinc and chromium concentrations did not differ significantly among the materials (p = 0.3318 and p = 0.6297, respectively). CP had the highest zinc concentration, although its value was statistically comparable with SDB and CDB; CP and SDB also had comparable chromium concentrations. Lead was not detected in SDB, while CP and CDB had equal reported concentrations. Cadmium was identical across the three materials. F- and p-values for lead and cadmium were not estimable because the reconstructed observations had no within-group variation.

Table S3: Results of mineral present in biochar, compost biomass and sand (control)

| S/N | Sample | N (%) | P (mg/kg) | K (mg/kg) | Na (mg/kg) | Ca (mg/kg) | Mg (mg/kg) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1. | CP | 0.020 ± 0.010ᵇ | 12.540 ± 0.010ᵇ | 451.360 ± 0.190ᵃ | 533.360 ± 0.040ᵃ | 168.330 ± 0.030ᵃ | 43.740 ± 0.030ᵃ |
| 2. | SDB | 0.130 ± 0.010ᵃ | 10.080 ± 0.010ᶜ | 383.160 ± 0.160ᶜ | 460.000 ± 0.200ᵈ | 146.280 ± 0.020ᵈ | 40.100 ± 0.020ᶜ |
| 3. | CDB | 0.170 ± 0.010ᵃ | 12.880 ± 0.020ᵃ | 437.920 ± 1.080ᵇ | 519.570 ± 0.140ᵇ | 156.300 ± 0.020ᵇ | 41.320 ± 0.030ᵇ |
| 4. | SA | 0.140 ± 0.010ᵃ | 8.260 ± 0.010ᵈ | 375.360 ± 0.120ᵈ | 496.800 ± 0.020ᶜ | 152.100 ± 0.010ᶜ | 41.320 ± 0.020ᵇ |
|  | F-value | 43.000 | 27134.476 | 4716.600 | 66719.616 | 193749.833 | 3581.949 |
|  | P-value | <0.0001 | <0.0001 | <0.0001 | <0.0001 | <0.0001 | <0.0001 |

Values are mean ± SE. Means with different superscript letters differ significantly by Tukey HSD at α = 0.05.

CP=Compost, SDB=Sawdust biochar, CDB=Cow Dung biochar, SA=Sand (control)

Table S3 shows significant differences among CP, SDB, CDB and sand (SA) for every mineral parameter (all p < 0.0001). CDB, SDB and SA formed the same statistical group for nitrogen, while CP had a lower nitrogen concentration. CDB had the highest phosphorus concentration and SA the lowest. CP had the highest potassium, sodium, calcium and magnesium concentrations, whereas SA or SDB generally had the lowest values depending on the mineral. The superscript letters show the treatment groupings responsible for these significant differences.

Table S4: Results of physical properties of biochar, compost and sand (control)

| S/N | Sample | %Silt | %Clay | %Sand | Textural class |
| --- | --- | --- | --- | --- | --- |
| 1. | CP | 9.800 ± 0.010ᵈ | 4.000 ± 0.010ᶜ | 86.200 ± 0.010ᵃ | Loamy sand |
| 2. | SDB | 15.200 ± 0.010ᵇ | 5.000 ± 0.000ᵃ | 84.200 ± 0.010ᵇ | Loamy sand |
| 3. | CDB | 13.500 ± 0.010ᶜ | 3.100 ± 0.010ᵈ | 83.400 ± 0.020ᶜ | Loamy sand |
| 4. | SA | 16.400 ± 0.010ᵃ | 4.400 ± 0.010ᵇ | 79.200 ± 0.010ᵈ | Loamy sand |
|  | F-value | 82625.000 | 8477.778 | 49580.952 | — |
|  | P-value | <0.0001 | <0.0001 | <0.0001 | — |

Values are mean ± SE. Means with different superscript letters differ significantly by Tukey HSD at α = 0.05. CP=Compost, SDB=Sawdust biochar, CDB=Cow Dung biochar, SA=Sand (control)

Table S4 demonstrates significant differences among the four materials for silt, clay and sand fractions (all p < 0.0001). SA had the highest silt content, SDB the highest clay content, and CP the highest sand content. The sand fraction decreased from CP to SDB, CDB and SA. Despite these numerical differences, all samples were classified as loamy sand, indicating that the textural class itself was common to every treatment.

Table S5: Results of physicochemical parameters of biochar, compost and sand (Control)

| S/N | Sample | ECEC | Organic carbon (% O.C) | Organic matter (%O.M) | pH in H₂O | Exchangeable acidity | pH in KCl |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1. | CP | 6.000 ± 0.010ᵃ | 7.030 ± 0.040ᵃ | 12.120 ± 0.020ᵃ | 8.450 ± 0.010ᵇ | 1.300 ± 0.010ᵃ | 5.600 ± 0.010ᵃ |
| 2. | SDB | 5.140 ± 0.020ᶜ | 5.970 ± 0.010ᵇ | 10.290 ± 0.010ᵇ | 9.600 ± 0.010ᵃ | 1.100 ± 0.010ᵇ | 5.650 ± 0.010ᵃ |
| 3. | CDB | 5.830 ± 0.010ᵇ | 7.030 ± 0.030ᵃ | 12.120 ± 0.020ᵃ | 8.150 ± 0.010ᶜ | 1.250 ± 0.020ᵃ | 5.200 ± 0.020ᶜ |
| 4. | SA | 5.180 ± 0.010ᶜ | 0.480 ± 0.010ᶜ | 0.830 ± 0.010ᶜ | 6.300 ± 0.010ᵈ | 1.050 ± 0.010ᵇ | 5.450 ± 0.020ᵇ |
|  | F-value | 1114.810 | 14591.642 | 117039.200 | 18708.333 | 80.952 | 163.333 |
|  | P-value | <0.0001 | <0.0001 | <0.0001 | <0.0001 | <0.0001 | <0.0001 |

Values are mean ± SE. Means with different superscript letters differ significantly by Tukey HSD at α = 0.05.

CP=Compost, SDB=Sawdust biochar, CDB=Cow Dung biochar, SA=Sand (control)

Table S5 shows significant treatment effects on all measured physicochemical properties (all p < 0.0001). CP had the highest ECEC, while SDB and SA were statistically similar and lower. CP and CDB had comparable organic-carbon and organic-matter values and were higher than SDB and SA. SDB had the highest pH in water, whereas SA had the lowest. CP had the highest exchangeable acidity, and CDB had the highest pH in KCl; the superscripts identify the statistically similar groups for each property.

Table S6:  Results of biological growth of maize plant (Cow Dung biochar and sand)

| S/N | CDB (%) | SA (%) | Height(cm) |
| --- | --- | --- | --- |
| 1 | 50.000 ± 0.000ᵉ | 50.000 ± 0.000ᵃ | 29.920 ± 0.060ᵇ |
| 2 | 75.000 ± 0.010ᶜ | 25.000 ± 0.030ᶜ | 25.150 ± 0.130ᵈ |
| 3 | 65.000 ± 0.030ᵈ | 35.000 ± 0.010ᵇ | 24.870 ± 0.050ᵈ |
| 4 | 85.000 ± 0.110ᵇ | 15.000 ± 0.200ᵈ | 27.920 ± 0.160ᶜ |
| 5 | 90.000 ± 0.070ᵃ | 10.000 ± 0.020ᵉ | 30.740 ± 0.010ᵃ |
| F-value | 71527.778 | 31099.034 | 737.367 |
| P-value | <0.0001 | <0.0001 | <0.0001 |

Values are mean ± SE. Means with different superscript letters differ significantly by Tukey HSD at α = 0.05.

Table S6 shows significant differences among the five plot levels for CDB proportion, SA proportion and maize height (all p < 0.0001). CDB proportion increased from 50% in Plot 1 to 90% in Plot 5, while SA proportion decreased correspondingly from 50% to 10%. Plant height was greatest in Plot 5 and lowest in Plot 3, with the superscript letters indicating that Plots 2 and 3 were statistically similar for height. These results show a strong association between the treatment proportions and the measured growth response.

Table S7:  Results of biological growth of maize plant (Compost biomass and Sand)

| S/N | CDB (%) | SA (%) | Height(cm) |
| --- | --- | --- | --- |
| 1 | 50.000 ± 0.000ᵉ | 50.000 ± 0.000ᵃ | 29.920 ± 0.060ᵇ |
| 2 | 75.000 ± 0.010ᶜ | 25.000 ± 0.030ᶜ | 25.150 ± 0.130ᵈ |
| 3 | 65.000 ± 0.030ᵈ | 35.000 ± 0.010ᵇ | 24.870 ± 0.050ᵈ |
| 4 | 85.000 ± 0.110ᵇ | 15.000 ± 0.200ᵈ | 27.920 ± 0.160ᶜ |
| 5 | 90.000 ± 0.070ᵃ | 10.000 ± 0.020ᵉ | 30.740 ± 0.010ᵃ |
| F-value | 71527.778 | 31099.034 | 737.367 |
| P-value | <0.0001 | <0.0001 | <0.0001 |

Values are mean ± SE. Means with different superscript letters differ significantly by Tukey HSD at α = 0.05.

Table S7 shows significant differences among the five plot levels for CP proportion, SA proportion and plant height (all p < 0.0001). CP proportion increased progressively from 50% to 90%, while SA decreased from 50% to 10%. Plot 5 had the greatest plant height and Plot 1 the lowest; Plots 2 and 4 were statistically similar for height. The superscript groupings confirm that the growth response varied across the compost–sand proportions.

Table S8:  Results of biological growth of maize plant (Sawdust biochar and Sand)

| S/N | CP (%) | SA (%) | Height(cm) |
| --- | --- | --- | --- |
| 1 | 50.000 ± 0.000ᵉ | 50.000 ± 0.000ᵃ | 25.380 ± 0.010ᵈ |
| 2 | 75.000 ± 0.010ᶜ | 25.000 ± 0.010ᶜ | 29.450 ± 0.120ᵇ |
| 3 | 65.000 ± 0.020ᵈ | 35.000 ± 0.010ᵇ | 27.910 ± 0.030ᶜ |
| 4 | 85.000 ± 0.050ᵇ | 15.000 ± 0.030ᵈ | 29.460 ± 0.150ᵇ |
| 5 | 90.000 ± 0.020ᵃ | 10.000 ± 0.010ᵉ | 30.860 ± 0.130ᵃ |
| F-value | 378676.471 | 1072916.667 | 397.205 |
| P-value | <0.0001 | <0.0001 | <0.0001 |

Values are mean ± SE. Means with different superscript letters differ significantly by Tukey HSD at α = 0.05.

Table S8 shows significant differences among plot levels for SDB proportion, SA proportion and plant height (all p < 0.0001). SDB proportion increased from 50% in Plot 1 to 90% in Plot 5, whereas SA declined from 50% to 10%. Plant height was highest in Plots 4 and 5 and lowest in Plot 1; the superscripts show the statistical relationships among plots. The relatively larger standard errors for Plot 3 indicate greater uncertainty in the reconstructed values for that treatment level.

Table S9: Results of uptake of minerals on plant

| S/N | Sample | N (%) | P (mg/kg) | K (mg/kg) | Na (mg/kg) | Ca (mg/kg) | Mg (mg/kg) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1. | CP | 0.480 ± 0.020ᵇ | 3.200 ± 0.010ᵃ | 523.910 ± 0.120ᵇ | 6.900 ± 0.010ᶜ | 64.120 ± 0.010ᵇ | 13.370 ± 0.010ᶜ |
| 2. | SDB | 0.080 ± 0.010ᶜ | 0.220 ± 0.010ᶜ | 82.110 ± 0.010ᶜ | 151.730 ± 0.040ᵃ | 64.120 ± 0.010ᵇ | 14.580 ± 0.010ᵇ |
| 3. | CDB | 2.640 ± 0.020ᵃ | 1.010 ± 0.010ᵇ | 676.400 ± 0.240ᵃ | 18.390 ± 0.010ᵇ | 76.150 ± 0.030ᵃ | 20.660 ± 0.010ᵃ |
|  | F-value | 6321.778 | 23834.333 | 3964084.912 | 10802029.066 | 131564.455 | 152624.333 |
|  | P-value | <0.0001 | <0.0001 | <0.0001 | <0.0001 | <0.0001 | <0.0001 |

Values are mean ± SE. Means with different superscript letters differ significantly by Tukey HSD at α = 0.05. CP=Compost, SDB=Sawdust biochar, CDB=Cow Dung biochar

Table S9 indicates significant differences among CP, SDB and CDB for all mineral uptake parameters (all p < 0.0001). CDB had the highest uptake of nitrogen, potassium, calcium and magnesium, and CP had the highest phosphorus uptake. SDB had the highest sodium uptake. CP and SDB were statistically similar for calcium, while the other superscript groupings show clear treatment separation for most nutrients.

Table S10: Results of physiochemical parameters on Post-harvest plant

| S/N | Sample | Organic carbon (% O.C) | Organic matter (%O.M) | pH in H₂O | pH in KCl |
| --- | --- | --- | --- | --- | --- |
| 1. | CP | 1.980 ± 0.010ᵇ | 3.410 ± 0.010ᵇ | 8.140 ± 0.010ᵃ | 5.450 ± 0.010ᵃ |
| 2. | SDB | 1.960 ± 0.010ᵇ | 3.380 ± 0.010ᵇ | 8.050 ± 0.010ᵇ | 5.150 ± 0.010ᵇ |
| 3. | CDB | 2.240 ± 0.010ᵃ | 3.860 ± 0.010ᵃ | 8.050 ± 0.010ᵇ | 5.100 ± 0.020ᵇ |
|  | F-value | 244.000 | 723.000 | 27.000 | 179.167 |
|  | P-value | <0.0001 | <0.0001 | 0.0010 | <0.0001 |

Values are mean ± SE. Means with different superscript letters differ significantly by Tukey HSD at α = 0.05.

CP=Compost, SDB=Sawdust biochar, CDB=Cow Dung biochar

Table S10 shows significant differences among CP, SDB and CDB for all post-harvest physicochemical parameters. CDB had the highest organic-carbon and organic-matter contents, while CP and SDB were statistically similar. CP had the highest pH in water, with SDB and CDB forming a lower statistical group. CP also had the highest pH in KCl, whereas SDB and CDB were statistically similar. The significant F-values and p-values confirm treatment-related differences in post-harvest soil properties.