Table 1 Parameters of cellulase adsorption on MSL and CEL isolated from biological treated and untreated wheat straw. The adsorption capacity (σ), affinity constant (A) and strength of binding (S) were evaluated by fitting Langmuir isotherm model.

| Lignin isolation | oC | Biomass | Pretreatment | σ (mg/g lignin) | A (L/g) | S=σ×A (mL/g) | Reference |
| --- | --- | --- | --- | --- | --- | --- | --- |
| EnzL | 4 | Poplar | AFEX | 56.8 | 2.14 | 121.6 | Kumar, R. and C.E. Wyman， 2009 |
| EnzL | 4 | Corn stover | DA | 53 | 0.68 | 36.0 | Kuma R and C.E. Wyman 2009 |
| CEL | 50 | Douglas-fir | SO2-steam | 79.3 | 1.86 | 147.5 | Nakagame, S., et al, 2011a |
| CEL | 50 | Lodgepole pine | organosolv | 34.9 | 1.43 | 49.9 | Nakagame, S., et al, 2011 b |
| MSL | 4 | Wheat straw | Untreated | 136.2 | 0.86 | 117.4 | In this study |
| MSL | 4 | Wheat straw | P.chrysosporium | 171.1 | 1.22 | 208.7 | In this study |
| CEL | 4 | Wheat straw | Untreated | 86.9 | 0.75 | 65.3 | In this study |
| CEL | 4 | Wheat straw | P.chrysosporium | 100.4 | 1.02 | 102.4 | In this study |

EnzL, Enzyme lignin

AFEX, Ammonia fiber expansion

DA, dilute acid