Characterization of Lignin Derived from Water-only and Dilute Acid Flowthrough Pretreatment of Poplar Wood at Elevated Temperatures

Libing Zhang 1, Lishi Yan 1, Zheming Wang 2, Dhrubojyoti D. Laskar 1, Marie S. Swita 3, John R. Cort 2*, and Bin Yang1*

_________________________________________

1 Bioproduct Sciences and Engineering Laboratory, Department of Biological Systems Engineering, Washington State University, Richland, WA 99354, USA.

2 Fundamental and Computational Sciences Directorate, Pacific Northwest National Laboratory, Richland, WA 99354, USA.

3 Bioproduct Sciences and Engineering Laboratory, Pacific Northwest National Laboratory, Richland, WA 99354, USA.

* Correspondence: Bin Yang binyang@tricity.wsu.edu; John R. Cort John.Cort@pnnl.gov

Addition file

Table S1 Major GC/MS detected aromatic compounds in hydrolysates

| Major lignin derivatives | Relative abundance |  |  |  |  |  |  | Structure | MW |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 4.2d ACIDa | 4.4d ACIDa | 4.7d ACIDa | 4.5d HWb | 6.0d HWb | 4.8d ACIDc | 5.1 d ACIDc |  |  |
| Vanillin | + | - | - | - | - | + | + |  | 152 |
| Butylated Hydroxytoluene (BHT) | ++ | ++ | ++ | ++ | +++ | ++ | + |  | 220 |
| Phenol, 4-(1,1,3,3-tetramethylbutyl)- | + | + | +++ | + | ++ | +++ | +++ |  | 206 |
| Coniferyl alcohol | - | - | - | - | - | + | - |  | 180 |
| Phenol, 2,2'-methylenebis[6-(1,1-dimethylethyl)-4- | +++ | +++ | +++ | ++ | ++ | +++ | +++ |  | 340 |

a: 0.05%(w/w) H2SO4, 62.5mL/min; b: Water-only, 25mL/min; c: 0.05%(w/w) H2SO4, 25mL/min; d: pretreatment severity factor. +     0－10%; ++      10%－20%; +++     20%－50%; -      not available.

Table S2 Assignments of main lignin 1H- 13C cross-peaks in the HSQC Spectra of the RISLs [1-6]

| Lignin linkages and monolignols | Chemical shift |
| --- | --- |
| -OCH3 | 55.47(C) 3.70(H) |
| A: β-O-4 | 71.70(S-Cα) 4.84(S-Hα) 59.50-59.70(Cγ) 3.40-3.63(Hγ) 85.90(S- Cβ) 4.09(S-Hβ) 83.49(G/H-Cβ) 4.28(G/H-Hβ) |
| B: resinol | 84.85(Cα) 4.62(Hα) 53.30(Cβ) 3.05(Hβ) 70.85(Cγ) 4.14/3.78(Hγ) |
| C: phenylcoumaran | 86.79(Cα) 5.41(Hα) 53.3(Cβ) 3.46(Hβ) 62.52(Cγ) 3.68(Hγ) |
| D: spirodienone | 59.67(Cβ) 3.19(Hβ) |
| G: guaiacyl | 111.02(C2) 6.95(H2) 115.05(G5) 6.74(H5) 119.01(G6) 6.78(H6) |
| G’: oxidized (Cα=O) guaiacyl | 111.56(C2) 7.50(H2) 123.55(C6) 7.54(H6) |
| S: syringyl | 103.95(C2/6) 6.67(H2/6) |
| S’: oxidized (Cα=O) syringyl | 106.52(C2/6) 7.29(H2/6) |
| E: p-hydroxybenzoate | 131.33(C2/6) 7.62(H2/6) |
| F: cinnamyl alcohol | 128.39(Cβ) 6.20(Hβ) 128.59(Cα) 6.42(Hα) |
| K: cinnamaldehyde | 126.23(Cβ) 6.74(Hβ) |

a Note: G, S, H-C or G, S-H refers to C and H in the lignin sub-units, guaiacyl, syringyl and p-hydroxyphenyl.

Figure S1 Gel permeation chromatography (GPC) analysis of flowthrough lignin samples; Red: lignin obtained under 240℃, residence time of 10mins, 0.05% sulfuric acid  and flow rate of 25ml/min (LogR0 ~5.0); Blue: lignin obtained under 270℃, residence time of 10mins, water-only and flow rate of 25ml/min (LogR0 ~6.0)

Figure S2 Assigned interunit linkages of lignin, including different side-chain linkages, and aromatic units: (A) β-O-4 aryl ether linkages; (B) resinol substructures (β-β′, α-O-γ′, and γ-O-α′ linkages); (C) phenylcoumarane substructures (β-5′and α-O-4′ linkages); (D) spirodienone substructures (β-1′ and α-O-α′ linkages); (G) guaiacyl units; (G′) oxidized guaiacyl units with an Cα-ketone; (S) syringyl units; (S′) oxidized syringyl units with a Cα ketone;  (E) p-hydroxybenzoate substructures; (F) alcohol end groups; (K) cinnamaldehyde end groups.

References

1.	Yuan TQ, Sun SN, Xu F, Sun RC: Characterization of lignin structures and lignin-carbohydrate complex (LCC) linkages by quantitative 13C and 2D HSQC NMR spectroscopy. Journal of agricultural and food chemistry 2011, 59(19):10604-10614.

2.	Pu Y, Hallac B, Ragauskas AJ: Plant Biomass Characterization: Application of Solution‐and Solid‐State NMR Spectroscopy. Aqueous Pretreatment of Plant Biomass for Biological and Chemical Conversion to Fuels and Chemicals:369-390.

3.	Del Río JC, Rencoret J, Prinsen P, Martínez AnT, Ralph J, Gutiérrez A: Structural characterization of wheat straw lignin as revealed by analytical pyrolysis, 2D-NMR, and reductive cleavage methods. Journal of agricultural and food chemistry 2012, 60(23):5922-5935.

4.	Wen J-L, Sun S-L, Xue B-L, Sun R-C: Recent advances in characterization of lignin polymer by solution-state nuclear magnetic resonance (NMR) methodology. Materials 2013, 6(1):359-391.

5.	Ralph J, Akiyama T, Kim H, Lu F, Schatz PF, Marita JM, Ralph SA, Reddy MS, Chen F, Dixon RA: Effects of coumarate 3-hydroxylase down-regulation on lignin structure. Journal of Biological Chemistry 2006, 281(13):8843-8853.

6.	Rencoret J, Marques G, Gutierrez A, Ibarra D, Li J, Gellerstedt G, Santos JI, Jimenez-Barbero J, Martinez AT, del Rio JC: Structural characterization of milled wood lignins from different eucalypt species. Holzforschung 2008, 62(5):514-526.