Table S1 Chemical composition of lignocellulosic substrates before and after sodium chlorite delignification
	Substrate
	Composition of raw substrate
	
	Composition of delignified substrate

	
	Glu
	Xyl
	Ara
	Lignin
	
	Glu
	Xyl
	Ara
	Lignin

	Switchgrass
	43.10
	21.88
	2.55
	25.90
	
	50.27
	27.52
	3.93
	2.41

	Jerusalem artichoke stalk
	38.64
	18.05
	4.53
	18.10
	
	46.48
	26.70
	6.12
	1.41

	Miscanthus
	34.71
	17.44
	2.76
	19.19
	
	49.64
	23.37
	3.09
	8.10

	Corn stover
	40.01
	14.60
	2.14
	20.49
	
	45.96
	20.40
	2.69
	9.93
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