Table S1 Chemical composition of lignocellulosic substrates before and after sodium chlorite delignification

| Substrate | Composition of raw substrate |  |  |  |  | Composition of delignified substrate |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Glu | Xyl | Ara | Lignin |  | Glu | Xyl | Ara | Lignin |
| Switchgrass | 43.10 | 21.88 | 2.55 | 25.90 |  | 50.27 | 27.52 | 3.93 | 2.41 |
| Jerusalem artichoke stalk | 38.64 | 18.05 | 4.53 | 18.10 |  | 46.48 | 26.70 | 6.12 | 1.41 |
| Miscanthus | 34.71 | 17.44 | 2.76 | 19.19 |  | 49.64 | 23.37 | 3.09 | 8.10 |
| Corn stover | 40.01 | 14.60 | 2.14 | 20.49 |  | 45.96 | 20.40 | 2.69 | 9.93 |