Table S1. Chemical composition and processing yield of sugarcane bagasse pretreated by an alkaline-sulfite process employing 5% NaOH and 10% Na2SO3

| Sugar cane bagasse sample | Chemical composition (g/100 g of the lignocellulosic material) |  |  | Processing yield (%) | Mass balance of bagasse components (g/100 g of original bagasse) |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Glucan | Hemicellulose | Lignin |  | Glucan | Hemicellulose | Lignin |
| untreated | 42 ± 2 | 26 ± 1 | 24.0 ± 0.1 | 100 | 42 ± 2 | 26 ± 1 | 24.0 ± 0.1 |
| alkaline-sulfite pretreated | 54.7 ± 0.6 | 20.3 ± 0.1 | 14.7 ± 0.5 | 74.9 | 41.0 ± 0.4 | 15.2 ± 0.1 | 11.0 ± 0.4 |