Table S1. Chemical composition and processing yield of sugarcane bagasse pretreated by an alkaline-sulfite process employing 5% NaOH and 10% Na2SO3
	Sugar cane bagasse sample
	Chemical composition
(g/100 g of the lignocellulosic material)
	Processing yield (%)
	Mass balance of bagasse components
(g/100 g of original bagasse)

	
	Glucan
	Hemicellulose
	Lignin
	
	Glucan
	Hemicellulose
	Lignin

	untreated
	42 ± 2
	26 ± 1
	24.0 ± 0.1
	100
	42 ± 2
	26 ± 1
	24.0 ± 0.1

	alkaline-sulfite pretreated
	54.7 ± 0.6
	20.3 ± 0.1
	14.7 ± 0.5
	74.9
	41.0 ± 0.4
	15.2 ± 0.1
	11.0 ± 0.4



