ESI to Biotechnology for Biofuels

Bioprocessing of tea oil fruit hull with acetic acid organosolv pretreatment in combination with alkaline H2O2

Song Tang 1,2, Rukuan Liu 3, Fubao Fuelbiol Sun 1*, Chunying Dong 3, Rui Wang 3, Zhongyuan Gao 1,4, Zhanying Zhang 5, Zhihong Xiao 3, Changzhu Li 3 and Hui Li 3*

1 Key Laboratory of Carbohydrate Chemistry and Biotechnology, Ministry of Education, School of Biotechnology, Jiangnan University, Wuxi 214122, China.

2 State Key Laboratory of Pulp and Paper Engineering, South China University of Technology, Guangzhou 510640, China.

3 National Engineering Research Center for Oil-tea Camellia, Hunan Academy of Forestry, Changsha 410004, China.

4 Key Laboratory of Advanced Textile Materials and Manufacturing Technology, Ministry of Education, Zhejiang Sci-Tech University, Hangzhou 310018, China.

5 Centre for Tropical Crops and Biocommodities, Queensland University of Technology, Brisbane, QLD 4001, Australia.

*Corresponding Author

Fubao Fuelbiol Sun (FFS)

Key Laboratory of Carbohydrate Chemistry and Biotechnology, School of Biotechnology, Jiangnan University, Wuxi 214122, China; fubaosun@jiangnan.edu.cn ;

Hui Li (HL)

Hunan Academy of Forestry, Changsha 410004, China

Email: lihuiluoyang@163.com

Co-authors:

Song Tang (ST), tangsongfuelbiol@163.com

Rukuan Liu (RL), liurukuan@gmail.com

Chunying Dong (CD), 1219921705@qq.com

Rui Wang (RW), gjyoucha@163.com

Zhongyuan Gao (ZG), 490509257@qq.com

Zhanying Zhang (ZZ), jan.zhang@qut.edu.au

Zhihong Xiao (ZX), xzhh1015@163.com

Changzhu Li (CL), lichangzhu2013@aliyun.com

Table title and legend

- PBD experimental design of the AAO pretreatment.

- Analysis of PBD design on optimization of each variables.

- Experimental range and levels of independent variables.

- Full factorial CCD matrix of three variables in coded units and the           experimentally observed response.

- ANOVA results for the quadratic equation for the delignification.

- Model coefficient estimated by multiple linear regression for the delignification.

- Crystalline of the lignocellulosic biomass before and after the two-stage pretreatment.

Tab. S1 PBD experimental design of the AAO pretreatment

| Variables | Symbol | Code levels |  |
| --- | --- | --- | --- |
|  |  | Lower (-1) | Higher (+1) |
| Time (h) | X1 | 0.5 | 2 |
| Acetic acid concentrations (%, v/v) | X2 | 20 | 60 |
| H2SO4 addition (%, w/v) | X3 | 0.2 | 0.7 |
| Pretreatment temperature (°C) | X4 | 115 | 135 |

Tab. S2 Analysis of PBD design on optimization of each variables

| Factors | Cellulose retention |  | Hemicellulose retention |  | Delignification |  | Pretreatment yield |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | T | P | T | P | T | P | T | P |
| X1 | 1.3 | 0.098 | -21.1 | 0.006 | 8.9 | 0.034 | -14.7 | 0.003 |
| X2 | 1.2 | 0.121 | -13.3 | 0.043 | 14.2 | 0.004 | -10.5 | 0.015 |
| X3 | 1.5 | 0.063 | -16.0 | 0.021 | 9.5 | 0.027 | -11.2 | 0.011 |
| X4 | -0.2 | 0.810 | -11.4 | 0.072 | 4.9 | 0.189 | -8.0 | 0.044 |
| Significance of the model | 91.7 | 0.103 | 59.2 | 0.008 | 31.0 | 0.008 | 65.1 | 0.003 |
|  | No significance |  | Significance |  | Significance |  | Significance |  |

T, P and F means coefficient estimate, prob and response significance, respectively

Tab. S3 Experimental rang and levels of independent variables

| Variables | Symbol | Code levels |  |  |
| --- | --- | --- | --- | --- |
|  |  | -1 | 0 | 1 |
| Time (h) | X1 | 1.4 | 1.6 | 1.8 |
| Acetic acid concentrations (%, v/v) | X2 | 45 | 50 | 55 |
| H2SO4 addition (%, w/v) | X3 | 0.51 | 0.58 | 0.64 |

Tab. S4 Full factorial CCD matrix of three variables in coded units and the experimentally observed response

| Run | X1 | X2 | X3 | Delignification (%) |
| --- | --- | --- | --- | --- |
| 1 | 1.9 | 50.0 | 0.58 | 64.5 |
| 2 | 1.6 | 50.0 | 0.58 | 64.0 |
| 3 | 1.6 | 41.6 | 0.58 | 50.4 |
| 4 | 1.8 | 55.0 | 0.51 | 64.8 |
| 5 | 1.8 | 55.0 | 0.64 | 68.7 |
| 6 | 1.6 | 50.0 | 0.58 | 65.4 |
| 7 | 1.8 | 45.0 | 0.64 | 65.0 |
| 8 | 1.4 | 55.0 | 0.51 | 50.2 |
| 9 | 1.6 | 50.0 | 0.58 | 65.5 |
| 10 | 1.6 | 50.0 | 0.58 | 66.1 |
| 11 | 1.8 | 45.0 | 0.51 | 54.0 |
| 12 | 1.6 | 50.0 | 0.58 | 63.2 |
| 13 | 1.6 | 50.0 | 0.47 | 48.7 |
| 14 | 1.4 | 45.0 | 0.64 | 58.9 |
| 15 | 1.4 | 45.0 | 0.51 | 41.6 |
| 16 | 1.6 | 50.0 | 0.68 | 69.1 |
| 17 | 1.4 | 55.0 | 0.64 | 61.7 |
| 18 | 1.6 | 50.0 | 0.58 | 65.5 |
| 19 | 1.6 | 58.4 | 0.58 | 65.3 |
| 20 | 1.3 | 50.0 | 0.58 | 48.7 |

Tab. S5 ANOVA results for the quadratic equation for the delignification

|  | Sum of squares | Freedom degrees | Mean square | F-value | P |
| --- | --- | --- | --- | --- | --- |
| Model | 1217.73 | 9 | 135.30 | 96.21 | < 0.0001 |
| Residual(error) | 14.06 | 10 | 1.41 | Not clear | Not clear |
| Lack of fit | 8.24 | 5 | 1.65 | 1.41 | 0.3566 > 0.1 |
| Pure error | 5.83 | 5 | 1.17 | Not clear | Not clear |
| Total | 1231.79 | 19 | Not clear | Not clear | Not clear |

R2=0.989; CV=1.97%; Adj R2=0.978; Pred R2=0.942; Adeq Precision=34.196

Tab. S6 Model coefficient estimated by multiple linear regression for the delignification

| Term | Coefficient | F-value | P |
| --- | --- | --- | --- |
| Intercept | 64.91 | No clear | No clear |
| X1 | 4.88 | 231.53 | < 0.0001 |
| X2 | 3.74 | 135.54 | < 0.0001 |
| X3 | 5.72 | 317.60 | < 0.0001 |
| X1X2 | 0.40 | 0.91 | 0.3631 |
| X1X3 | -1.74 | 17.27 | 0.002 |
| X2X3 | -1.62 | 14.87 | 0.0032 |
| X12 | -2.79 | 79.84 | < 0.0001 |
| X22 | -2.34 | 56.28 | < 0.0001 |
| X32 | -1.98 | 40.34 | < 0.0001 |

Tab. S7 Crystalline of the lignocellulose before and after the two-stage pretreatment

| Intensity | Crystal size (002) |  | Crystalline (%) |
| --- | --- | --- | --- |
|  | 2θ (°) | Size (nm) |  |
| The original | 21.1 | 1.5 | 21.3 |
| AAO pretreated | 21.8 | 1.9 | 41.3 |
| AAO-AHP pretreated | 21.9 | 3.8 | 52.1 |

Figure title and legend

Figure S1 Predicted values versus experimental values of CCD on the delignification (R2= 0.978).

Figure S2 SEM images of material before and after the AAO and AAO-AHP pretreatment. A, B and C means the original, AAO pretreated and AAO-AHP pretreated substance, respectively.

Figure S3 X-ray diffraction patterns of the substance before and after the AAO and AAO-AHP pretreatment.