Stimulation and inhibition of enzymatic hydrolysis by organosolv lignins as determined by zeta potential and hydrophobicity

Yang Huang1, Shaolong Sun2, Chen Huang1, Qiang Yong1,*, Thomas Elder3,  Maobing Tu2,*

1College of Chemical Engineering, Nanjing Forestry University, Nanjing 210037, China

2Department of Biomedical, Chemical and Environmental Engineering, University of Cincinnati, 2901 Woodside Drive, Cincinnati, Ohio, 45221, United States.

3USDA-Forest Service, Southern Research Station, 521 Devall Drive, Auburn, Alabama 36849, United States

* Corresponding author

Email address: tumg@uc.edu  or swhx@njfu.com.cn

Tel: +1 513 556 2259; or +86 25 85427702

Table S1: Assignments of 13C-1H cross-signals in 2D-HSQC NMR spectra of EOL lignins

Figure S1: Effect of different concentration of added lignin on enzymatic hydrolysis of Avicel

Figure S2: SEM images of EOL lignins

Figure S3: Particle size distribution of EOL lignins

Figure S4: Main structures of EOL lignins: (A) β-aryl-ether units (β-O-4); (B) resinol substructures (β-β); (C) phenylcoumaran substructures (β-5); (G) guaiacyl units; (S) syringyl units; (S′) oxidized syringyl units bearing a carbonyl at Cα; (PB) p-Hydroxybenzoate units.

Table S1 Assignments of 13C-1H cross-signals in HSQC spectra of EOL lignins

| Lables | δC/δH (ppm) | Assignments |
| --- | --- | --- |
| Cβ | 53.0/3.45 | Cβ−Hβ in phenylcoumaran substructures (C) |
| Bβ | 53.5/3.04 | Cβ−Hβin β-β (resinol) substructures (B) |
| −OCH3 | 55.7/3.73 | C−H in methoxyls |
| Aγ | 59.8/3.60 | Cγ−Hγ in β-O-4 substructures (A) |
| Cγ | 62.7/3.71 | Cγ−Hγin phenylcoumaran substructures (C) |
| A′α-OEt | 63.7/3.33 | C−H in α-OEtβ-O-4′ substructures (A′) |
| Bγ | 71.2/3.82−4.18 | Cγ−Hγin β-βresinol substructures (B) |
| Aα | 71.9/4.88 | Cα−Hα in β-O-4 substructures (A) |
| Eα | 78.3/5.57 | Cα−Hα in α,-β-diaryl ethers (E) |
| A′α | 79.9/4.50 | Cα−Hα in α-ethoxylated β-O-4 substructures (A′) |
| Aβ(G) | 83.3/4.29 | Cβ−Hβ in β-O-4 linked to G unit (A) |
| A′β(G) | 82.2/4.39 | Cβ−Hβ in β-O-4 linked to G unit (A′) |
| Bα | 85.1/4.65 | Cα−Hα in β-β resinol substructures (B) |
| Aβ(S) | 86.1/4.14 | Cβ−Hβin β-O-4 linked to a S unit (A) |
| A′β(S) | 84.7/4.20 | Cβ−Hβin β-O-4 linked to a S unit (A′) |
| Cα | 87.2/5.48 | Cα−Hαin phenylcoumaran substructures (C) |
| S2,6 | 103.7/6.68 | C2,6−H2, 6 in syringyl units (S) |
| S′2,6 | 106.5/7.33 | C2,6−H2,6 in oxidized S units (S′) |
| G2 | 111.4/6.95 | C2−H2 in guaiacyl units (G) |
| G5 | 115.0/6.75 | C5−H5 in guaiacyl units (G) |
| G6 | 119.9/6.85 | C6−H6 in guaiacyl units (G) |
| PB2,6 | 131.3/7.62 | C2,6−H2, 6 in p-hydroxybenzoate substructures (PB) |

Fig.S1 Effect of different concentration of added lignin on enzymatic hydrolysis of Avicel

Fig.S2 Scanning electron microscopy (SEM) images of EOL lignins. Lignin preparations were obtained from organosolv pretreated aspen (A), black willow (B), cottonwood (C), eucalyptus (D) and loblolly pine (E).

| A | B |
| --- | --- |
| C | D |
| E |  |
| Fig.S3 Particle size distribution of isolated lignins. Lignin preparations were obtained from organosolv pretreated aspen (A), black willow (B), cottonwood (C), eucalyptus (D) and loblolly pine (E). |  |

Fig.S4 Main structures in the organosolv lignins: (A) β-aryl-ether units (β-O-4); (B) resinol substructures (β-β); (C) phenylcoumaran substructures (β-5); (G) guaiacyl units; (S) syringyl units; (S′) oxidized syringyl units bearing a carbonyl at Cα; (PB) p-Hydroxybenzoate units.