Electronic Supporting Information

The Effect of Liquid Hot Water Pretreatment on the Chemical Structural Alteration and the Reduced Recalcitrance in Poplar

Mi Li 1,2†, Shilin Cao 3†‡, Xianzhi Meng5, Michael Studer 1,4§, Charles E. Wyman1,4, Arthur J. Ragauskas 1,2,5,6*, Yunqiao Pu 1,2*

1 BioEnergy Science Center (BESC), USA

2 Biosciences Division, ORNL, Oak Ridge, TN, USA

3 School of Chemistry and Biochemistry, Georgia Institute of Technology, Atlanta, GA, USA

4 College of Engineering - Center for Environmental Research and Technology (CE-CERT), Bourns College of Engineering, University of California, Riverside, CA

5 Department of Chemical and Biomolecular Engineering, University of Tennessee, Knoxville, TN, USA

6 Department of Forestry, Wildlife, and Fisheries, Center for Renewable Carbon, University of Tennessee Institute of Agriculture, Knoxville, TN, USA

This manuscript has been authored by UT-Battelle, LLC under contract no. DE-AC05-00OR22725 with the U.S. Department of Energy. The publisher, by accepting the article for publication, acknowledges that the United States Government retains a non-exclusive, paid-up, irrevocable, world-wide license to publish or reproduce the published form of this manuscript, or allow others to do so, for United States Government purposes. The Department of Energy will provide public access to these results of federally sponsored research in Accordance with the DOE Public Access Plan (http://energy.gov/downloads/doe-public-access-plan).

† The two authors contributed equally to this work.

‡ S. Cao is currently at College of Material Engineering, Fujian Agriculture and Forestry University, Fuzhou, P. R. China.

§ M. Studer is currently at Laboratory for Bioenergy and Biochemicals, School of Agricultural, Forest and Food Sciences, Bern University of Applied Sciences, Switzerland.

* Correspondence: Arthur J. Ragauskas, aragausk@utk.edu ; Yunqiao Pu, puy1@ornl.gov.

Table S1 Enzymatic hydrolysis results of glucan and xylan after LHW pretreatment

| Time (min) | Severity | Glucan% | Xylan% | Total% |
| --- | --- | --- | --- | --- |
| 0 | 0 | 20.2 | 9.8 | 20.6 |
| 18 | 3.6 | 38.7 | 19.8 | 35.1 |
| 28 | 3.8 | 38.5 | 19.9 | 34.7 |
| 44.0 | 4 | 64.2 | 17.4 | 52.8 |
| 56 | 4.1 | 64.3 | 14.7 | 52.3 |
| 70 | 4.2 | 70.1 | 15 | 57.4 |

Note: the yield presented was saccharification results based on the total glucan/xylan weight contained in the biomass/residues. Enzymatic hydrolysis conditions [1]: enzyme loadings were 15 + 5 to 105 + 35 mg of cellulase (Spezyme CP, protein content 116.0 mg/ml, Genencore, Palo Alto, CA) and xylanase (Multifect Xylanase, protein content 56.6 mg/ml, Genencore), respectively, per gram of glucan and xylan in the raw biomass. All of the resulting samples were incubated at 50°C in a shaking incubator at 150 with a throw of 25 mm (Multitron 2, Infors-HT, Bottmingen, Switzerland) for 72 hours.

Table S2. Original data used for Fig. 1: Chemical composition (wt%) of untreated and LHW pretreated poplar and its corresponded severity. The numbers in parenthesis are standard error of duplicates.

|  | Severity | Ara | Gal | Glc | Xyl | Man | Lignin |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Untreated | 0 | 0.4(0) | 0.7(0.05) | 52.5(5.39) | 12.3(1.21) | 1.9(0.85) | 23.8(0.83) |
| 18 min | 3.6 | 0 | 0.2(0.03) | 67.3(2.21) | 6.2(0.40) | 1.7(0.38) | 21.6(0.01) |
| 28 min | 3.8 | 0.0 | 0.1(0.02) | 69.8(1.24) | 4.7(0.27) | 1.7(0.18) | 21.8(0.78) |
| 44 min | 4 | 0.0 | 0.1(0.08) | 73.0(0.43) | 4.0(0.12) | 1.4(0.27) | 21.6(0.18) |
| 56 min | 4.1 | 0.0 | 0.1(0.06) | 75.5(0.96) | 3.5(0.07) | 1.3(0.15) | 21.4(0.70) |
| 70 min | 4.2 | 0.0 | 0.1(0.05) | 72.4(1.69) | 2.8(0.22) | 1.2(0.11) | 21.3(0.72) |

Table S3 Assignments of the lignin 13C–1H correlation signals observed in the HSQC spectra of the lignins.

| Labels | C/H (ppm) | Assignment |
| --- | --- | --- |
| Bβ | 53.2/3.47 | Cβ/Hβ in β-5' phenylcoumaran substructures (B) |
| Cβ | 53.6/3.06 | Cβ/Hβ in β-β' resinol substructures (C) |
| OMe | 55.5/3.71 | C/H in methoxyls |
| Aγ | 59.8/3.36 & 3.58 | Cγ/Hγ in normal (γ-hydroxylated) β-O-4' substructures (A) |
| Iγ | 59.7/4.01? | Cγ/Hγ in cinnamyl alcohol end-groups (I) |
| Bγ | 62.5/3.75 | Cγ/Hγ in β-5' phenylcoumaran substructures (B) |
| A'γ | 62.8/3.70 | Cγ/Hγ in γ-acylated β-O-4' substructures (A′) |
| Cγ | 701.2/3.80 &4.17 | Cγ/Hγ in β-β' resinol substructures (C) |
| Aα/A'α | 71.5/4.75& 71.9/4.89 | Cα/Hα in β-O-4' substructures (A, A′) -G&-S, respectively |
| A'β(G) | 83.0/4.23 | Cβ/Hβ in γ-acylated β-O-4' substructures linked to a G unit (A′) |
| A'β(S) | 83.3/4.33 | Cβ/Hβ in γ-acylated β-O-4' substructures linked to an S unit (A′) |
| Dα | 81.4/4.74 | Cα/Hα in 5-5' dibenzodioxocin substructures (D) |
| Aβ(G) | 83.4/4.31 | Cβ/Hβ in β-O-4' substructures linked to a G unit (A) |
| Cα | 85.2/4.63 | Cα/Hα in β-β' resinol substructures (C) |
| Aβ(S) | 85.8/4.09 | Cβ/Hβ in β-O-4' substructures linked to an S unit (A) |
| Bα | 87.0/5.46 | Cα/Hα in β-5' phenylcoumaran substructures (B) |
| S2/6 | 103.9/6.65 | C2/H2 and C6/H6 in etherified syringyl units (S) |
| S'2/6 | 106.4/7.26 | C2/H2 and C6/H6 in α-oxidized syringyl units (S′) |
| G2 | 110.9/6.95 | C2/H2 in guaiacyl units (G) |
| PB3/5 | 114.8/6.73 | C3/H3 and C5/H5 in p-hydroxybenzoate (PB) |
| G5 | 115.1/6.75 & 6.98 | C5/H5 in guaiacyl units (G) |
| G6 | 118.8/6.78 | C6/H6 in guaiacyl units (G) |
| PB2/6 | 131.4/7.68 | C2/H2 and C6/H6 in p-hydroxybenzoate (PB) |

Table S4. Relative abundance of lignin subunits and inter-units linkages (% presented on a basis of aromatic abundance S+G).

|  | Untreated | LHW-70 |
| --- | --- | --- |
| S% | 55.5 | 63.4 |
| G% | 44.5 | 36.6 |
| PB% | 14.7 | 7.9 |
| ArH% | 2.4 | 2.3 |
| OMe% | 1.4 | 1.4 |
| S/G | 1.24 | 1.13 |
| β-O-4'% | 55.4 | 43.6 |
| β-5'% | 3. 9 | 4.0 |
| β-β'% | 3.9 | 3.2 |

Note: S: syringyl, G: guaiacyl, PB: p-hydroxybenzoate; ArH: aromatic: OMe: methoxyl; S/G: ratio of syringyl over guaiacyl units.

Table S5 Signal assignment in the 13C NMR quantitative analysis of lignin from BESC Poplar standard.

| C (ppm) | Assignment |
| --- | --- |
| 169.4 | C=O in acetyl |
| 165.6 | C=O in PB |
| 162.0 | PB4 |
| 152.2 | S3/5 etherified |
| 149.3 | G3 etherified |
| 147.5 | G4 etherified |
| 147.0 | S3/5 non-etherified |
| 145.4 | G4 non-etherified |
| 137.9 | S4 etherified |
| 135.0 | S1/G1 etherified |
| 134.5 | S1/G1 etherified |
| 131.3 | PB2/6 |
| 128.6 | H2/6 |
| 121.1 | PB1 |
| 120.4 | H1 |
| 119.4 | G6 |
| 115.2 | G5 |
| 114.8 | PB3/5 |
| 111.8 | G2 |
| 104.6 | S2/6 |
| 87.0 | Cβ in S β-O-4’ threo |
| 85.9 | Cβ in S β-O-4’ erythro |
| 85.1 | Cβ in G/H β-O-4’ threo |
| 83.9 | Cβ in G/H β-O-4’ erythro |
| 72.4 | Cα in G/S β-O-4’ erythro |
| 71.3 | Cα in G/S β-O-4’ threo |
| 63.1 | Cγ in γ-acylated β-O-4’ |
| 61.6 | Cγ in I end group |
| 59.8 | Cγ in β-O-4’ |
| 56.0 | OMe in S/G |
| 53.7 | Cβ in β-β’ |
| 52.2 | Cβ in β-5’ |
| 20.7 | Acetyl |

Table S6. Data used for Fig. 2, Fig. 3, and Fig. 6. Cellulose crystallinity index (CrI), the number-average (DPn) and weight-average (DPw) degree of polymerization of cellulose and hemicellulose, the number-average (Mn) and weight-average (Mw) molecular weights of hemicellulose, and polydispersity index (PDI) of cellulose and hemicellulose. The numbers in parenthesis are standard error of duplicates.

| Severity | Cellulose |  |  |  |  | Hemicellulose |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | CrI% | DPn | DPw | PDI |  | Mn (g/mol) | Mw (g/mol) | DPn | DPw | PDI |
| 0 | 58.6 (1.72) | 266 (18) | 3042 (181) | 11.44 |  | 30760 | 40138 | 205 | 267 | 1.30 |
| 3.6 | 57.5 (1.20) | 172 (0) | 1882 (58) | 10.93 |  | 10510 | 14917 | 70 | 99 | 1.42 |
| 3.8 | 57.8 (0.96) | 158 (2) | 1505 (28) | 9.52 |  | 9047.7 | 13159 | 60 | 88 | 1.45 |
| 4.0 | 58.2 (0.77) | 159 (24) | 1383 (19) | 8.71 |  | 8409.7 | 12179 | 56 | 81 | 1.45 |
| 4.1 | 58.4 (0.66) | 111 (3) | 1116 (46) | 10.07 |  | 7892.1 | 10610 | 53 | 71 | 1.34 |
| 4.2 | 58.8 (0.71) | 125 (15) | 1060 (17) | 8.46 |  | 7980.9 | 10523 | 53 | 70 | 1.32 |

1.	Studer MH, Brethauer S, DeMartini JD, McKenzie HL, Wyman CE. Co-hydrolysis of hydrothermal and dilute acid pretreated populus slurries to support development of a high-throughput pretreatment system. Biotechnol Biofuels 2011, 4(1):19.