### Table S1 Assignment of lignin and polysaccharide correlation signals in the HSQC spectra shown in Fig. 7

| Labels | δC/δH (ppm) |  |  | Assignments |
| --- | --- | --- | --- | --- |
| Lignin cross-signals: |  |  |  |  |
| OCH3 |  | 56.2/3.73 |  | C–H in methoxyls |
| Cβ |  | 56.3/3.44 |  | Cβ-Hβ in phenylcoumaran (C) |
| Bβ β |  | 54.7/3.10 |  | Cβ-Hβ in β-β′(resinol) (B) |
| Aγ |  | 60.2/4.03 |  | Cγ-Hγ in β-O-4′ substructures (A) γ –H γ in β–O–4 substructures γ –H γ in β–O–4 substructures |
| A′γ |  | 63.1/3.34 |  | Cγ-Hγ in γ-acylated β-O-4′ (A′) |
| Bγ |  | 71.2/3.04-3.14 |  | Cγ-Hγ in β-β′ (resinol) (B) γ –H γ in β-β resinol (B |
| Aα |  | 71.7/4.86 |  | Cα-Hα in β-O-4′ substructures (A) |
| Aβ(G) |  | 84.3/4.28 |  | Cβ-Hβ in β-O-4′ linked to G (A) |
| Bα |  | 85.4/4.49 |  | Cα-Hα in β-β′(resinol) (B) |
| A′β(G) |  | 80.7/4.47 |  | Cβ-Hβ in acylated β-O-4′ linked to G (A) |
| Aβ(S) |  | 86.4/4.11 |  | Cβ-Hβ in β-O-4′ linked to S (A) |
| Cγ |  | 63.6/3.88 |  | Cγ-Hγ in phenylcoumaran (C) |
| Iγ |  | 60.2/4.03 |  | Cγ-Hγ in cinnamyl alcohol end-groups (I) |
| Eα |  | 79.7/5.55 |  | Cα-Hα in α, β-diaryl ethers (E) α –H α in α,β-diaryl ethers (E) |
| Cα |  | 87.7/5.57 |  | Cα-Hα in phenylcoumaran (C) |
| S2,6 |  | 104.4/6.70 |  | C2-H2 and C6-H6 in syringyl units (S) |
| S′2,6 |  | 104.7/7.32 |  | C2-H2 and C6-H6 in oxidized S units (S′) |
| G2 |  | 111.6/7.28 |  | C2-H2 in guaiacyl units (G) |
| G5 |  | 115.3/6.72 |  | C5-H5 in guaiacyl units (G) |
| G6 |  | 119.6/6.77 |  | C6-H6 in guaiacyl units (G) |
| H2,6 |  | 128.6/7.23 |  | C2,6-H2,6 in H units (H) |
| PCE3,5 |  | 114.4/6.85 |  | C3,5-H3,5 in p-coumarate |
| PCE2,6 |  | 130.3/7.51 |  | C2,6-H2,6 in p-coumarate |
| PCE7 |  | 144.3/7.49 |  | C7-H7 in p-coumarate |
| FA6 |  | 122.5/7.12 |  | C6-H6 in ferulate |
| Polysaccharide signals: |  |  |  |  |
| X1(R) |  | 99.4/4.63 | C1-H1 in β-D-xylopyranoside or β-D-glucopyranoside (R) |  |
| X′1 |  | 97.1/4.22 | C1-H1 in 2-O-acetyl-β-D -xylopyranoside |  |
| Gl1 |  | 102.2/4.25 | C1-H1 in (1→4) β-D -glucopyranoside |  |