Additional file

Microbial biogas production from hydrolysis-lignin - Insight into lignin structural changes

Daniel Girma Mulata, Janka Dibdiakovab and Svein Jarle Horna*

aFaculty of Chemistry, Biotechnology and Food Science, Norwegian University of Life Sciences, P.O.Box 5003, 1432 Ås, Norway.

bNorwegian Institute of Bioeconomy Research, P.O.Box 115, 1432 Ås, Norway

*Correspondence to: Svein Jarle Horn; E-mail: svein.horn@nmbu.no

3 pages, 1 Table and 1 Figure are included in the supporting material.

Table S1

Assignments of 13C-1H correlation signals in the HSQC spectra of the lignin components in birch.

| Labela | δC/δH (ppm) | Assignments |
| --- | --- | --- |
| Bβ | 53.6/3.04 | Cβ−Hβ in β-β resinol substructures (B) |
| –OCH3 | 55.6/3.71 | C−H in methoxyls |
| Aγ | 59.5/3.69 | Cγ−Hγ in β-O-4' substructures (A) |
| Cγ | 62.3/3.70 | Cγ−Hγ in β-5 phenylcoumaran substructures (C) |
| Bγ | 71.0/3.88-4.17 | Cγ−Hγ in β-β resinol substructures (B) |
| Aα | 71.9/4.85 | Cα−Hα in β-O-4' units (A) |
| BEα | 81.3/4.65 | Cα−Hα in benzyl ether (BE) LCC structures |
| A′α | 83.1/5.21 | Cα−Hα in γ-acylated β-O-4' substructures (A′) |
| Aβ(G) | 83.9/4.33 | Cβ−Hβ in β-O-4' linked to G/H unit (A) |
| Bα | 84.9/4.64 | Cα−Hα in β-β resinol substructures (B) |
| Aβ(S) | 85.9/4.11 | Cβ−Hβ in β-O-4' linked to a S unit (A) |
| Cα | 87.0/5.45 | Cα−Hα in β-5 phenylcoumaran substructures(C) |
| S2,6 | 104.0/6.70 | C2,6−H2,6 in syringyl units (S) |
| S′2,6 | 106.3/7.31 | C2,6−H2,6 in oxidized (Cα=O) S units (S′) |
| G2 | 111.1/6.98 | C2−H2 in guaiacyl units (G) |
| G5 | 114.7/6.71 | C5−H5 in guaiacyl units (G) |
| G6 | 118.9/6.80 | C6−H6 in guaiacyl units (G) |

aThe labels refer to the lignin units and substructures shown in Figures 2 and 3 (main text).

Figure S1 FTIR spectra of untreated (A), steam-exploded (B), HL (C) and HL birch after AD (D).