SUPORTING INFORMATION

Electron Carriers Increase Electricity Production in Methane Microbial Fuel Cells That Reverse Methanogenesis

Ryota Yamasaki1, Toshinari Maeda2 and Thomas K. Wood1*

1Department of Chemical Engineering, Pennsylvania State University,

University Park, Pennsylvania, 16802-4400, USA

2Department of Biological Functions Engineering, Kyushu Institute of Technology,

2-4 Hibikino, Wakamatsu, Kitakyushu 808-0196, Japan

*For correspondence. E-mail twood@engr.psu.edu

Tel.(+)1 814-863-4811; Fax (1) 814-865-7846

Running title:	Electrical carriers increase electricity in methane MFCs

Keywords:     	microbial fuel cells, anaerobic, Geobacter, methane, current density

Calculation for a 560 Ω external resistance or a 0 Ω internal resistance. The highest voltage was obtained in the base case #2 + humic acids MFC which had a maximum voltage of 712.5 mV and maximum current of 366 µA (Fig. 2A). For this case, R (Ω) = 712.5 mV/366 × 10-3 mA = 1,947 Ω, which includes the 1000 Ω external resistance. Therefore, the internal resistance is 947 Ω. The maximum current density in a MFC was obtained with a 560 Ω external resistance [27]. For comparison, if the external resistance of our MFC was 560 Ω, our system resistance would be: R (Ω) = 1,947 – 1000 + 560 = 1,507 Ω. Because voltage that the anode produces does not change, I (µA) = 712.5 mV/1,507 Ω = 473 µA. Because our cathode surface area of cathode is 50 × 10-6 m2, the current density with 560 Ω resistance would be 473 µA/50 × 10-6 m2 = 9.5 A/m2. Also, the power density would be 712.5 mV × 9.5 A/m2 = 6,769 mW/m2. If the internal resistance approaches 0 Ω (i.e., there is only 1000 Ω external resistance), the current would be 795.9 µA (= 795.9 × 103 µV/1000 Ω). Because our cathode surface area is 50 × 10-6 m2, the current density would be 795.9 µA/50 × 10-6 m2 = 15.9 A/m2. Also, the power density would be 0.8 V × 15.9 A/m2 = 12.7 W/m2.

Electric energy available in the methane MFC. A 155 mL bottle is used for the anode, and it is filled with 100 mL of culture; hence, there are 55 mL of headspace filled with methane, which is 1.5 × 1021 molecules [1 mol of gas is 22.4 L at standard conditions, so 0.055 L/(22.4 L/mol) x 6.022 × 1023 molecules/mol].

For the anode reaction, 4CH4 + 2HCO3− → 3CH3COO− + 8e− + 9H+; hence, 1 mole of methane can produce 2 mole of electrons. So, if all the methane reacts, 3.0 × 1021 electrons are produced.

In our MFC, the maximum current is approximately 366 µA. 366 µA = 366 µC/s. 1 electron = 1.6 × 10-19 C. So, (366 µC/s)/(1.6 × 10-19 C) = 2.3 × 1015 electrons react/s at the cathode. Hence, the amount of time the MFC can provide power is (3.0 × 1021 electrons)/(2.3 × 1015 electrons/s) = 1.3 × 106 s or 15 days.

Our best MFC produced 713 mV and 366 × 10-6 A. Hence, the electric power may be calculated as P = V × I = 713 × 10-3 V × 366 × 10-6 A = 256 µW. The power density may be calculated as P divided by surface area of cathode electrode (50 × 10-6 m2) = 261 × 10-6 W/50 × 10-6 m2 = 5,216 mW/m2. The total energy may be calculated as W = V × I × t = 713 × 10-3 V × 366 × 10-6 A × 1.3 × 106 s = 339 W·s (or 339 J). Hence, our MFC can produce 256 µW of power for 15 days and contains a total of 339 J of energy.

Table S1. Composition of HSNR medium.

| Chemical | Final concentration (mM) | Chemical | Final concentration (mM) |
| --- | --- | --- | --- |
| NaCl | 400 | Puromycin dihydrochloride | 0.0037 |
| MgCl2.6H2O | 54 | aCoSO4.7H2O | 0.0036 |
| NaHCO3 | 45 | aFeSO4.7H2O | 0.0036 |
| NH4Cl | 19 | bLipoic acid | 0.0024 |
| KCl | 13 | aBoric acid | 0.0016 |
| KH2PO4 | 5.0 | bThiamine hydrochloride | 0.0015 |
| Cysteine.HCl | 3.2 | bRiboflavin | 0.0013 |
| CaCl2.2H2O | 2.0 | bPantothenic acid (Ca salt) | 0.0010 |
| Na2S.9H2O | 1.0 | aNa2MoO4.2H2O | 0.0010 |
| aMgSO4.7H2O | 0.10 | aNiCl2.6H2O | 0.0010 |
| aNitrilotriacetic acid | 0.079 | bBiotin | 0.00082 |
| aMnSO4.H2O | 0.030 | bFolic acid | 0.00045 |
| aZnCl2 | 0.0059 | aCuSO4.5H2O | 0.00040 |
| bPyridoxine hydrochloride | 0.0049 | aKAl(SO4)2.12H2O | 0.00021 |
| bNicotinic acid | 0.0041 | bVitamin B12.HCl | 0.0000074 |
| bp-Aminobenzoic acid | 0.0037 |  |  |

aTrace element solution, bVitamin solution

Table S2. Resistance (Ω) for base case #1 with additional components. These resistances occurred during the time of maximum voltage and current.

| Base case #1 | Base case #1 + cysteine-HCl (16 mM) | Base case #1 + Na2S (5 mM) | Base case #1 + Sodium acetate (10 mM) | Base case #1 + Humic acids (0.5 %) | Base case #1 without cysteine-HCl |
| --- | --- | --- | --- | --- | --- |
| 2,398 | 35,168 | 46,719 | 4,803 | 2,225 | 4,885 |